## Slide 1: Multimodal Options for Materials Research to Advance the Basis for Fusion Energy in the ITER Era
Steve Zinkle1, Anton Möslang2, Takeo Muroga3, Hiro Tanigawa4
1Oak Ridge National Laboratory, Oak Ridge, Tennessee, USA
2Karlsruhe Institute for Technology, Eggenstein-Leopoldshafen, Germany
3National Institute for Fusion Science, Toki, Gifu, Japan
4Japan Atomic Energy Agency, Aomori, Japan
24th IAEA Fusion Energy Conference
San Diego, California October 8-13, 2012
Notes: SDM meeting July 10-11, 2001
1

## Slide 2: Why Multimodal Research Options?
Although current international fusion energy roadmaps have many common elements, there are also some key differences
  Time schedule, post-ITER facility R&D objectives (FNSF, DEMO, etc.), degree of aggressiveness in DEMO design, scientific discovery vs. engineering confirmation emphasis, etc.
Japan fusion roadmap
IFMIF irradiation
ITER-TBM Operation
Design activity
ITER Q>10 steady state operation
2020~2025
~ 2030
~ 2040
★Material specification
★Draft Fusion design code
~ 2020
~ 2050
★Final Fusion design code
Note: This is the digest version of the technical roadmap studied by Roadmap working group organized under ITER/BA technology advisory committee of Fusion energy forum of Japan (and further modified to include recent ITER schedule changes), and is NOT the roadmap authorized by Japanese government.

## Slide 3: Why Multimodal Research Options? (cont’d)
(TL = TBM Leader)
HCLL : Helium-cooled Lithium Lead, HCPB : He-cooled Pebble Beds (Ceramic/Beryllium)
WCCB : Water-cooled Ceramic Breeder (+Be), HCCR : Helium Cooled Ceramic Reflector
HCCB : He-cooled Ceramic Breeder (+Be), LLCB : Lithium-Lead Ceramic Breeder (He/LiPb)
Every fusion blanket and materials system has shortcomings; there is no utopian solution
  Multiple blanket systems are being explored in an effort to identify at least one viable blanket concept
  E.g., 6 blanket concepts are being proposed for exploration on ITER (not including DCLL concept, etc.)
M : Thermal Stress factor
λ： thermal conductivity
σ： tensile strength
ν： Poisson ratio
α： thermal expansion coeff.
Ｅ ： Young’s modulus
Brittleness
Ferromagnetic
Reactive

## Slide 4: Parameter regimes under investigation in US/JP program on structural materials for fusion

## Slide 5: Current status and recent highlights for fusion materials
Reduced activation ferritic martensitic steels are the leading fusion structural material option worldwide, due to good properties, generally favorable fission neutron irradiation resistance, and extensive industrial capability
  Key uncertainties include ductile-brittle transition temperature (DBTT) increase due to fusion H, He effects and dose limits in fusion neutron environment
  Risk mitigation options include oxide dispersion strengthened (ODS) steels and new ferritic/martensitic steels with a very high precipitate density designed with computational thermodynamics tools.
Notes: RAFM is equivalent to the Tokamak in plasma physics; Gen IV steels are equivalent to AT or ST versions
ODS steels are akin to stellarators
SiC/SiC are akin to other advanced configuration concepts (RFPs, etc.)

## Slide 6: Provisional temperature and dose regimes for radiation-induced embrittlement of current fusion grades of ferritic/martensitic steels have been identified
M.A. Sokolov ICFRM15 and H. Tanigawa
Lower operating temperature limit due to neutron embrittlement is ~300oC
Steels with modified thermomechanical treatment can offer slightly improved DBTT
Tirr=
Fission neutron irrad. (<5 appm He)
Notes: Radiation-induced DBTT shifts are large for irradiation temperatures of 300C and lower. Modifications in the microstructure of RAFM steels can mitigate the DBTT shift by ~50C.

## Slide 7: Effect of fusion-relevant He production on ferritic/martensitic steels is being investigated using simulation techniques
Good resistance to simulated fusion irradiation environment observed up to ~20 dpa
Open question: Are B-doping and He-injector (Ni foil) simulation tests prototypic for actual fusion reactor condition?
Significant void swelling observed in ferritic/martensitic steel after 1400 appm He and 25 dpa at 500°C (56 appm/dpa)
G.R. Odette (ICFRM-15); He injection from Ni foil during fission reactor irradiation
EUROFER, <10 appm He
EUROFER, 10-500 appm He
E. Gaganidze et al., KIT
Notes: Co-production of fusion-relevant He can enhance void swelling ((0.5% in left hand photo)

## Slide 8: Status and recent highlights: SiC/SiC composites
Fission reactor irradiation stability up to 40 dpa recently confirmed for SiC/SiC composites at 800oC
Scoping low dose irradiation studies on SiC joints found no degradation
Outstanding issues include improvements in leak-tightness and fabrication (complexity and cost) and development of structural design criteria
Data from recent US/J HFIR study
Notes: SiC/SiC are akin to other advanced configuration concepts (RFPs, etc.)

## Slide 9: Status and recent highlights: V alloys and coatings
Higher strength V alloys have been demonstrated using mechanical alloying approach
New processes for fabricating Er2O3 and Y2O3 MHD insulator and T2 barrier coatings are being developed (suitable for coating complex geometries)
(Chikada, Shimada, J-US TITAN Program)
100-1000x
0
2
4
6
8
10
12
14
16
0
200
400
600
Mechanical Alloying
Cold-work and precipitation
Standard
Stress/MPa
Strain/%
700
o
C
Li temperature (oC)
Notes: V alloys and SiC/SiC are akin to other advanced configuration concepts (RFPs, etc.)

## Slide 10: Status and recent highlights: Tungsten
Hot wall operation introduces several new phenomena
  e.g., Nanofuzz surface formation during plasma exposure
R.P. Doerner, UCSD

## Slide 11: Status and recent highlights: Tungsten (cont’d)
Hot wall operation introduces several new phenomena
  enhanced D/T retention after neutron irradiation (due to trapping at defect complexes)
Neutron irradiation in HFIR
D plasma exposure in TPE
Thermal desorption
Hatano et al. FTP 4-1 (Friday)
Calculated fraction of hydrogen that is trapped in the vicinity of a 2 nm radius He bubble in tungsten at 900 K (B.D. Wirth).
Modeling
Experiment
Desorption experiments on W neutron-irradiated at high temperature are scheduled to be performed in the near future
Tirr~70oC

## Slide 12: H retention increases dramatically in the presence of cavity formation
500-700 appm H
(few cavities)
F.A. Garner et al., J. Nucl. Mater. 356 (2006) 122
Baffle-former bolt removed from Tihange-1 (Belgium) pressurized water reactor
Type 316 austenitic stainless steel
1700-3700 appm H
(rad.-induced cavities present)
3 to 5x increase in retained hydrogen when cavities are present, even with 2-3x reduction in neutron fluence exposure
Retained H level is ~100x higher than expected from Sievert’s law solubilities
Notes: Note: 1000 appm corresponds to 5 kg Tritium per 100 tonnes of steel
Note FFTF samples in contact with Na (H solubility equipartition coefficent of 170-320 for Ni and Fe at 500C, respectively) still had retained H contents of 320-570 appm in 316 SS samples with ~0.3 to 8% cavity swelling; also note that Na H content was maintained at 1ppm H by cold trapping.
I presume Sieverts law curves for Fig. 6 in Garner paper were generated by assuming 1 atm H pressure & then multiplying bulk H solubility by volume fraction of cavities (CH~d^3)

## Slide 13: 3 High-Priority Materials R&D Challenges
Is there a viable divertor & first wall PFC solution for DEMO/FNSF?
  Is tungsten armor at high wall temperatures viable?
  Do innovative divertor approaches (e.g., Snowflake, Super-X, or liquid walls) need to be developed and demonstrated?
Can a suitable structural material be developed for DEMO?
  What is the impact of fusion-relevant transmutant H and He on neutron fluence and operating temperature limits for fusion structural materials?
  Is the current mainstream approach for designing radiation resistance in materials (high density of nanoscale precipitates) incompatible with fusion tritium safety objectives due to tritium trapping considerations?
  Is the reduced activation mandate too restrictive for next-step devices, considering that ITER will utilize materials that are not reduced activation?
  Can recent advanced manufacturing methods such as 3D templating and additive manufacturing be utilized to fabricate high performance blanket structures at moderate cost that still retain sufficient radiation damage resistance?
What range of tritium partial pressures are viable in fusion coolants, considering tritium permeation and trapping in piping and structures?
  What level of tritium can be tolerated in the heat exchanger primary coolant, and how efficiently can tritium be removed from continuously processed hot coolants?

## Slide 14: Urgency for a high-intensity fusion-relevant neutron source
The second materials R&D challenge and parts of the 1st and 3rd R&D challenge listed above require an intense neutron source for their resolution.
  Scientific studies of radiation degradation phenomena and tritium trapping issues in candidate HHF/blanket materials exposed to prototypical fusion operating environment.
Obtaining engineering data from an intense fusion neutron source is a significant critical path item for DEMO design and licensing
  Prioritize research on a limited number of DEMO material and blanket concepts (e.g., is ODS steel or another special material required?)

## Slide 15: Void Swelling is typically maximized when the cavity and dislocation sink strengths are comparable
E.H. Lee & L.K. Mansur, Met. Trans. A 21 (1990) 1021
High He/dpa ratio
(e.g., spallation neutrons)
Moderate He/dpa ratio
(e.g., DT fusion neutrons)
low He/dpa ratio
(e.g., fission neutrons)
Notes: Low swelling values at balanced sink condition are associated with very high cavity densities that cause a delay in bubble to void conversion

## Slide 16
Recent in situ He injector study during fission reactor (HFIR) irradiation suggests void swelling may emerge as an issue at ~25 dpa for ferritic/martensitic steels
MA957 (ODS steel) and Eurofer97 9%Cr ferritic/martensitic steel
Eurofer97: 7.5x1022 cavities/m3 with bimodal size distribution (1.3 nm bubbles & 5 nm voids - precursor to significant swelling)
MA957: 7.8x1023 bubbles/m3 & no voids
Eurofer97
MA957 ODS steel
Odette et al. ICFRM-15, Charleston, South Carolina
1400 appm He and 25 dpa at 500°C (56 appm/dpa)
Notes: ∆V/V~0.5% for Eurofer; many bubbles have converted to voids; cavity sink strength is ~2*pi*d*N~1.5e15/m2, which is somewhat higher than dislocation sink strength.
He/dpa is ~5 times higher than fusion-relevant value

## Slide 17: There are several options to close the current knowledge gap in fusion-relevant radiation effects in materials
Fusion
reactor
Current knowledge base on ferritic steels
Option A: IFMIF + fission reactors +ion beams + modeling
Option B: robust spallation (e.g., MTS) + fission reactors + ion beams + modeling
Option C: modest spallation (e.g.,SNS/SINQ) + fission reactors + ion beams + modeling
An intense neutron source (in concert with enhanced theory and modeling) is needed to improve understanding of basic fusion neutron effects and to develop & qualify fusion structural materials
Notes: Massively parallel computing will also play an important role
ITER DT results on TBM components would only be available after 2030

## Slide 18: Comparison of Gen IV and Fusion Structural Materials Environments
fusion
SiC
V alloy, ODS steel
F/M steel
All Gen IV and Fusion concepts pose severe materials challenges
S.J. Zinkle & J.T. Busby, Mater. Today 12 (2009) 12
S.J. Zinkle ,OECD NEA Workshop on Structural Materials for Innovative Nuclear Energy Systems, Karlsruhe, Germany, June 2007

## Slide 19: Timeline of some key events for nuclear energy and materials and computational science
1940
1950
1960
1970
1980
1990
2000
2010
CP-1
Graphite
Shippingport
Development of Mat. Sci.
as an academic discipline
reactor
JET: Q=0.65, 0.5s
1 Gflops achieved;
high performance
computing centers
established
1 Tflops
1 Pflops
Nuclear >10% US electricity
ENIAC
Tokamak era begins
ITER
NIF
1st stellarator
& Tokamak
1st MD simulation of radiation damage
(500 atoms, 1 min. time step)
multimillion atom MD simulations
(~1 fs time step)
TFTR: Q=0.27
JT-60: Qeq=1.25
Notes: 1968: T3 Tokamak at Kurchatov Inst. In Russia (Tokamak concept originally designed in 1951; T1 tokamak first became operational in 1958)
1st MD simulations of radiation damage by BNL group (G.H. Vineyard and coworkers)
JT60: DT-equivalent Q of 1.25 was obtained using DD plasma (highest recorded Q for DT plasma was 0.65 in JET)
TFTR: max fusion power=10.7 MW; JET max fusion power=16MW

## Slide 20: Detailed timeline of some key facilities for nuclear energy and materials
1942
1944
1946
1948
1950
1952
1956
1958
CP-1
Shippingport
ORR
Obninsk AM-1
1st radiation damage paper
E.P. Wigner
J. Appl. Phys. 17 (1946) 857
1954
MTR
BSR
Graphite reactor
ETR
Calder Hill
CP-5
BGRR
Notes: Note: ~30 reactor piles were constructed at Columbia University by Fermi, Szilard and coworkers in 1941-1942 (with improving material impurity, etc.) prior to the Chicago Pile
1946: Eugene Wigner advocates construction of a high flux test reactor for nuclear physics research AND radiation effects on materials
Note evolution in reactors from physics to materials research and technology (e.g., shielding) missions; similar evolution also occurred in accelerators (X-section measurements, then radiation effects studies)
EBR-I: 1st electricity-producing nuclear power plant (Dec. 20, 1951); operated until 1964.
52 reactors have been built to date at the Idaho test site; 3 were specifically dedicated to materials radiation effects research (MTR, ETR, ATR)
As of 1959 there were at least 7 materials test reactors available with the correct neutron spectrum for performing materials irradiation tests

## Slide 21: Contribution of major facilities to Materials degradation science and technology issues
Red: TRL 1-3 issues
Yellow: TRL 4-6 issues
Green: TRL 7-9 issues
ITER-
TBM
FNSF
Demo
Fusion-relevant neutron source
Non-nuclear test stands
after DOE/SC-0149 (2012); ITER TBM column revised/corrected by materials degradation subpanel
Ion & fission irrad.
Notes: Several items for the ITER TBM column have been revised upward relative to the FESAC report (FESAC report column was initially prepared for ITER, not for ITER TBM).

## Slide 22: Conclusions
Substantial progress continues to be made in understanding and developing high-performance fusion structural materials.
  Ferritic/martensitic steels appear to be suitable for fusion doses up to ~20 dpa
  Higher performance options (e.g., ODS steels) may offer significantly better radiation resistance, but joining technology and others issues need to be resolved.
In order to accelerate the pace for developing practical fusion energy, the construction of an intense fusion neutron source is needed.
  Tritium retention (fusion safety)
  Viability of blanket and first wall structural materials
  Engineering database activities for design and licensing purposes, when a viable candidate has been identified