## Slide 1
S. Brezinsek
T. Loarer
V. Phillips
H.G. Esser
S. Grünhagen, R. Smith
R. Felton, U. Kruezi and JET-EFDA contributors
Fuel Retention Studies with the ITER-like Wall in JET
IAEA 24th Fusion Energy Conference / San Diego / 8.-13. October 2012

## Slide 2: Contributors
S. Brezinsek1, T. Loarer2, V. Philipps1, H.G. Esser1, S. Grünhagen3, R. Smith3, R. Felton3
U. Kruezi1, J. Banks3, P. Belo4, J. Bucalossi2 , M. Clever1, J.W. Coenen1, I. Coffey5, D. Douai2
M. Freisinger1, D. Frigione6 , M. Groth7, A. Huber1, J. Hobirk8, S. Jachmich9, S. Knipe3
G.F. Matthews3, A.G. Meigs3, F. Nave4, I. Nunes4, R. Neu8, J. Roth8, M.F. Stamp3
S. Vartagnian2, U. Samm1 and JET EFDA contributors
1Institute of Energy and Climate Research - Plasma Physics, Forschungszentrum Jülich,
Association EURATOM-FZJ, Trilateral Euregio Cluster, 52425 Jülich, Germany
2CEA, IRFM, F-13108 Saint-Paul-lez-Durance, France
3EURATOM/CCFE Fusion Association, Culham Science Centre, Abingdon, OX143DB, UK
4Institute of Plasmas and Nuclear Fusion, Association EURATOM-IST, Lisbon, Portugal
5Queen's University Belfast, BT71NN, UK
6Associazione EURATOM-ENEA sulla Fusione, CP 65, Frascati, Rome, Italy
7Aalto University, Association EURATOM-Tekes, Espoo, Finland
8Max-Planck-Institut für Plasmaphysik, EURATOM Association, D-85748 Garching , Germany
9Association EURATOM-Belgian State, ERM/KMS, B-1000 Brussels, Belgium
Main author contact:
S.Brezinsek@fz-juelich.de

## Slide 3: Outline
Motivation: Limitation in long term fuel retention in ITER
Retention mechanisms and measurement techniques
Experimental results with the ITER-like Wall in JET
Conclusions for ITER

## Slide 4: Material Combinations in ITER
ITER
Beryllium
Tungsten
Carbon
http://www.iter.org/
Critical issues: safety and lifetime
„or“ fuel retention and first wall erosion
Fuel retention predictions made on basis of CFC devices, laboratory experiments and modelling
Benchmark tokamak experiment required
~1 year full DT
operation
J. Roth et al.
JNM 2009
ITER

## Slide 5: Metallic Walls: ITER-Like Wall at JET
Expected change in operational space
  Better plasma control required
  Heat load mitigation schemes required
ITER-material mix used for the first in a tokamak
Expected “carbon-free” environment
  Reduced migration to remote areas
  Reduced tritium retention in codeposits
  Loss of carbon as main radiator
Demonstrate low fuel retention, migration
and possible fuel recovery
Demonstrate plasma compatibility
with metallic walls
Main goals of the ILW experiment
Compare ILW experiments with carbon walls
Input to the decision about the first ITER divertor
Tungsten
Beryllium
JET ITER-Like Wall
E. Joffrin Ex1/1

## Slide 6: Residual C-content with the JET-ILW
Main chamber CIII and outer divertor CII edge fluxes:
Residual C dropped with ILW installation by one order of magnitude (statistical)
Dedicated JET-C/JET-ILW comparison pulses show a drop of about a factor 20
Comparable C reduction also observed in core and edge concentrations by CXRS
Typical Be core concentration about 2% (comparable averaged level to C in JET-C)
Averaged Zeff dropped from 1.9 (JET-C) to 1.2 (JET-ILW)
CC=0.50%
CC=0.05%
x20
Comparison pulses: JET-CFC vs. JET-ILW
S. Brezinsek et al.
PSI 2012
J. Coenen EXP/P5-04

## Slide 7: Retention Mechanisms
At JET wall temperature:
fuel content in laboratory Be layers one order lower than in C layers!
Dynamic retention: mostly recovered by outgassing in between pulses
Long term retention: remains in walls and global gas balance provides upper limit
J. Roth et al.
JNM 2009
Codeposition

## Slide 8: Retention Measurement Techniques
Intershot
gas balance
Global
gas balance
Post mortem
analysis
Single discharge only
Transient effect
Short-term retention
Multiple identical discharges
Includes inter-shot outgassing
Long-term retention (1 day)
All discharges of a campaign
Includes outgassing in
campaign / intervention
Long-term retention (1 year)
Gas
injected
Gas recovered
Gas
retained
This contribution:
Upper limit of D remaining in vessel
Expected in 2013:
D remaining in vessel
in codeposits and implantation
JET-C with W test stripe
on outer target plate
P. Coad et al.
Phys. Scripta 2012
Safety Aspect: Tritium Inventory
Gin
Gout
ne
npres
fDa

## Slide 9: Global Gas Balance Measurements
Calibrated particle source
(here: gas injection modules)
Gas collection on divertor cryo pumps
Fuel retention:
long (co-deposition and implantation) +
short term (surface)
Repeat sets identical discharges
Typical: 10-35 => one day of operation
Injected gas = Pumped gas+ Short term retention + Long term retention
Regeneration of cryogenic pumps before and after experiment
T. Loarer, V. Philipps
JNM 2010, PSI 2012
Variant 1: ohmic / L-mode => divertor cryo pumps only – rest closed (standard)
Variant 2: higher statistics / L-mode => turbo molecular pumps only – rest closed
Variant 3: H-mode => divertor and NBI cryo pumps => fraction of gas pumped by NB cryo is
calculated from pumping speed ratio with divertor cryo pump
Better than 1.2% measured in mulitple reference calibrations
with temperature monitoring at gas injection side
Precision:

## Slide 10: Global Gas Balance Measurements
Calibrated particle source
(here: gas injection modules)
Gas collection on divertor cryo pumps
Fuel retention:
long (co-deposition and implantation) +
short term (surface)
Injected gas = Pumped gas+ Short term retention + Long term retention
Regeneration of cryogenic pumps before and after experiment
General observation of JET-C vs. JET-ILW comparison:
Stronger gas consumption during limiter phase and stronger outgassing after end of the discharge in comparison with JET-C => JET-ILW dynamic retention higher
High purity of recovered gas of more than 99% D => absence of hydrocarbons in later phase
Strong reduction of integrated retention by gas balance measured over one day
=> Long term retention one order magnitude lower in JET-ILW than in JET-C
Repeat sets identical discharges
Typical: 10-35 => one day of operation
T. Loarer, V. Philipps
JNM 2010, PSI 2012

## Slide 11: Normalisation and Fuel Retention Rates
Example: L-mode plasma experiment
-Ip
PICRH
Gas
fDa
(In Div)
Heating time~12s
Divertor time ~19s
#81973
0
5
10
15
20
25
Balance: particles retained = Injected particles - recovered particles
Time normalisation: time with main particle flux to divertor PFCs
time [s]
L-mode
34 discharges
646 s divertor time
without divertor
cryogenic pump
MA
105 W
1021 e s-1
1019 ph
s-1m-2 sr-1

## Slide 12: Long Term Fuel Retention: Experiments
Long term fuel retention rate below 1.5x1020Ds-1 (w.r.t. to divertor operation time / all scenarios)
Moderate increase of retention rate with divertor flux
Retention rate reflects the upper limit as long term outgassing reduces the inventory further
Direct comparison of JET-C and JET-ILW possible for low power discharges => for high power discharges inter-shot outgassing time is twice as long for JET-ILW
Reduction

## Slide 13: Example: type III ELMy H-mode
Comparison discharges JET-C vs. JET-ILW:
Type III ELMy H-mode at Bt=2.4T
Main and edge plasma conditions are
comparable in JET-C and JET-ILW
Change of auxiliary heating required
Shorter limiter phase in JET-ILW
Retention rate drop:
JET-C => JET-ILW
1.37x1021 Ds-1 => 7.2x1019 Ds-1
JET-ILW experiment:
18 discharges
Divertor time: 317 s
Injected D2: 2495 Pam3
Retained D2: 47 Pam3
Normalisation to T=293.15K gas temperature

## Slide 14: Last Experiment before Tile Intervention
151 comparable discharge in H-mode
(Ip=2.0MA, Bt=2.4T, Zeff=1.2, Paux=12MW)
High reproducibility of discharges
2500 s plasma in divertor configuration
Time between discharges ~55 min
Divertor fluence: 5.25x1026 Dm-2
corresponds to ¼ ITER pulse
3 dedicated gas balances over 1 day
with comparable retention rates
Comparable retention to mid-campaign gas balance experiment

## Slide 15: Fuel Retention in ITER
Assumption: quasi steady-state conditions reached and co-deposition process dominates
Comparison with ITER predictions by Roth et al.: from hypothetical all-C to Be/W material mix
Simple comparison: factor 4 in absolute value of retention rate between JET and ITER
JET measured upper limit of 1.5x1020Ds-1 translates to 3.0x1020Ts-1 in D:T mixture
Significant increase of number of ITER-discharges before cleaning is required (>1250)
JET shows in the covered range of plasma conditions the same trend in reduction: comparable reduction in retention rate from all-C to Be/W plasma-facing component mix
Scaling in particle flux to PFCs would lead to further increase
Long term outgassing will lead to a reduction of retention in PFCs by a factor ~4-5
=> Detailed JET modelling comparable to Roth predictions for ITER started
JET (exp.)
ITER (model.)
all C: 1.0-3.0x1021 D/s
all C: 0.4-1.2x1022 D/s
Be/W: 0.5-1.5x1020 D/s
Be/W: 2.0-6.0x1020 D/s
:10-20
:20
Roth et al. JNM 2009
Notes: Number of discharges before cleaning interverntion from Roth (median):
75 (all C)
250 (C/Be/W)
2500 (Be/W)

## Slide 16: Summary
Experiments with global gas balance executed in JET with Be/W material mix
Reduction in retention rate by one order of magnitude from JET-C to JET-ILW
Robust result of upper limit of the long term retention rate of 1.5x1020Ds-1
Higher dynamic retention and outgassing with metallic walls observed
Post-mortem analysis results expected for 2013, but if outgassing comparable to
JET-C at least a factor 4 lower long term retention to be expected
Main mechanism for retention in Be/W mix: implantation and codeposition
Reduction in retention rate in line with laboratory experiments for codeposition
Confirmation of the trend in reduction of retention rates with change of material mix according to predictions for ITER
Extension of the operational time before cleaning intervention in ITER

## Slide 17: Long Term Outgassing
Philipps et al.
J. Vac. Soc.1993
outgassing after operation without cryo pump
Long term outgassing observed in old JET limiter configuration
Similar observations with new JET-ILW
Continuous outgassing after operation / nights / weekends
In JET-C not as important as retention in co-deposits dominated whole retention
In JET-ILW this becomes a significant process in the overall analysis
F(t)~t-n
n=0.8
Deuterium
Total Pressure
V. Philipps et al.
PSI 2012

## Slide 18: Phases During a Discharge
Ip
nl
PICRH
Gas injected
1 - More gas injected in limiter ramp up phase: ~5x1021D for C and 1.0x1022D for Be/W
2 - Less gas injection during divertor phase for Be/W (Plasma scenario, particle fluxes)
3 - More gas recovered by outgasing in between pulses ~1x1022D more recovered
72386 (Carbon)
80729 (Be/W)
2.0MA/2.4T
PICRH=1.5-1.8 MW
Limiter phase
~5x1021 D
3 phases
1. Ip/ne Ramp up (limiter Be)
2. Divertor & Heating (W)
3. Recovery by outgasing in
between pulses
70% pumped during pulse
30% in between pulses
Ramp-up
Divertor and Heating
Recov