## Slide 1: Probing Forensic Signatures of Nuclear Materials
Marianne P. Wilkerson, S. D. Conradson, J. Ellis, S. Kozimor, R. Martin, A. Pugmire, B. Scott, A. Tamasi, G. Wagner, J. Walensky, M. Zimmer
11 July 2014
LA-UR 14-24839
Transformational and Applied Research Directorate, National Technical Nuclear Forensics Center
U.S. Department of Homeland Security
Notes: Content Slide Notes
“UNCLASSIFIED” marking of slides is not a security requirement and may be deleted from the Slide Master (View › Master › Slide Master). In general, slides should be marked “UNCLASSIFIED” if there is potential for confusion or misinterpretation of something that could be deemed classified. For guidance on marking slides containing classified and unclassified controlled information, see the Protecting Information Web site at http://int.lanl.gov/security/protectinfo/.

## Slide 2: What is the problem that a Molecular and Chemical Forensic approach is addressing?
Increasingly varied and asymmetric threats are expanding the scope of nuclear forensics
Signatures are varied and can evolve, while any given sample may include multiple signatures
The scale of a signature may be tiny or LARGE
Accurate, effective technical analysis depends on
- identifying new signatures
- understanding measurement limitations
- evaluating complementary nature between traditional and new measurements
- assessing the value of the information
Production, conversion and aging of actinide materials are chemical in nature
Pu chip
LA-UR 14-24839

## Slide 3: What do we mean by chemical speciation?
Levels of “Chemical Analysis”
Refers indirectly to the phase association: dissolved, or associated with various mineral or colloidal phases
Physical (or Phase) Speciation
Refers to the chemical form and generally includes a knowledge of phase
Depending on the type of information, various levels exist
  Identity of the element
  Physical state
Chemical Speciation
LA-UR 14-24839

## Slide 4: What do we mean by chemical speciation?
Levels of “Chemical Analysis”
Refers indirectly to the phase association: dissolved, or associated with various mineral or colloidal phases
Physical (or Phase) Speciation
Refers to the chemical form and generally includes a knowledge of phase
Depending on the type of information, various levels exist
  Identity of the element
  Physical state
  Oxidation state
Chemical Speciation
U(III) U(IV) U(V) U(VI)
LA-UR 14-24839

## Slide 5: What do we mean by chemical speciation?
Levels of “Chemical Analysis”
Refers indirectly to the phase association: dissolved, or associated with various mineral or colloidal phases
Physical (or Phase) Speciation
Refers to the chemical form and generally includes a knowledge of phase
Depending on the type of information, various levels exist
  Identity of the element
  Physical state
  Oxidation state
  Empirical formula
Chemical Speciation
UO2(OH)+
U(III) U(IV) U(V) U(VI)
LA-UR 14-24839

## Slide 6: What do we mean by chemical speciation?
Levels of “Chemical Analysis”
Refers indirectly to the phase association: dissolved, or associated with various mineral or colloidal phases
Physical (or Phase) Speciation
Refers to the chemical form and generally includes a knowledge of phase
Depending on the type of information, various levels exist
  Identity of the element
  Physical state
  Oxidation state
  Empirical formula
  Molecular formula
  Molecular structure
Chemical Speciation
UO2(OH)+
U(III) U(IV) U(V) U(VI)
LA-UR 14-24839

## Slide 7: Actinide processing is rich in chemical information
LA-UR 14-24839
Uranium
Ore
> 10 phases between UO2
and UO3, in addition to
hydrated forms of UO3
Deceptively simple formula
and cubic structure of UO2
masks incredibly complex
speciation
Weathering under
environmental conditions may
effect changes in morphology, chemical speciation
Can chemical speciation of major and minor constituents be measured?
Do signatures of chemical speciation change over time?
How can we ground these measurements with standards?

## Slide 8: What tools provide access to chemical speciation?
Morphology
SEM-Energy
Dispersive
Spectroscopy
Inductively Coupled
Plasma – Mass Spectrometry
X-ray diffraction analysis
X-ray Absorption
Spectroscopy
Elemental
Structural (lattice)
Scanning Electron Microscopy
g-UO3
LA-UR 14-24839

## Slide 9: Measurement Capabilities
Bruker D8 ADVANCE
powder X-ray
diffractometer
Stanford Synchrotron Radiation Lightsource
Menlo Park, CA
FEI Quanta 200F Field Emission Scanning Electron Microscope
Morphology
Elemental/isotopic Analysis
Chemical Speciation
LA-UR 14-24839
Thermo Finnigan Element XR ICP-MS

## Slide 10: How is local structure through XAFS determined?
XAFS- X-ray Absorption Fine Structure
high energy X-rays allow for excitation of core electrons to bound states
XANES- X-ray Absorption Near Edge Structure
arises from differences in oxidation state, local structure
EXAFS- Extended X-ray Absorption Fine Structure
distribution of interatomic distances around atoms
22 keV
21 keV
17 keV
100 keV
LA-UR 14-24839

## Slide 11: Systematic experiments on UO2 using EXAFS to measure sensitivity to oxidation.
Increased oxidation yields monotonic changes.
With H2O, intermediate temperature Weak CO:CO2 oxidizer, high temperature
Conradson, S. D.; Manara, D.; Wastin, F.; Clark, D. L.; Lander, G. H.; Morales, L. A.; Rebizant, J.; Rondinella, V. V. . Inorg. Chem. 2004, 43(22), pp 6922-6935.
LA-UR 14-24839

## Slide 12: Reference information is derived from high-purity uranium oxide bulk materials
Uº UO22+
UO22+ + H2O2 UO2(O2)·xH2O
UO2(O2)·2H2O A-UO3
A-UO3 U3O8
A-UO3 UO2
UO2(O2)
precipitate
Reaction vessel
Tube furnace
UO2
LA-UR 14-24839
pH 3
air
400ºC
air
900ºC
air
500ºC
H2
NIST SRM U960
NBL A112A

## Slide 13: Can trace chemical species be measured from legacy samples of U3O8
Precipitate Source Precipitate Sample Product
UNH
UO4
U3O8
pH 1
20ºC
800ºC
UNH
UO2F2
UO4
pH 1
20ºC
975ºC
pH 8.4
20ºC
ADU
800ºC
U3O8
U3O8
LA-UR 14-24839
Age of samples: ~2-3 years
Common source of starting material
Preparation scale: 10 g

## Slide 14: Comparison of SEM images of U3O8 materials at time 0
S1
L1
L2
L3
LA-UR 14-24839
A-UO3  U3O8
900ºC
UNH  UO4  U3O8
UNH  UO4  U3O8
UO2F2  ADU  U3O8
20ºC
20ºC
20ºC
pH 1
pH 1
pH 8.4
800ºC
800ºC
975ºC
air

## Slide 15: Comparison of reference lines with pXRD patterns of U3O8 materials identifies speciation
A-UO3  U3O8
900ºC
UNH  UO4  U3O8
UNH  UO4  U3O8
UO2F2  ADU  U3O8
20ºC
20ºC
20ºC
pH 1
pH 1
pH 8.4
800ºC
800ºC
975ºC
LA-UR 14-24839
S1
L1
L2
L3
air

## Slide 16: EXAFS of U3O8 materials reveals disorder
air
(UO2(O2)·xH2O)
(U3O8 + UO3·xH2O)
(U3O8 + UO2F2·xH2O)
LA-UR 14-24839
S1
L1
L2
L3
A-UO3  U3O8
900ºC
UNH  UO4  U3O8
20ºC
pH 1
800ºC
UNH  UO4  U3O8
20ºC
pH 1
975ºC
UO2F2  ADU  U3O8
20ºC
pH 8.4
800ºC

## Slide 17: Aging Vessels and Circulating Bath
Anovitz, L. M.; Riciputi, L. R.; Cole, D. R.;
Gruszkiewicz, M. S.; Elam, J. M. J.
Non-Cryst. Solids 2006, 352, 5652.
LA-UR 14-24839

## Slide 18: Do these chemical signatures change over time?
Constant relative humidity (+/- 2%) is produced by an excess of a water soluble salt in contact with its saturated solution.
  ASTM International, Designation: E104-02, Standard Practice for Maintaining Constant Relative Humidity by Means of Aqueous Solutions
  CRC Manual, Constant Humidity Solutions
RH = A*exp(B/T)
Lithium Iodide: 25% RH at 278.15 K
15% RH at 310.15 K
Potassium Nitrate: 97% RH at 278.15 K 89% RH at 310.15 K
LA-UR 14-24839
Relative Humidity = Actual Vapor Density
Saturation Vapor Density
Conditions | Water vapor density
LTLH | 1.7e-06 g/cm3
HTLH | 6.6e-06 g/cm3
LTHH | 6.7e-06 g/cm3
HTHH | 39e-06 g/cm3
Liquid water | ~1 g/cm3

## Slide 19: Morphology of S1 at all conditions after 0 and 2 years
LA-UR 14-24839
A-UO3  U3O8
900ºC
air

## Slide 20: pXRD patterns of S1 at all conditions after 3 years reveals speciation
LA-UR 14-24839
A-UO3  U3O8
900ºC
air

## Slide 21: EXAFS of S1 at all conditions after 0 and 3 years
LA-UR 14-24839
A-UO3  U3O8
900ºC
air

## Slide 22: Morphology of L2 U3O8 at all conditions after 0 and 2 years
LA-UR 14-24839
(U3O8 + UO3·xH2O)
UNH  UO4  U3O8
20ºC
pH 1
975ºC

## Slide 23: pXRD patterns of L2 U3O8 at all conditions after 2 years reveals speciation
LA-UR 14-24839
(U3O8 + UO3·xH2O)
UNH  UO4  U3O8
20ºC
pH 1
975ºC

## Slide 24: EXAFS of L2 U3O8 at all conditions after 0 and 2 years
LA-UR 14-24839
(U3O8 + UO3·xH2O)
UNH  UO4  U3O8
20ºC
pH 1
975ºC

## Slide 25: Morphology of L3 U3O8 at all conditions after 0 and 2 years
LA-UR 14-24839
(U3O8 + UO2F2·xH2O)
UO2F2  ADU  U3O8
20ºC
pH 8.4
800ºC

## Slide 26: pXRD patterns of L3 U3O8 at all conditions after 2 years reveals oxidation
LA-UR 14-24839
(U3O8 + UO2F2·xH2O)
UO2F2  ADU  U3O8
20ºC
pH 8.4
800ºC

## Slide 27: EXAFS of L3 U3O8 at all conditions after 0 and 2 years
LA-UR 14-24839
(U3O8 + UO2F2·xH2O)
UO2F2  ADU  U3O8
20ºC
pH 8.4
800ºC

## Slide 28: Morphology of L1 at all conditions after 0 and 2 years
LA-UR 14-24839
T=2 yrs.
LTLH-5°C @ 25% RH
(UO2(O2)·xH2O)
UNH  UO4  U3O8
20ºC
pH 1
800ºC

## Slide 29: pXRD patterns of L1 U3O8 at all conditions after 3 years reveals hydration
LA-UR 14-24839
(UO2(O2)·xH2O)
UNH  UO4  U3O8
20ºC
pH 1
T=2 yrs.
LTLH-5°C @ 25% RH

## Slide 30: EXAFS of L1 U3O8 at all conditions after 0 and 3.5 years
LA-UR 14-24839
(UO2(O2)·xH2O)
UNH  UO4  U3O8
20ºC
pH 1

## Slide 31: Conclusions
Processing of uranium oxides is chemical in nature, providing opportunities for measurements of chemical signatures
Results from an integrated approach rely upon synthesis, spectroscopy and morphologic characterization of a variety of materials
Chemical speciation following aging under environmental conditions is providing insights into chemical transformations
Speciation can be characterized, not only by m-XRD and m-XANES spectroscopy, but also via m-EXAFS measurements, an incisive technique for determining chemical speciation and changes in local structure
LA-UR 14-24839

## Slide 32: Acknowledgements
Synthesis
Dallas D. Reilly, Univ. Nevada-Las Vegas
Alison L. Tamasi, Univ. Missouri-Columbia (NTNFC Graduate Fellow)
Morphology
Beau J. Barker, LANL Seaborg Institute Postdoc Fellow
Gregory L. Wagner, Technologist 2
Sandra A. Zerkle, UCSD undergraduate
Mindy M. Zimmer, Postdoc
Powder X-ray Diffraction Analysis
Brian L. Scott
X-ray Absorption Spectroscopy
Steven D. Conradson
Stosh A. Kozimor
Alison L. Pugmire (LANL LDRD Early Career Award)
Isotopic Analysis
William S. Kinman
Computational Analysis
Tyler Mullen, High School Co-Op
Reid B. Porter
Christy E. Ruggiero
Lav Tandon
Theory
Jason K. Ellis, Postdoc
Richard L. Martin
Additional Collaborators
Larry Anovitz, University of Tennessee
Corwin H. Booth, LBNL
Carol J. Burns
David L. Clark
Kenneth Czerwinski, Univ. Nevada-Las Vegas
Julianna E. Fessenden-Rahn
Susan D. Hanson
Justin Holland, Y-12 NSC
Andrew Sutton
Larry E. Ussery
Gregory J. Van Tuyle
Justin R. Walensky, Univ. Missouri
Sam Webb, SSRL
This work has been supported by the U.S. Department of Homeland Security, Domestic Nuclear Detection Office, under competitively awarded IAA HSHQDC-08-X-00805. This support does not constitute an express or implied endorsement on the part of the Government.
LA-UR 14-24839