## Slide 1: Characterization of a Uranium Ore Concentrate Sample Interdicted in Durban, South Africa
IAEA Conference on Advances in Nuclear Forensics
July 2014
Ian D. Hutcheon
Glenn Seaborg Institute

## Slide 2: A 1-kg uranium-rich sample was interdicted in Durban, South Africa on 14 November 2013
South Africa police seized a shopping bag containing ~1 kg of a uranium-rich material in a “sting” operation
Two individuals arrested
Material analyzed by Necsa
  Uranium ore concentrate, depleted in 235U: 0.38% 235U
10 g aliquot transferred to LLNL in December 2013 under the MOU describing cooperation in nuclear forensics between South Africa and the United States
Kobus Hancke visited LLNL in January 2014 to participate in the analyses

## Slide 3: We used a variety of analytical techniques to characterize the Durban UOC
Gamma ray spectroscopy
X-ray diffraction
X-ray fluorescence
Optical spectroscopy
Scanning electron microscopy
Davies-Gray titration
Inductively-coupled plasma mass spectrometry (ICP-MS)
Thermal ionization mass spectrometry (TIMS)

## Slide 4: The sample is a fine-grained yellow powder

## Slide 5: The sample is a fine-grained yellow powder

## Slide 6: The sample is a fine-grained yellow powder

## Slide 7: VIS/near IR spectroscopy indicates the sample is an ammonium uranate

## Slide 8: Gamma ray spectroscopy confirmed the depleted U-isotope composition of the UOC

## Slide 9: X-ray diffraction indicated four phases are present in the UOC

## Slide 10: U-assay and trace element abundances are unremarkable and do not point to a specific location or process
Davies-Gray titration yields a U-content of 74.9 ± 0.5 wt.%
  Compares to 67.5 wt.% measured by Necsa
Total impurity content of ~300 mg/g
Major impurities are Na, K, Ca, Fe, Mo and Cs
    Cs makes up over 50% of the total
    Pu is ~10 pg/g

## Slide 11: Mass spectrometry confirms depleted uranium with high 236U and very low Pu

## Slide 12: Sr and Pb isotopes indicate the UOC source is not represented in the U-Sourcing Database

## Slide 13: Reactor modeling suggests the UOC could represent reprocessed, irradiated fuel from a graphite-moderated reactor
Modeled a graphite moderated, natural uranium (NU) fueled reactor using the MAGNOX reactor model included in the Origen-ARP component of SCALE 6.1
NU fuel irradiated for ~100 days to a burnup of 1.6 GWD/MTU would have a 240Pu content of ~14% at discharge
Using this fuel as feed for an enrichment cascade producing 235U enriched to 2%, the ORNL MSTAR program calculates 234U /235U = 9.1 x 10-3 and 236U /235U = 4.2 x 10-2, both values consistent with measurements

## Slide 14: Summary
The UOC is ammonium uranyl flouride plus two hydrated uranyl oxides
Total impurity content of ~300 mg/g
Major impurities are Na, K, Ca, Fe, Mo and Cs
The UOC is depleted in 235U with a 235U/238U ratio ~2x lower than that of natural uranium (NU)
The elevated 236U content indicates the parent material was irradiated in a nuclear reactor
The UOC likely originated as NU fuel irradiated in a graphite-moderated reactor and used as feedstock for an enrichment cascade

## Slide 15: Acknowledgements
The LLNL/NECSA nuclear forensics team:
Lars Borg
Amy M. Gaffney
Victoria G. Genetti
Patrick M. Grant
Kobus J. Hancke
Ian D. Hutcheon
Theresa M. Kayzar
Gregory L. Klunder
Kim B. Knight
Michael J. Kristo
Rachel E. Lindvall
Naomi Marks
Reuben P. Mogafe
Aubrey N. Nelwamondo
Christina E. Ramon
Erick C. Ramon
Martin Robel
Michael A. Sharp
Michael J. Singleton
Ross W. Williams
Work supported by NNSA’s Office of Defense Nuclear Nonproliferation and the South African Nuclear Energy Corporation