## Slide 1: Exploring spectroscopic and morphological data as new signatures for uranium ore concentrates
D. M. L. Ho, D. Manara, Z. Varga, L. Fongaro, A. Nicholl,
M. Ernstberger, A. Berlizov, P. Lindqvist-Reis, T. Fanghänel and K. Mayer
IAEA Nuclear forensics conference (7-10 July 2014)

## Slide 2: Introduction
Uranium ore concentrates

## Slide 3: Current signatures based on literature
Uranium ore concentrate
Morphology
Organic impurities
Isotopes
Trace elements
Anionic impurities
Composition
U
Pb
Sr
Th
Rare earth
elements
*SO42- *CO32- *NO3-
F-
Cl-
Infrared spectroscopy*
Ion chromatography
reflectance
IR
Laser induced breakdown
spectroscopy
Scanning electron microscopy
ICP-MS
TIMS
Image Analysis (?)
S
Raman fingerprints (?)
Alamine® 336
Decanol
GC-MS
Introduction
Other elements
Nd

## Slide 4: Raman spectroscopy
Raman spectroscopy (Bulk analysis)
Hand-held
(Ahura Scientific)
Bench-top
(Bruker Senterra)
Laboratory
(Jobin Yvon T64000)
Methods
A laser (Ʋ0) is used to excite the molecules to virtual states. As a result of the interaction with molecules, incident photons are scattered inelastically
(only 1 out of 108 photons)
 Raman effect (ƲR)
http://www.wiley-vch.de/books/sample/3527405062_c01.pdf
http://www.nomenrl.com
http://www.bruker.com
http://www.physik.fu-berlin.de

## Slide 5: Interpretation of Raman spectrum
1
2
3
Raman bands relating to:
  Uranium compound
  Process related impurities
  Electronic transitions (non-Raman effects)
Results:
Raman spectroscopy
D.M.L. Ho, D. Manara, Zs Varga, A.Berlizov, Th. Fanghänel and K. Mayer, Radiochimica Acta 12 (2013) 779-784.
Applicability of Raman spectroscopy to nuclear forensics

## Slide 6: Comparison of 3 different dispersive Raman spectrometers
D.M.L. Ho, D. Manara, P. Lindqvist-Reis, Th. Fanghänel and K. Mayer, Vibrational Spectroscopy 73 (2014) 102-110.
Results:
Raman spectroscopy

## Slide 7: Comparison of 3 different dispersive Raman spectrometers
D.M.L. Ho, D. Manara, P. Lindqvist-Reis, Th. Fanghänel and K. Mayer, Vibrational Spectroscopy 73 (2014) 102-110.
Results:
Raman spectroscopy

## Slide 8: Unsupervised classifications of UOCs + other uranium compounds using principal component analysis (PCA)
D.M.L. Ho, Z. Varga, L. Fongaro, P. Lindqvist-Reis, Th. Fanghänel and K. Mayer, Forensic Science International, -to be submitted for publication (together with AWE/Liverpool)
Results:
Raman spectroscopy
Scores on PC 2 (13.74 %)
Scores on PC 1 (51.44 %)

## Slide 9
Sample 1
Sample 2
Methods
Image analysis of UOC
Sample 1
Sample 2
Morphology
17 samples
(2-5 images per sample at 500x magnification)
Total of 65 images
30 descriptors of shapes and sizes obtained
PCA analysis
Image texture analysis
26 samples
(5 images per sample at 1000x magnification)
Total of 130 images
Using Angular Measure Technique
(based on angular measure algorithm)
PCA analysis
Sizes & shapes
Image texture analysis
K.H. Esbensen, K.H. Hjelmen and K. Kvaal,
'The AMT Approach in Chemometrics-First Forays',
Journal of Chemometrics 10 (1996) 569-590.

## Slide 10
Results:
Image Analysis - Morphology

## Slide 11
Results:
Image Analysis - Morphology
Rössing
Key Lake
South Alligator
Belgian Congo

## Slide 12
Results:
Image texture analysis
K.H. Esbensen, K.H. Hjelmen and K. Kvaal,
'The AMT Approach in Chemometrics-First Forays',
Journal of Chemometrics 10 (1996) 569-590.
MA value
Scale

## Slide 13
Results:
Image texture analysis

## Slide 14: Summary
Uranium ore concentrate
Morphology
Organic impurities
Isotopes
Trace elements
Anionic impurities
Composition
U
Pb
Sr
Th
Rare earth
elements
*SO42- *CO32- *NO3-
F-
Cl-
Infrared spectroscopy*
Ion chromatography
reflectance
IR
Laser induced breakdown
spectroscopy
Scanning electron microscopy
ICP-MS
TIMS
Size/shape of dispersed particles + image texture analysis
S
Raman fingerprints
Alamine® 336
Decanol
GC-MS
Raman fingerprints
Nd

## Slide 15: Acknowledgements
Dieter Schild
(Institute for Nuclear Waste Disposal, Karlsruhe)
International Atomic Energy Agency, Vienna
(for hand-held Raman and UOC samples)
Springfields, UK for the UOC samples