## Slide 1: New free-streaming/recycling model for W gross erosion during ELMs validated by DIII-D measurements; predictions made for ITER
Model for ELM particle/energy flux to target developed that accounts for local recycling
Chart: 
| 0.93252839872000004 | 0.76066239623999998 | 1.1851741326399998 | 0.95162765871999999 | 0.69896083587000002 | 1.1209412642999999 | 1.7244867619299999 | 1.2829922279999999 | 1.11676552095 | 1.221115049
 | 1.3621 | 0.23719 | 1.0573 | 0.7969 | 0.35005 | 2.7173 | 1.5982 | 0.97962 | 2.5723 | 0.69782
 | 0.97895 | 0.7365 | 0.60652 | 0.60515 | 0.3893 | 1.5832 | 1.199 | -0.42538 | 0.93057 | -0.4334 | 1.0154 | 1.5279 | 0.969 | -0.42068 | 0.99663 | 0.80632 | 0.76643 | 0.66118
Unity | 0 | 10
 | 1.0381 | 1.0345 | 1.2799 | 0.89239 | 1.0665 | 0.48458 | 0.73049 | 0.69184 | 0.61028 | 0.32239 | -0.24781 | 0.71981 | 0.92163 | 0.18761 | 1.0425
Model Perp. ELM Ion Fluence (1017 m-2)
1:1
Meas. Perp. ELM Ion Fluence (1017 m-2)
, Free-streaming + recycling model (Reff=0.96)
= 0.85
Model predicts energetic free-streaming ions from pedestal top dominate W erosion during ELMs
Good agreement w/ DIII-D data (WI filterscopes)
Predictions for unmitigated ELMs in ITER DT:
  W erosion during ELMs mostly by D+ and T+ pedestal ions
  10x more W atoms/m2/ELM eroded on ITER than DIII-D, implying ELM mitigation also important to reduce W sourcing
Chart: 
Chart: 
FS+Recycling Model
DIII-D Data (WI spectros.)
ne,ped = 3.7x1019 m-3
Te,ped = 670 eV
Te,div = 25 eV
W gross erosion (1016 cm-2 s-1)
Time relative to ELM start (ms)
Time relative to ELM start (ms)
Total W erosion, Model
Free-streaming D+W
Free-streaming C6+W
Recycling C6+W
Chart: 
GAMMA_W_ADDL_D
ITER DT 15 MA, 5.3 T
(Q=10)
ne,ped = 8x1019 m-3
Te,ped = 4700 eV
Te,div = 5 eV
FS T+W
FS D+W
FS Be4+W
Time relative to ELM start (ms)