## Slide 1: High-temperature creep properties of NIFS-HEAT-2 high-purity low-activation vanadium alloy
T. Nagasakaa, b, T. Murogaa, b, T. Tanakaa, b, A. Sagaraa, b, K. Fukumotoc, P. F. Zhengd, and R. J. Kurtze
aNational Institute for Fusion Science
bThe Graduate University for Advanced Studies
cResearch Institute of Nuclear Engineering, University of Fukui
dSouthwestern Institute of Physics
ePacific Northwest National Laboratory

## Slide 2: Vanadium alloy is one of options Back-up and alternative to ferritic steels
No magnetization
 | SS316 | V alloy (NIFS-HEAT-2)
Magnetic permeability (RT) | 1.004 @H=200 Oe | 1.0005 @H=1300 Oe
Stronger above 600oC
Higher thermal conductivity
Fig. Tensile strength
Fig. Thermal conductivity
Back-up if the ferromagnetism causes big problems
Alternative for higher thermal efficiency blanket
ferritic steel

## Slide 3: Scale-up of alloy production is ongoing in the world
Scale-up for V alloy was pursued in the US for the first time. Fabrication technology for 1.2 ton-scale melting and breakdown process have been developed.
Development of advanced technology for purification, joining and coating are ongoing in the world
1995
2000
2010
US832665, 832864, V-4Cr-4Ti, US-DOE
500, 1200 kg
NIFS-HEAT-1 & 2, V-4Cr-4Ti, NIFS, Japan
RF-VVC2 & 3, V-(4-8)Cr-(4-5)Ti, A. A. Bochvar Inst., RF
30, 160 kg
42, 110 kg
SWIP-30, V-4Cr-4Ti, SWIP, China
30 kg
CEA-J57, V-4Cr-4Ti, CEA Saclay, France
30 kg
2005
Project
US-DOE Fusion
Fusion & FBR
SFR & GFR
NIFS Fusion Eng.
Fusion HL-2A
Fig. Activities with the fabrication scale of 30 kg or more

## Slide 4: The highest-purity vanadium alloy in the world: NIFS-HEAT-2
ID | Country | Fabrication size / kg | Alloying elements / mass% |  |  | Interstitial impurities / mass ppm |  |  | 
 |  |  | V | Cr | Ti | C | N | O | C+N+O
NIFS-HEAT-2[1] | Japan | 166 | Bal. | 4.02 | 3.98 | 69 | 122 | 148 | 339
US832665[2] | USA | 500 | Bal. | 3.25 | 4.05 | 170 | 100 | 330 | 600
RF-VVC3[3] | Russia | 110 | Bal. | 3.76 | 4.64 | 290 | 100 | 200 | 590
SWIP-30[4] | China | 30 | Bal. | 3.81 | 3.92 | 130 | 20 | 270 | 420
CEA-J57[5] | France | 30 | Bal. | 3.76 | 3.93 | 70 | 110 | 290 | 470
ID | Harmful radioactive impurities / mass ppm |  |  |  |  | 
 | Al | Co | Nb | Ni | Mo | Al+Co+Nb+Ni+Mo
NIFS-HEAT-2 | 59 | 0.7 | 0.8 | 7 | 24 | 92
US832665 | 355 | 0.295 | 60 | 9.6 | 315 | 740
RF-VVC3 | 240 |  | < 10 | < 5 | 68 | 308
SWIP-30 | 100 |  |  | 82 | 35 | 217
CEA-J57 | 190 | 0.4 | < 10 | 17 | 75 | 282
Fig. Lattice of V alloy
a
V
O
Nb
Interstitial solute:
Much hardening
Substitutional
solute
Both interstitial impurities and radioactive impurities are successfully reduced using industrial-scale technologies
[1] T. Nagasaka et al., J. Plasma and Fusion Res. SERIES, 5 (2002) 545., [2] M. L. Grossbeck et al., J. Nucl. Mater., 258-263 (1998) 1778., [3] M. M. Potapenko et al., ICFRM-14, Sep. 6-11, 2009, Sapporo, Japan., [4] H. Y. Fu et al., J. Nucl. Mater. 442 (2013) S336., [5] V. Duquesnes et al., J. Nucl. Mater. 426 (2012) 96.

## Slide 5: Many properties have been improved by the purification - Interstitial impurity effect -
The reduction of interstitial impurities enabled welding and room-temperature heavy working
US
C+N+O: ~1380
mass ppm
Fig. Cross section after tubing at RT[1]
1 mm
5 mm
Workability
Weldability
Fig. Laser weld and its cross section
Fig. Impact absorbed energy of weld joint
IAEA FEC 2000 & 2004
9 rolling +
10 annealing
Defects on tube wall
Plates: 0.25-25.4 mm t
Tubes: f4.57 x 0.25t,
f10 x 0.5t mm
Wires: f2, 8 mm
NH2
C+N+O: 1174
C+N+O: 313-570
[1] Rowcliffe et al., Fusion Mater. Semi-annual Progress Rep., US-DOE/ER-0313/34 (2003) 6.
Fig. Various products of NH2

## Slide 6: Low-activation characteristics have been improved by the purification - Metallic impurity effect -
The reduction of the harmful high activation impurities resulted in one-order smaller contact dose rate compared with US alloy after 100 y cooling
NH2 satisfies the quasi-hands-on limit, 10-4 Sv h-1, where material recycling is possible with simple radiation shields, such as 4 cm-thick lead blocks
Fig. Decay of contact dose rate after the irradiation with neutron wall loading of 1.5 MW/m2 for 7.5 y (110 dpa)
Low-activation characteristics
Remote recycling
Hands-on recycling
No impurity
US
RF&CEA
NH2
One order reduction at 100 y
Quasi-hands-on recycling

## Slide 7: A big concern: possible degradation of high-temperature strength due to purification softening
Degradation of yield strength was observed at 750 and 800oC in tensile tests
The degradation is attributed to reduction in interstitial impurity (C, N and O) level
Fig. Comparison of yield strength (YS) and ultimate tensile strength (UTS) of NIFS-HEAT-2 (NH2) and US832665 (US) in tensile tests

## Slide 8: Creep: Deformation under small constant load – Determine the upper limit of operation temperature –
Creep tests apply small and constant stress, several 10 MPa, which is typical and normal in fusion blanket condition
For blanket design, creep lifetime determines the upper limit for operation temperature
Tensile test:
1 min~1 hr, ~500 MPa
Creep test:
1 day~3 year, ~100 MPa
Fig. Principles for tensile tests and creep tests
Fixed: Deformation speed
Measured: Load & displacement
Load
Displacement & time

## Slide 9: Creep test facility in NIFS: Eight creep testing machines
Design features
  Miniature specimen: 5 mm in gauge length
  High temperature: Max. 900oC
  High vacuum: <10-4 Pa with Zirconium getter
Fig. Creep testing machines
# | Base mechanics | Temp. | Load | Vacuum
1 | INTESCO MC-100 Dead weight | RT 300-800oC | 10-500 N | <10-4 Pa Zr getter
2 | INTESCO MT-100 Crosshead |  |  | 
3 | INTESCO MT-100 Crosshead |  |  | 
4 | SHIMADZU AG-1kNXplus Crosshead | RT 300-900oC Constant temp. air booth | 50-1,000 N | 
5 |  |  |  | 
6 |  |  |  | 
7 |  |  |  | 
8 | SHIMADZU AG-20kNXplus Crosshead |  | 200-20,000 N | 
Materials in ongoing collaborations: V alloys, RAF steels, ODS steels, W alloys, Zr alloys, Nb alloys
International activity: Standardization of small specimen test technique (IAEA-CRP-F1.30.17)
3
2
1
4
5
6
7

## Slide 10: Results of creep tests Purification softening limited at high stress region
In the higher stress region, rupture time of NH2 were shorter than the dashed trend line for US data
 Purification softening at higher stress region than 150 MPa
Creep rupture time of NH2 in the lower applied stress region was comparable to those of US alloy
 The purification did not degrade creep strength around 100 MPa
  Detailed analysis on mechanisms: the degradation of yield stress might lead to deformation by dislocation glide, in addition to deformation by dislocation climbing, the predominant creep process in this stress and temperature regime
Fig. Typical time-strain creep curves
Fig. Creep rupture stress vs. rupture time

## Slide 11: Scaling with Larson-Miller parameter Expected rupture time: 105 h at 700oC, 110 MPa
Larson-Miller Parameter for time-temperature equivalence analyses
Creep strength of NH2 is degraded at 200 MPa and above, while is still superior to other fusion structural materials, such as RAF & ODS steels, and comparable to US under 100 MPa and below.
100,000 h is expected for creep rupture time at 700oC under 110 MPa
Fig. Larson-Miller plot of creep data
High creep strength
High temperature and long rupture time

## Slide 12: Operation window for vanadium alloys
s1% has not been obtained for NH2 because of large error for primary creep measurement
s1% for the US heat was used for preliminary analysis, assuming creep properties of NH2 is similar to the US heat at 100 MPa or less
A design allowable stress, 73 MPa, is possible up to 700oC
An example: ASME code
Fig. Allowable stress window
[1] R. J. Kurtz et al., J. Nucl. Mater. 329-333 (2004) 47.

## Slide 13: Allowable heat flux to V alloy blanket
Based on the preliminary analyses for the thermal stress, 700oC is possible for operation temperature of vanadium alloy blanket, if the heat flux is set as 1 MW m-2 or less
One-side heating with edge constraint
Coolant
Plasma
& vacuum
First wall of blanket
Coolant
First wall
Plasma
& vacuum
700oC operation of vanadium alloy blanket is feasible
First wall thickness, tw | Allowable heat flux, qS
3 mm | 1 MW m-2
5 mm | 0.6 MW m-2

## Slide 14: Conclusions and future plan
The purification for NIFS-HEAT-2 improved many properties, however the concern was degradation of creep strength
No negative effect of purification is observed in creep, if applied stress is around 100 MPa, which is enough for blanket design
According to the creep properties, 700oC is possible for operation temperature of vanadium alloy blanket
Longer creep tests than 10,000 h are planned in future, to validate the allowable stress in long-term operation
Condition | NIFS-HEAT-2 |  |  | US832665 |  | 
 | Uniaxial | Biaxial (Pressurized tube) |  | Uniaxial | Biaxial（Pressurized tube) | 
Time / h | 2375 | 240 [1] | 2000 [2] | 4000 [3] | 9663 [4] | 2000 [2]
Stress / MPa | 200 | 150 | 110 | 160 | 120 | 120
Atmosphere | Vacuum | Vacuum | Liq. Li | Vacuum | Vacuum | Liq. Li
Table The longest creep data for vanadium alloys at 700oC
[1] K. Fukumoto et al., ICFRM-12, De. 5-9, 2005, Santa Barbara, USA., [2] M. M. Li et al., Journal of Nuclear Materials 367-370 (2007) 788., [3] K. Natesan et al., US-DOE/ER 3013/29 (2000) 37., [4] R. Kurtz et al. US-DOE/ER 3013/31 (2001) 7.
Progress by the present study