## Slide 1
Erosion/Deposition in the JET Divertor During the ITER-like Wall Campaigns
Erosion/Deposition in the JET divertor studied using marker tiles
Decrease of material deposition rate by factor 4-9 compared to JET-C
Decrease of D retention by factor 10-20 compared to JET-C
Confirmed in all three ILW campaigns
Campaign | D (g) | Be (g) | C (g)
ILW-1 | 0.9 | 53 | 13
ILW-2 | 0.7 | 60 | 7
ILW-3 | 0.9 | 46 | 6
0
A
B
C
D
1
3
4
5
6
7
8
0
JET ILW divertor
Deposition in the JET ILW divertor