20 Years of Nuclear Forensics at ITU: between R&D and Case Work

Th. Fanghänel, K. Mayer, Z. Varga, M. Wallenius

European Commission
 Joint Research Centre, Institute for Transuranium Elements
76125 Karlsruhe, Germany

Abstract

Nuclear Material is kept under a stringent system of national control and international verification. This includes physical protection and safeguards measures.  Still, in early 1992 the first case of "nuclear smuggling" was detected with the seizure of a number of uranium fuel pellets. Those pellets were taken to the Institute for Transuranium Elements (ITU) for closer examination.  Since then, more such incidents have been reported and the phenomenon has been understood in a broader sense and referred to as "illicit trafficking". The methodology applied for the examination of the nuclear material (and any associated material) and the respective interpretation of data is referred to as "nuclear forensic science". From the onset of "Illicit trafficking" in the early 1990's till today, the phenomenon has changed and also the analytical and interpretational methods have evolved.

In more than two decades of involvement in nuclear forensic investigations at ITU, the analytical techniques were developed further, adapted to the specific needs and perfected with regard to timeliness and reliability of results.  Collaboration with authorities involved in the response process was strengthened and their specific needs have been included in the nuclear forensics methodologies. A systematic approach was developed for investigating samples of seized material, and a comprehensive, though efficient, process for conducting the various analyses was implemented. Taking into account that nuclear forensic samples are always unique in terms of the circumstances of the incidents, of the nature of the material and of the objectives of the investigation, the scientific investigations on the actual nuclear material are carried out under the same boundary conditions. On the other hand, we have to include in our considerations also the fact that illicit nuclear trafficking is a border crossing problem. In consequence, also the nuclear forensic investigations need to take this aspect into account. As can be seen, nuclear forensics is not only a multi-disciplinary branch of science; it involves further dimensions such as law enforcement, international safeguards, radiation protection etc. The paper will present selected examples of casework conducted during the past 20 years and illuminate recent methodological developments.

1. Introduction

The phenomenon of illicit trafficking of nuclear and other radioactive material appeared in the early 1990's. Since then, illicit trafficking, the associated risk of nuclear proliferation and the threat of nuclear terrorism remain areas of international concern. Continuous efforts for further enhancing nuclear security have been undertaken. This includes the prevention and detection of and the response to illicit incidents involving nuclear or other radioactive material. Nuclear forensic science is a key element of nuclear security. It is a relatively new discipline, which emerged with the first incidents of "nuclear smuggling" that were detected in 1992 in Europe. Nuclear forensic science, colloquially referred to as "nuclear forensics", aims at providing clues on the history of nuclear materials of unknown origin [1, 2]. This includes hints on the place and date of production and on the intended use of the material.

Such information is of relevance to nuclear security (e.g. in order to improve physical protection and safeguards measures at the pace of theft or diversion for preventing future diversions), or to prosecution (e.g. for providing evidence related to criminal acts involving nuclear or other radioactive materials). This information is obtained by measuring various parameters, such as major constituents, isotopic composition of the major elements or trace elements, products of radioactive decay, chemical, elemental, anionic or organic impurities, macroscopic appearance, microstructure, molecular composition and age [1-6]. Nuclear forensic science from its very beginning drew upon  a variety of different analytical techniques already available from nuclear safeguards, isotope geology or other areas [1].

2. Case Work

The first illicit trafficking incidents were reported in 1991 in Switzerland and in Italy. In the subsequent years numerous incidents were reported from central and eastern European Countries. Most of the seized nuclear material was taken to ITU for detailed material analysis. A new discipline in science was born: nuclear forensics. At the time, however, no systematic approach and no established methodology for analysing nuclear material of unknown origin were available. The analytical schemes were incident driven and established on an ad-hoc basis: nuclear forensics was still at its infancy.

2.1 The First Decade

The first case, where the intercepted material was subject to a detailed investigation occurred in 1992 in Germany and involved some 72 LEU pellets with a total mass of more than 1 kg. The national authorities asked ITU to analyse the material for obtaining hints on the potential origin of the material. During the following three years, twenty-one investigations of materials seized in Germany were performed. The circumstances of all of these incidents pointed at intentional smuggling of nuclear material supposedly preceded by a theft of nuclear material in the country of origin of the material. The majority of the cases concerned uranium fuels that were intended for use in early-generation graphite-moderated or pressurized-water nuclear power reactors. The most serious incidents involved kilograms of highly enriched uranium, several hundred grams of plutonium mixed oxide, and weapon-grade plutonium. Table 1 provides an overview of the illicit trafficking incidents where the nuclear material was investigated at ITU.

Table 1 Overview of seized material analysed at ITU in the period 1993 to 2003

| Find No. | Date | Place | Seizure |
| --- | --- | --- | --- |
| 1 | 05.03.1992 | Augsburg | 72 LEU pellets, 1099 g |
| 2 | 07.07.1992 | Berlin | Metal rod, Unat, 1772 g |
| 3 | 09.10.1992 | Windsbach | 22 Unat pellets, 320 g |
| 4 | 13.10.1992 | Taufkirchen | 54 LEU pellets, 843 g + Unat powder, 2017 g |
| 5 | 11.11.1992 | München | 1 Pu ionisation source |
| 6 | 03.12.1992 | München | 383 Pu ionisation source |
| 7 | 21.12.1992 | Böblingen | Metal cylinder, Unat, 2528 g |
| 8 | 24.12.1992 | Nürnberg | 1 Pu ionisation source |
| 9 | 17.02.1993 | München | 2 LEU pellets + 2 Unat pellets, 51 g |
| 10 | 16.03.1993 | Waidhaus | 1 LEU pellet, 14.9 g |
| 11 | 00.04.1993 | Berlin | Unat powder, 3.9 g |
| 12 | 15.07.1993 | Mainz | 3 pellets, Unat, 48 g |
| 13 | 10.05.1994 | Tengen | Pu in “red mercury” powder, 56 g |
| 14 | 06.06.1994 | München | 2 LEU pellets, 20 g |
| 15 | 08.06.1994 | Bavaria | DU in lead container, ~ 1 g |
| 16 | 15.06.1994 | Landshut | HEU granulate, 0.8 g |
| 17 | 08.07.1994 | München | 189 LEU pellets, 894 g |
| 18 | 08.08.1994 | Pforzheim | 2 LEU pellets, 19 g |
| 19 | 11.08.1994 | München | U and Pu powder, 560 g + Li metal, 201 g |
| 20 | 06.09.1994 | Berlin | Csnat metal |
| 21 | 14.10.1994 | Karlsruhe | 1 Unat pellet, 15 g |
| 22 | 29.05.1996 | Ulm | 206 LEU pellets, + Unat powder, 1.8 kg |
| 23 | 27.02.1997 | Karlsruhe | Parts of spent fuel assembly |
| 24 | 00.07.2001 | Karlsruhe | Contaminated items |

A total of 24 incidents were analysed at ITU during the first decade of "nuclear smuggling". As can be seen from table 1, almost half of the cases involved uranium fuel pellets. The need for attributing pelletized nuclear material to a reactor type and to a potential fabrication site triggered a joint project between ITU and the A.A. Bochvar All Russia Research Institute of Inorganic Materials (VNIINM) for jointly establishing a nuclear materials database that compiles data of Russian and Western European fuel manufacturers [7]. This database served first of all as analytical guidance in order to optimize the analytical process and to focus on the measurement of those parameters that would be the most useful for identifying possible origin and intended use of the material.

In parallel to the case work, research and development activities were started in order to establish the scientific basis for nuclear forensic investigations.

2.2 The Second Decade

After the "hype" of illicit trafficking in the first half of the 1990's, the number of cases reported in central Europe decreased. With the transition to first decade of the 21st century another type of incidents started being reported in increasing numbers: radioactively contaminated scrap metal. Table 2 provides an overview of those cases of contaminated scrap metal which involved nuclear material.

Table 2 Overview of incidents in the period 2003 to 2013 involving scrap metal contaminated with uranium

| Find No. | Date | Place | Seizure |
| --- | --- | --- | --- |
| 26 | 16.12.2003 | Rotterdam, NL | Unat (yellow cake) |
| 27 | 30.03.2006 | Hennigsdorf, D | HEU (contaminated scrap) |
| 29 | 02.06.2006 | Baarn and Bunschoten, NL | Various DU and Unat. powder |
| 32 | 00.11.2008 | Dordrecht, NL | Contaminated metal scrap |
| 33 | 00.07.-11.2009 | Dordrecht and Rotterdam, NL | Contaminated metal scrap |
| 34 | 02.2010 | Tornio, FIN | Contaminated metal scrap |
| 35 | 04.2010 | Rotterdam, NL | Contaminated metal scrap |
| 36 | 04.2010 | Dordrecht, NL | Contaminated metal scrap |
| 37 | 06.2010 | Dordrecht, NL | Contaminated metal scrap |
| 38 | 09.2010 | Dordrecht, NL | Contaminated metal scrap |
| 39 | 10.2010 | Dordrecht, NL | Contaminated metal scrap |
| 41 | 21.03.2011 | Dordrecht, NL | Contaminated metal scrap |
| 42 | 17.05.2011 | Dordrecht, NL | Contaminated metal scrap |
| 43 | 02.11.2011 | Rotterdam, NL | Contaminated metal scrap |
| 44 | 03.2012 | Moerdijk, NL | Contaminated metal scrap |

The samples from these incidents typically showed higher levels of chemical impurities and did not offer macroscopic features (as additional signature) supporting  a nuclear forensic interpretation. Consequently, the isotopic composition of the major element (uranium) provides the essential nuclear forensic information. Often, the samples consist of mixtures of materials, as can be revealed by micro-analytical techniques, such as secondary ion mass spectrometry (SIMS). This is illustrated in fig.1 showing several items carrying uranium contaminations (Find 38 in table 2), detected at a scrap metal recycling facility. Samples were taken from all the individual items and taken for analysis to ITU. Chemical analysis provided an average of the isotopic composition of the uranium deposits. It proved to be more useful in this case, however, to grind the material to a fine powder and to analyse individual particles by SIMS.

Figure 1 Items carrying radioactive contamination that triggered a radiation alarm at a scrap metal recycling facility. The items were singled out and subject to initial measurement by the competent national authority. Samples were taken to ITU for further analysis.

Figure 2 Measurement results obtained on individual particles by SIMS indicating distinct populations of low enriched uranium (left graph) and highly enriched uranium with 235U abundances up to 96% (right graph).

The SIMS measurement revealed the contamination to consist of a mixture of different enrichments, as shown in fig. 2. The 235U enrichment was found to range up to 96 mass% . Such highly enriched uranium is very rarely encountered. One application, however, is in lightweight nuclear reactors used in space (e.g. TOPAZ), thus providing also hints on the facility where the uranium was processed and where the contaminated metal possibly originates from.

3. Research and Development

Basically, nuclear forensics relies on the fact that certain measurable parameters (e.g. chemical impurities, isotopic composition, macroscopic appearance, microstructure) in a sample may be combined to form a characteristic "signature" for the given material. This signature provides hints on the history of the material, including the source material it was prepared from, the processes used for its transformation, the intended use, the date of production and possibly the origin of the material. The main challenges consist first of all the identification of those parameters providing useful hints on the history of the material and secondly, the interpretation of the analytical data. Thus, R&D activities focus on signature development and on method development.

The pattern of rare earth elements (REE), for example, has proven to be a useful signature for provenancing natural uranium. A method was developed for group separation of the REE (i.e. separating the REE from uranium without changing their relative abundance [8,9].  Also the isotopic composition of certain chemical impurities (e.g. Sr, Nd, or Pb) may provide hints on the geological environment the uranium was mined from. The products of the radioactive decay of uranium (e.g. 234U/230Th) are another important signature providing information on the last chemical separation of the nuclear material, usually referred to as the "age" of the material [10]. Classical methods of molecular spectroscopy such as Raman or Infrared-spectroscopy are also applied for identifying the chemical compound and anionic impurities [11]. The latter may point at the chemical processing the material was subjected to. Some of these aspects will be presented in some more detail in dedicated papers at this conference [12-15].

Conclusion

Nuclear forensics is a key element of nuclear security. Starting with the first cases of "nuclear smuggling" that were reported in Europe, ITU got closely involved in nuclear forensic investigations. In this period samples of nuclear material from more than 40 nuclear security incidents were investigated and information on the history of the material, its intended use and its potential origin was provided to the competent national authorities. The application of nuclear forensics methodology was backed by a comprehensive research and development program which results validated methods and useful nuclear signatures, ultimately supporting credible nuclear forensics conclusions.

References

1.  Mayer, K.; Wallenius, M.; Fanghänel, T.: Nuclear forensic science-From cradle to maturity. Journal of Alloys and Compounds 444-445, 50 (2007).

2.   Mayer, K.; Wallenius, M.; Ray, I: Nuclear forensics- a methodology providing clues on the origin of illicitly trafficked nuclear materials. Analyst 130, 433 (2005).

3.   Wallenius, M.; Mayer, K.; Ray, I.: Nuclear forensic investigations: Two case studies. Forensic Science International 156, 55 (2006).

4.   Keegan, Elizabeth; Wallenius Maria; Mayer, Klaus; Varga, Zsolt; Rasmussen, Gert: Attribution of uranium ore concentrates using elemental and anionic data. Applied Geochemistry 27, 1600 (2012).

5.   Badaut, V.; Wallenius, M.; Mayer, K.: Anion analysis in uranium ore concentrates by ion chromatography. Journal of Radioanalytical and Nuclear Chemistry 280, 57 (2009).

6.   Kennedy, A. K.; Bostick, D. A.; Hexel, C. R.; Smith, R. R.; Giaquinto, J. M.: Non-volatile organic analysis of uranium ore concentrates. Journal of Radioanalytical and Nuclear Chemistry (2012).

7.	Dolgov, J., Bibilashvili, Y. K., Chorokhov, N. A., Schubert, A., Janssen, G., Mayer, K., Koch, L.;  Installation of a database for identification of nuclear material of unknown origin at VNIINM Moscow; 21st ESARDA Symposium, 1999, Sevilla, Spain; Report EUR 18963 EN

8.	Varga, Z., Katona, R., Stefanka, Z., Wallenius, M.,Mayer, K., Nicholl, A.; Determination of rare-earth elements in uranium-bearing materials by inductively coupled plasma mass spectrometry; Talanta 80 (2010) 1744–1749

9.	Varga, Z., Mayer, K., Wallenius, M., Origin assessment of uranium ore concentrates based on their rare-earth elemental impurity pattern; Radiochim. Acta 98 (2010) 1–8

10.	Varga, Z., Wallenius, M., Mayer, K., Age determination of uranium samples by inductively coupled plasma mass spectrometry using direct measurement and spectral deconvolution; J. Anal. At. Spectrom., 25 (2010) 1958–1962

11.	Varga, Z., Öztürk, B., Meppen, M., Mayer, K., Wallenius, M., Apostolidis, C., Characterization and classification of uranium ore concentrates (yellow cakes) using infrared spectrometry; Radiochim. Acta 99 (2011) 807–813

12. Varga, Z. et al., Measurement of sulphur isotopic ratio for the nuclear forensic investigation of uranium ore concentrates (yellow cakes) (this conference)

13. Hrnecek, E. et al., Strategies for DNA Analysis from Contaminated Forensic Samples (this conference)

14. Varga, Z. et al., Proof of Principle for the Preparation and validation of an uranium age dating reference material (this conference)

15. Ho Mer Lin, D. et al., Exploring spectroscopic and morphological data as new signatures for uranium ore concentrates (this conference)