## Slide 1: CEA research programs related to the Severe Accident phenomenology in the lower plenum of a SFR
R. Clavier, N. Seiler, A. Lecoanet, B. Bigot, C. Brayer, J. Francescato, R. Chauvin, C. Treol, A. Avrit, P. Sciora, V. Petiteau
IAEA Technical Meeting on the Safety Approach for Liquid Metal Cooled Fast Reactors and the Analysis and Modelling of Severe Accidents, 13-17 March 2023

## Slide 2: Introduction: Context
Severe Accident sequence typically caused by an Unprotected Loss Of Flow (ULOF) on an ASTRID-like Sodium Fast neutron Reactor (~1500 MWth)
  Degradation of fuel assemblies  formation of Corium
  Opening of the Transfer Tube (TT)
  Transfer of the corium through the TT before power excursion in the core
  Downwards relocation of the corium in the lower plenum
Purpose of this presentation: give an overview of the research activities at CEA on the behaviour of corium in the lower plenum of a SFR

## Slide 3: Situations of interest in the lower plenum
Following the arrival of corium in the lower plenum through a TT:
  Fragmentation of the corium jet, more or less intense depending of the physical conditions in the sodium, with antagonist effects regarding the safety:
    Cold sodium (early relocations)  Intense
      Solidification of the debris  Safety +
      Risk of vapour explosions  Safety -
    Hot sodium (later relocations)  Weak
      Jet impingement, ablation of CC  Safety -
      Corium spreading on CC  Safety +
  Debris bed on CC, following sedimentation, may stabilize or not depending on the competition between:
    New arrival of corium  Safety –
    Self-levelling of debris  Safety +
      Risk of neutron criticality and re-melting of debris
  Corium pool on CC after corium jet spreading or re-melting of debris, may stabilize or not depending on the heat removal by the sodium
      Risk of ablation of the core catcher

## Slide 4: Contents
Fuel-Coolant Interaction
  SCONE calculation tool (CFD)
  SERUA experiments
  SAFETY experimental program
Jet impingement on the core catcher
  HAnSoLO and JIMEC experiments
  Simulation
Debris bed behaviour
  Thermal-hydraulic behaviour of the debris bed
  Neutron reactivity of the debris bed
Corium pool behaviour
  0D transient modelling: PROCOR-CC
  CFD simulations of corium pools
Conclusions

## Slide 5: Fuel-Coolant Interaction
1

## Slide 6: The SCONE simulation tool: presentation
Mechanistic code to simulate the Fuel-Coolant Interaction (Multiphase-multi-component):
  Multi-fluid, multi-material numerical fluid flow simulation software for 3D calculations with fast transients
  Eulerian description of Na liq / vap, continuous corium and fragmented corium (multi-group)
  3 conservation equations (mass, energy, momentum) are solved for each phase. The closure laws will carry the physics of the interaction and couplings between the phases.
Software for COrium sodium (Na) Evaluation

## Slide 7: SCONE – MMICADO – TRUST architecture
Main development phases since 2017 (development plan):
  2019: SCONE → MMICADO (“high level” numerical platform based on DUNE numerical platform) + SCONE (physical application)
  2023: (on-going) Replacement of the DUNE numerical platform by TRUST (CEA)
Models &
closure laws
SCONE
Models &
closure laws
microSCONE
(micro scale)
MMICADO
Mesh-based Multiphase Interactions Capabilities for severe Accident Dedicated cOdes
Numerical platform
Management of phases, fields, laws, data (XML), models
Multi-phase models + common numerical methods
Common closure laws
TRUST platform
Schematic view of the integration of SCONE into TRUST
“BALTIK”: Building Application Linked with TrioCFD Kernel

## Slide 8: Elements of verification
Multi-phase management
  Observation: motion of different phases with imposed velocities within a carrying phase
  Phase separation
Development and Verification of the ICE numerical scheme implementation: Shock wave propagation in 2D
Extension of shock wave propagation to a 2D system
Particles progression versus time
1D Test of sedimentation (test TRUST)

## Slide 9: SERUA experimental program at CEA
Modelling of FCIs in SFRs at the scale of a corium droplet:
  Characterize heat transferts during sodium film boiling around a corium droplet
  Identify the point where the vapor film becomes unstable
Lack of experimental data: only one experiment with sodium (Farahat PhD thesis, 1972), with limited instrumentation
Main purpose: perform a set of controlled immersions of a hot tantalum sphere (~2500°C, 25.4 mm diameter) in liquid sodium close to saturation (~850 °C)
SERUA Facility under construction at Cadarache
  2024: Commissionning tests: First tests will be conducted in sodium at 300-400°C
  2025: Test series with variation of and
Sodium boiling Experimental Rig for Understanding of fuel-coolant interaction

## Slide 10: SERUA experiments: Principle
1 – Inductive heating of Tantalum sphere at ~2500 °C
2 – Quenching in saturated sodium (~850 °C)
3 – Study of film boiling around the sphere
Study of the boiling regimes at imposed temperature ():
  Film boiling (beyond the Lidenfrost point)
  Transition (below the Lidenfrost point)
  Nucleate (end of experiment)

## Slide 11: SAFETY (formerly PLINIUS-2)
New experimental platform for Severe Accidents to replace the current PLINIUS platform at CEA Cadarache and extend experimental capabilities to more representative prototypical masses:
  A furnace able to melt ~100 kg of UO2-containing prototypical corium
  A 2nd hall to carry out experiments with up to ~500 kg uranium thermite
  Possibility to handle liquid sodium with a dedicated sodium loop
  For SFRs and LWRs
  X-ray instrumentation to observe the FCI phenomena.
Commissioning tests expected end 2026, 1st test section in 2027/28 dedicated to the study FCI with prototypical materials:
  Fragmentation (1st test section, left)
    Smaller mass
    Thinner test section
      observable with X-rays
  Explosion (2nd test section, right)
    Larger mass
11

## Slide 12: Jet Impingement on the core catcher
2

## Slide 13: Framework
  ASTRID-like Core catcher: metallic material (Steel / Molybdenum)
  2-phase corium (oxide / metallic)  2 single-phase cases to be considered:
    Oxide (mainly UO2)   Solid crust above liquid metal at the impact point (left figure)
    Metallic (mainly Steel)   No crust at the impact point (right figure)
  Corium crust acts as a thermal resistance between the jet and the core catcher
  Ablation slower in the case of an oxide jet
  Metallic jet is more severe  studies focus on this case
Metallic CC
Corium Jet
Corium crust
Molten CC
Oxide corium jet
Metallic corium jet
No crust
 Faster ablation

## Slide 14: Objectives and organisation
Numerical simulation
  Perform CFD simulation of the jet impact and CC ablation → on-going Ph.D. thesis (A. Avrit) to simulate the thermal erosion of a surface by an immersed jet
  Need for experimental data for validation
Experimental programs including analytic (with simulant materials) and prototypic experiments:
  Analytic experiments: HAnSoLO (water/ice system) at LEMTA → Understanding of governing phenomenon
  Prototypic experiments: JIMEC (steel/steel system) at KIT → Confirmation of anticipated behaviour with real materials
HAnSoLO
(water/ice)
JIMEC
(steel/steel)
Programs performed in the frame of European projects ESFR-SMART and ESFR-SIMPLE

## Slide 15: CFD simulation of the thermal erosion due to an immersed jet
Initial Solid
Temperature (K)
CFD Simulation (OpenFOAM)
Result of 2D simulation
Adaptation of the HAnSoLO experiments to produce immersed jets

## Slide 16: CFD simulation of the thermal erosion due to an immersed jet
Importance of turbulence in the jet at the inlet boundary → Over estimation of the ablation velocity when no turbulence is considered at the inlet boundary
  Generation of turbulence at the inlet boundary using the method proposed by Poletto et al., 2013 to ensure zero divergence at the boundary
  LES simulation to account for turbulence in the jet with WALE model for small scale modelling
Treatment of the fusion of the impacted wall:
  Penalization method proposed by Voller et Prakash, 1987
  Requires only to add source terms in the Navier-Stokes equations
  Supports implicit resolution
On the mid-term, the objective is to perform similar simulation in the TRUST platform (CEA)

## Slide 17: Debris bed behaviour
3

## Slide 18: Framework and objectives
Evolution of the debris bed after sedimentation (short term):
  Heat removal by the sodium → boiling
  Particles at the surface of the bed are driven by the liquid/vapor flow → boiling self-levelling
Related safety issues:
  Cooling sufficient to evacuate all the residual power? → re-melting of the debris?
  Does the bed remain neutronically sub-critical? → transient power excursion in the debris bed?
Self-levelling has a positive impact on both aspects because of the increase of the surface / volume ratio, but arrival of new corium material may cancel this effect.
CEA adopts a seperate effect approach:
  Transient description of the self-levelling of debris bed in sub-critical configuration
  Evaluation of the neutron criticality of debris
Figure from Cheng et al. 2018

## Slide 19: Transient description of self-levelling
Application of the Volume Averaging method proposed by Whitaker, 1986 to the 3-phase local boundary value problem
  Derivation of macroscopic equation structures
  Derivation of closure problems for the macroscopic properties of the medium
Definition of a practically operable model:
  Resolution of the closure problems necessitates DNS on a REV
  Or incorporation of empirical closure relations
  Implementation in OpenFOAM (on-going)
Mid-term objective: implement this modelling into the TRUST plaform
Local Problem
Deviation Problem
Closure Variable Problems
Unclosed Averaged Problem
Closed Averaged Problem
Closure Relations
Volume Averaging
Gray decomposition
Determine sources
One per source

## Slide 20: Neutron reactivity of debris beds
Evaluation of the neutron reactivity (static) of a debris bed in postulated configurations
  Shape: Cylinder, Cone, Several cones
  Composition: Fuel / Structure ratio, sodium content, bed porosity
    → What is the critical mass?
Example (right):
  Cylindrical shape
  74% fuel / 26% structure
  Porosity: 40%
    → 3.3 increase factor on the critical mass when the radius increases from 150 cm to 300 cm
  Next step: evaluation on more realistic configurations obtained from the previous self-levelling model.
Fuel mass in the corium [kg]
Case: 1 homogeneous cylindrical bed – Porosity 40% - fuel/steel ratio 74/26

## Slide 21: Corium pool behaviour
4

## Slide 22: Framework and objectives
Mid-term and long-term behaviour of the liquid corium on the core catcher
Modelling approach
  Integral modeling: PROCOR-CC
  CFD simulation of corium pools
Related experiments
  LIVE-ESFR experiments at KIT
Schematical view of a corium pool on an ASTRID-like Core Catcher

## Slide 23: Integral modeling with PROCOR-CC
PROCOR platform:
  Dedicated to fast-running transient calculations of Severe Accidents
  Historically dedicated to PWRs, currently extended to SFRs
    → PROCOR is intended to incorporate all the fast-running calculation tools for Severe Accidents at CEA
PROCOR-CC modelling (under implementation):
  Transient zone model for two-layer stratified corium pool
  Corium heat flux repartition : dimensionless correlations
  Determination of the crust thickness
  Lower sodium circulation & cooling (thermosiphon)
Propagation of Corium - Core Catcher

## Slide 24: CFD simulations of corium pools on the core catcher
Need to better characterize the corium pool thermal-hydraulics, in particular to better predict the heat fluxes on the thermal structures of the core catcher (average and spatial repartition)
Strategy : CFD simulation of corium pools on the core catcher: TRUST/TrioCFD
  DNS over partial geometries
  Large-Eddy-Simulation (LES) using turbulence modelling for small scales lower than Taylor scales determined with DNS
  Derivation of an adapted RANS modelling
… in relation with dedicated experiments: LIVE-ESFR
  Liquid corium pool with simulant material (eutectic mixture KNO3-NaNO3)
    Representative conditions in terms of internal Rayleigh number:
    Prandtl number higher than the one of the corium: vs
  Validation point at and study of the effect of the Prandtl number on turbulence with CFD calculations.

## Slide 25: Conclusions
5

## Slide 26: Conclusions
  Following the ASTRID program, CEA Severe Accident R&D teams are conducting research programs to simulate the behaviour of corium in the lower plenum of a SFR
    Objective: enable the safety demonstration of the Core Catcher
  Phenomenological analysis emphasizes 4 situations of interest:
    Fragmenting corium jet over the Core Catcher
    Jet impingement on the Core Catcher
    Solid debris bed on the Core Catcher
    Liquid corium pool on the Core Catcher
  Dedicated research programs have been launched on each situation, including:
    Development of 0D Fast-running simulation tools
    Development of CFD simulation tools
    Dedicated experiments
  Objective to converge all developments in the mid-term:
    0D fast-running simulation tools PROCOR platform
    CFD simulation tools → TRUST platform

## Slide 27: Overview of experimental programs and collaborations
Theme | Ongoing Exp. |  | Future SAFETY (PLINIUS-2) |  | Codes | Collaborations
FCI: FRagmentation EXPLOsion | SERUA (CEA/Cad.) MELT steel operated by JAEA |  | PLINIUS2-FR (with XR) PLINIUS2-EXPLO (Large masse) |  | MMICADO SCONE EUROPLEXUS | Japan: JAEA
Jet impingement on core catcher | HANSOLO (Univ. of Lorraine) JIMEC (KIT) |  | PLINIUS2-IMPACT |  | PROCOR-CC TRIOCFD | Univ. de Lorraine Germany: KIT
Corium interaction with core catcher | LIVE-ESFR (KIT) |  | PLINIUS2-Core Catcher |  | PROCOR-CC TRIOCFD | Germany: KIT

## Slide 28: References
S. Whitaker, “Flow in porous media I: A theoretical derivation of Darcy’s Law”, Transp. Porous Med., vol. 1, pp. 3-25, 1986
Voller, V. R. et Prakash, C. A fixed grid numerical modelling methodology for convection-diffusion mushy region phase-change problems. International Journal of Heat and Mass Transfer, 30(8), 1709‑1719, 1987 https://doi.org/10.1016/0017-9310(87)90317-6
Poletto, R., Craft, T. et Revell, A. A New Divergence Free Synthetic Eddy Method for the Reproduction of Inlet Flow Conditions for LES. Flow, Turbulence and Combustion, 91(3), 519‑539, 2013 https://doi.org/10.1007/s10494-013-9488-2
S. Cheng, J. Cui, Y. Quian, P. Gong, T. Zhang, S. Wang, G. Jiang, “An experimental investigation on flow-regime characteristics in debris bed formation behavior using gas-injection”, Annals of Nuclear Energy, vol. 112, pp. 856-868, 2018

## Slide 29: Appendix

## Slide 30: SERUA experiments: qualification
3 – Ta sphere inductive heating up to 2500°C
 VITI furnace of the PLINIUS experimental platform
1 – Na Heating up to 850°C
 DOLMEN facility of the PAPIRUS Platform
2 – Ta sphere Instrumentation
 Coef-h® technology (sensor + inverse conduction algorithm, CEA patent)