## Slide 1
Christian Cupak
TU Wien, Institute of Applied Physics
cupak@iap.tuwien.ac.at
christian.cupak@gmx.at
2nd Technical Meeting on the Collisional-Radiative Properties
of Tungsten and Hydrogen in Edge Plasma of Fusion Devices
Sputtering of rough systems: experiments and simulations
Diploma Thesis
Fusion@ÖAW Vienna, Austria
This work has been carried out within the framework of the EUROfusion Consortium, funded by the European Union via the Euratom Research and Training Programme (Grant Agreement No 101052200 — EUROfusion). Views and opinions expressed are however those of the author(s) only and do not necessarily reflect those of the European Union or the European Commission. Neither the European Union nor the European Commission can be held responsible for them.
Notes: Thank you very much for the warm introduction!
First of all I‘d like to thank the organisers of this conference to give me the opportunity to present the results of my research, focusing on the effect of surface roughness on sputtering, here at the 3S conference.

## Slide 2
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Acknowledgements
Many thanks to colleagues and research partners!
Notes: In addition, I would like to thank my colleages at TU Wien, and also our international research partners,
from Germany to Sweden
to Spain, and also to Finland.
We appreciate your support and look forward to our future collaborations.

## Slide 3
Plasma-wall interaction, space weathering, surface cleaning in UHV, PVD
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Sputtering
Notes: In my talk, I will focus in detail on the contribution of surface roughness on the sputtering of materials under ion bombardment.
Generally, sputtering theory and many numerical simulation codes show good agreement to experiments with perfectly flat surfaces, and this is established since years.
However, real surfaces are rarely flat, but have a certain surface roughness which can change sputtering yields severely.
This is an ongoing topic of investigation, especially in the field of Plasma Wall interaction for nuclear fusion reactors, which is my background.
In addition, this is also of relevance in example for space weathering, where the rough surface of celestial bodies is exposed to solar wind ions
Furthermore, this is also relevant for industrial coating techniques like physical vapour deposition, where a crucible may develop a surface roughness.
Therefore, our desire was to find a robust roughness parameter, which enables to predict the effects on the sputter yields.

## Slide 4
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Sputtering
Plasma-wall interaction, space weathering, surface cleaning in UHV, PVD
Sputtering theory, simulations → for perfectly flat surfaces
C. Cupak, Master Thesis,
TU Wien 2019
C. Cupak et al., Appl. Surf. Sci., 570, 2021
Notes: In my talk, I will focus in detail on the contribution of surface roughness on the sputtering of materials under ion bombardment.
Generally, sputtering theory and many numerical simulation codes show good agreement to experiments with perfectly flat surfaces, and this is established since years.
However, real surfaces are rarely flat, but have a certain surface roughness which can change sputtering yields severely.
This is an ongoing topic of investigation, especially in the field of Plasma Wall interaction for nuclear fusion reactors, which is my background.
In addition, this is also of relevance in example for space weathering, where the rough surface of celestial bodies is exposed to solar wind ions
Furthermore, this is also relevant for industrial coating techniques like physical vapour deposition, where a crucible may develop a surface roughness.
Therefore, our desire was to find a robust roughness parameter, which enables to predict the effects on the sputter yields.

## Slide 5
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Sputtering
C. Cupak et al., Appl. Surf. Sci., 570, 2021
Plasma-wall interaction, space weathering, surface cleaning in UHV, PVD
Sputtering theory, simulations → for perfectly flat surfaces
Real surfaces not flat → surface roughness
Can we identify a roughness parameter to predict sputtering yields?
Notes: In my talk, I will focus in detail on the contribution of surface roughness on the sputtering of materials under ion bombardment.
Generally, sputtering theory and many numerical simulation codes show good agreement to experiments with perfectly flat surfaces, and this is established since years.
However, real surfaces are rarely flat, but have a certain surface roughness which can change sputtering yields severely.
This is an ongoing topic of investigation, especially in the field of Plasma Wall interaction for nuclear fusion reactors, which is my background.
In addition, this is also of relevance in example for space weathering, where the rough surface of celestial bodies is exposed to solar wind ions
Furthermore, this is also relevant for industrial coating techniques like physical vapour deposition, where a crucible may develop a surface roughness.
Therefore, our desire was to find a robust roughness parameter, which enables to predict the effects on the sputter yields.

## Slide 6
Local incidence angles
Redeposition
Shadowing
Second order sputtering
most ion beam / plasma experiments modify surface
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Roughness effects on sputtering
computational costs high for simulation codes (3D – BCA, MD)
M. Küstner et al., Nucl. Inst. Meth. Sec. B, 145, 1998
Notes: At first, I would like to talk a little more about the individual roughness effects that can occur during ion bombardment.
In example, the local inclination of a surface feature can affect the actual ion incidence angle, which alters the local sputter yield and reflection coefficients.
Also, redeposition of sputtered atoms on neighbouring surface features can severely reduce the total sputter yield
Shadowing of certain surface areas can also occur, especially under grazing ion incidence.
Finally, secondary sputtering may also contribute to the total erosion, if reflected ions hit the surface again.
These individual effects are hard to investigate, especially since most ion beam experiments would modify the surface dynamically.

## Slide 7
Experimental method QCM
SPRAY simulation code
Conventional roughness effects on sputtering
Outlook
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Outline
Notes: These conditions motivated us to investigate this field more, both experimentally and numerically, which can be seen here in the outline:
One the one hand, we used a so-called QCM to experimenteally investigate the connection between surface roughness and the total sputter yield, with a special focus on static sputter yields, or in other words: when the surface is not yet altered due to the ion beam.
Furthermore, we developed a new raytracing simulation code which allows any larger surface sections as input, enabling to study the roughness effect for a liberal choice of topographies.
With both approaches, we then worked on the key goal, which is to identify a good roughness parameter, allowing to characterise rough surfaces to even enable predictions of total sputter yields.

## Slide 8
QCM = Quartz Crystal Microbalance
Sauerbrey equation [1]
Thin layer on top (e.g., W) -> ion beam experiments
SiO2
Au
Au
e.g., W
[1] G. Sauerbrey, Z. Physik 155 (1959), 206-222
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Experimental Approach: QCM
Notes: In this context, I will shortly present our experimental approach: The QCM. QCM stands for quartz crystal microbalance. The fundamental basis of this technique is a thin quartz crystal with 2 gold electrodes on each side, forming a piezoelectric resonator.
When this quartz is provided with an alternating current with corresponding eigen-frequency, the quartz performs shear vibrations due to the piezoelectric effect.
With the sauerbrey equation, a direct connection between this resonance frequency and the mass of the quartz can be drawn. In other words, small mass changes can be determined by recording the change of this resonance frequency.
It is very useful for us, that this method is still working if a thin layer of different material, like Tungsten, is applied on the quartz, which is, in our experiments, exposed to an ion beam for erosion studies.
At our institute, measuring with a QCM has a long history. Specialised electronics and resonators allow very high sensitivity for our QCM. In example, it is possible to achieve a mass change sensitivity of 10 to the power of -4 tungsten monolayers per second.
Due to this high sensitivity, we were able to use very small ion fluxes for our experiments on the rough surfaces, which therefore allowed to neglect surface alteration. This is very important, since dynamic changes of the rough surface would limit conclusions in the context of this project.
The classic QCM configuration can be seen here: The quartz is directly bombarded by ions which cause a mass loss.
In addition, we developed a cacher QCM configuration, where the quartz is used to probe the angular distribution around the target.
My mentor Friedrich Aumayr will provide a more detailed overview to the QCM in his talk on Thursday.

## Slide 9
At TU WIEN:
Specialised electronics + SC-cut quartz [1]
≈ 90 pg/cm²/s (3 ⋅ 10-4 W monolayers/s)
Low ion fluxes for minimal surface alteration
Monoenergetic, mass-filtered ion beam
In-situ sputtering yield measurement
Classic Target QCM: sputtering causes mass reduction [1]
Catcher QCM: deposited atoms cause mass increase [2]
[1] R. Stadlmayr et al., Rev. Sci. Instrum. 91 (2020), 125104
[2] B. Berger et al., NIMB 406 (2017), 533-537
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Experimental Approach: QCM
A = ion beam
B = sputtered atoms C = reflected ions
D = QCM
Notes: At our institute, measuring with a QCM has a long history. Specialised electronics and resonators allow very high sensitivity for our QCM. In example, it is possible to achieve a mass change sensitivity of 10 to the power of -4 tungsten monolayers per second.
Due to this high sensitivity, we were able to use very small ion fluxes for our experiments on the rough surfaces, which therefore allowed to neglect surface alteration. This is very important, since dynamic changes of the rough surface would limit conclusions in the context of this project.
The classic QCM configuration can be seen here: The quartz is directly bombarded by ions which cause a mass loss.
In addition, we developed a cacher QCM configuration, where the quartz is used to probe the angular distribution around the target.
If you are more interested in this method, stay tuned for Friedrich Aumayr‘s talk on Thursday.

## Slide 10
  Our in-house developed code SPRAY
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Simulation of rough surface sputtering
SPRAY = SPuttering simulation via RAYtracing of particles
Flat surface repository data from BCA codes
(sputtering yields, emission vectors)
2) Topography input (limitless), e.g., by AFM
3) Raytracing loop
No cluster necessary, fast, benchmarked with exp. data (QCM)
Raytracing
BCA
  Cupak et al., Appl. Surf. Sci. 570 (2021), 151204
geometric roughness effects
Notes: At next, I introduce you to our numerical method used: The raytracing code SPRAY.
SPRAY stands for SPuttering simulation via RAYtracing of particles.
Here, a repository data set from earlier conducted BCA code simulations is used (for instance from SDTRimSP). The repository is obtained for a perfectly flat surface of given composition.
Afterwards, a topography input of liberal size, like from AFM, is loaded to the code
Then, the raytracing algorithm projects the repository data to the neighbourhood around each individual ion impact.
The code is parallelised, runs under Python 3 and can be executed on desktop PCs without need for cluster infrastructure.
Also, all former mentioned surface roughness effects like Changes of local ion incidence angle, shadowing, redeposition or secondary sputtering are included.

## Slide 11
Experimental method QCM
SPRAY simulation code
Conventional roughness effects on sputtering
Outlook
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Outline
Notes: These conditions motivated us to investigate this field more, both experimentally and numerically, which can be seen here in the outline:
One the one hand, we used a so-called QCM to experimenteally investigate the connection between surface roughness and the total sputter yield, with a special focus on static sputter yields, or in other words: when the surface is not yet altered due to the ion beam.
Furthermore, we developed a new raytracing simulation code which allows any larger surface sections as input, enabling to study the roughness effect for a liberal choice of topographies.
With both approaches, we then worked on the key goal, which is to identify a good roughness parameter, allowing to characterise rough surfaces to even enable predictions of total sputter yields.

## Slide 12
SPRAY code for large numerical study:
1) Scaling nm- to µm roughness from microscopy images of W samples
2) Artificially smoothed/roughened images
3) Also use a purely artificial rough surface (Gaussian distr. height values)
4) Simulate sputtering yields with SPRAY (here, 2 keV Ar -> W)
scaling s
s = 0.2
s = 1 (original)
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Conventional roughness effects on sputtering
  Cupak et al., Appl. Surf. Sci. 570 (2021), 151204
Is there a roughness parameter enabling to predict sputter yields of rough surfaces?
Notes: We then used the samples to conduct a parameter sweep study by changing the global ion incidence angle for a final benchmark.
As you can see, the data are in good agreement as well. Interestingly, we could identify that even the nanometre scale roughness of sample 1 had an effect under grazing ion incidence, compared to a purely flat plane surface.
Based on the benchmark, we then prepared for a larger numerical study. We aimed to sweep roughness from nanometre to microns regime, by applying a scaling factor to microscopy images which I’ve shown you before.
Also, a completely artificial surface was chosen, obtained from a gaussian height values generator
For example, when the scaling factor is 1, we receive the original surface, but if it higher or as here, lower, the surface is smoothed.

## Slide 13
Which roughness parameter to predict sputter yields of rough surfaces?
RMS
RMS:
No consistent trend
RMS not reliable
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Conventional roughness effects on sputtering
SPRAY sweep : surface inputs with rising roughness
(2 keV Ar+ on W, 0° and 60°)
Characterise roughness by root mean square (RMS) → common in science and technology
  Cupak et al., Appl. Surf. Sci. 570 (2021), 151204
2 keV Ar on rough W
Notes: The large stack of images was first characterised by RMS and then piped into the SPRAY code for a sweep. Here you can see results again for 2keV Ar irradiation, under 0 and 60 deg incidence angle. The roughness of the surfaces was characterised first by the root mean square roughness, which is commonly used in science and technology
As you can see, no consistent trend was found. The individual data stacks did show independend behaviour. Furthermore, the same RMS value can lead to completely different sputter yields. Therefore, we found the RMS parameter not to be reliable.

## Slide 14
Can you distinguish the mountain landscape from the AFM image?
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Conventional roughness effects on sputtering
Notes: With this in mind, I would like to discuss this also from an alternative point of view.
When I was hiking in the mountains, I often observed the similarities which you can see from AFM images of rough surfaces and alpine views. Therefore I would like you to ask the question, which sketch resembles a mountain image, and which one the AFM image…?
I give you some seconds to make a personal judgement before I solve this small riddle…

## Slide 15
AFM image rough W surface RMS = 420 nm
Dachstein, Austria, 31.12.2021 RMS = several 100 m
x 109
scale-independent parameter desired
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Conventional roughness effects on sputtering
Notes: So, here is the answer!
The left side shows an AFM image of a rough tungsten surface with about 420nm root mean square roughness.
The right hand side shows many mountains around the Dachstein in Austria– I guess the RMS would be in the range of some 100 meters.
There is a scale difference of 10 to the power of 9, while the appearance is very similar.
But why do I tell you this. I think this also motivates a scale-independent parameter to describe sputtering of rough surfaces, since sputtering is a very small scale atomistic process. I think, it can be assumed that as long as the collision cascade in the target material is substantially smaller than the expansion of the mountains on a rough surface, the actual scale becomes unimportant, limiting therefore parameters like root mean square roughness.

## Slide 16
Scale-independent parameter:
Mean inclination angle δm
Calculation:
Quantitative surface data (AFM,...)
Calculate local surface normal vectors
Histogram → mean value
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Conventional roughness effects on sputtering
  Cupak et al., Appl. Surf. Sci. 570 (2021), 151204
Notes: Therefore, I‘d like to introduce you to an alternative metric, the mean inclination angle delta m.
This can be interpreted as a mean tilt of all surface features, therefore a scale independent representative.
It can be calculated relatively simple:
At first, quantitative data like from AFM is needed,
Then, all local surface normal vectors are needed. Our option to achieve this was to create a mesh from the AFM data, and perform a triangulation of the data.
All surface vectors from the triangles can then be projected towards the global surface normal, which enables to plot the angles as a histogram.
Finally, just the mean angle is required, which can characterise the surface roughness.
Just as a rule of thumb: delta values below 10 are still representing very smooth surfaces.
Up to 35°, I‘d interpret them as moderately rough, while beyond, the surfaces start to appear more spiky.

## Slide 17
Which roughness parameter is good to predict effective sputtering yields of rough surfaces?
RMS
δm
RMS:
No consistent trend
RMS not reliable
δm
Common trends found
0°: δm acts like increase of ion incidence angle
60°: linear fit found
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Conventional roughness effects on sputtering
  Cupak et al., Appl. Surf. Sci. 570 (2021), 151204
2 keV Ar on rough W
Notes: We then used this delta parameter to characterise the large stack of surfaces used for SPRAY simulations, and suddenly, we obtained much better trends!
For instance under 60° degree incidence, we see a common linear decrease for all images.
Under normal incidence, we even see a slight increase of the sputtering yield up to moderate roughness of about 20°.
This is explained by the dependence of the yield on incidence angle, as known for flat surfaces, while redeposition is not yet strong enough to be effective.
This changes for rougher surfaces dramatically.
Generally, we concluded that indeed the delta m parameter is a good metric for rough surface sputtering.

## Slide 18
2 keV Ar on rough W
  Which roughness parameter is good to predict effective sputtering yields?
Double sweep: roughness + ion incidence angle
δm : empirical fit function → prediction [1]
Supported by mathematical model (for Gaussian-rough surfaces) [2]
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Coventional roughness effects on sputtering
δm
RMS
  [1] Cupak et al., Appl. Surf. Sci. 570 (2021), 151204
  [2] Szabo et al., Surf. Interfaces 30 (2022), 101924
→ mean inclination angle δm
Notes: We then extended this study also towards another dimension.
To fully investigate the trends, we included variable ion incidence angles to the sweep and the results show, overall, a much more consistent trend with the delta m parameter.
This even allowed to deduce an empiric fit formula, which enables to predict sputter yields of a rough surface with a given roughness parameter delta m.
It has to be mentioned, that this primarily holds for conventional, isotropically rough surfaces
For those of you who are more interested, I suggest to take a look on our recent paper in applied surface science.
I also want to draw attention that our empirical experiences were recently supported by an analytical concept established by my colleague Paul Szabo.
He linked the delta m parameter to the ratio of root mean square roughness over autocorrelation length.
With this, I come to the end of my talk. If any questions arised, I‘d be happy to answer them now. Thank you for your attention!

## Slide 19
Comparative study with SPRAY, QCM and MD: Nano-columnar W (NCW)
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
SPRAY for complex surface roughness
SEM
NCW on QCM -> direct sputtering measurements
50 nm diameter, 500 nm high NCs, areal density 58%
SPRAY can well predict sputtering yield of NCW
Studies with Ar and D ions [1,2,3]
PVD on QCM resonator by R. González-Arrabal (UPM)
[1] A. Lopez-Cazalilla & C. Cupak et al., Phys. Rev. Mater. 6 (2022), 075402
[2] C. Cupak et al., Phys. Rev. Mat. 7 (2023) 065406
[3] J. Brötzner et al., Nucl. Mater. Energy 37 (2023), 101507
2 keV Ar on NCW
-> also MD results available, see Talk by F. Granberg

## Slide 20
Experimental method QCM
SPRAY simulation code
Conventional roughness effects on sputtering
Outlook
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Outline
Notes: These conditions motivated us to investigate this field more, both experimentally and numerically, which can be seen here in the outline:
One the one hand, we used a so-called QCM to experimenteally investigate the connection between surface roughness and the total sputter yield, with a special focus on static sputter yields, or in other words: when the surface is not yet altered due to the ion beam.
Furthermore, we developed a new raytracing simulation code which allows any larger surface sections as input, enabling to study the roughness effect for a liberal choice of topographies.
With both approaches, we then worked on the key goal, which is to identify a good roughness parameter, allowing to characterise rough surfaces to even enable predictions of total sputter yields.

## Slide 21
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Outlook
[1] K. Schlueter et al., Phys. Rev. Lett. 125 (2020), 225502.
[2] G. Hobler, Nucl. Instrum. Methods Phys. Res., Sect. B 96 (1995), 155-1
[3] A. Mutzke et al., IPP Report: SDTrimSP Version 6.00 (2019).
Inplementing crystalline texture effects in SPRAY
Sputtering yield also depends on orientation of crystal grains wrt. incoming ion direction [1]
Idea:
Use BCA codes sensitive to crystal texture for creation of extended repository data (e.g., IMSIL [2], or new SDTrimSP version [3] currently dev. by U. v. Toussaint and A. Mutzke)
AFM/CFM + EBSD maps to capture topography and crystalline texture of surfaces
Update SPRAY to include both local topography and crystalline texture
Potential challenges:
Repository data size limitation (RAM)
EBSD requires grain sizes >100nm
K. Schlueter et al., Int J Refract Hard Met, 88 (2020), 105189.

## Slide 22
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Outlook
[1] J. Romazanov et al., Nucl. Mater. Energy 18 (2019) 331-338.
[2] A. Eksaeva et al., Nucl. Mater. Energy 19 (2019) 13-18.
Inplementing electromagnetic forces
Altered height of surface segments, via local particle flux balances after a given timestep
Local fluxes already available (after update for celestial bodies)
Potential challenges:
Increase of computational time
Similarity to ERO2.0 code [1,2]
Inplementing dynamic sputtering mode
Current raytracing: straight-line particle trajectories
In fusion plasma: charged particles, EM forces
Leads to different transport / redeposition
Potential challenges:
Large change to the code structure, trace charge states
Additional data input (plasma background)
Increase of computational time
Similarity to ERO2.0 code [1,2]
time

## Slide 23
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Outlook
[1] Szabo et al., Surf. Interfaces 30, 2022, 151204
[2] He et al., ACM SIGGRAPH Comput. Graph. 25 (1991) 175-186.
[3] Ertmer et al., Plasma Phys. Control. Fusion 63 (2020), 015008.
Application of δm concept for dynamic experiments (e.g., linear plasma device)
General relation between δm and sputtering yield is now available [1]
δm also affects intensity of specular light reflection from a surface [2]
Idea for a dynamic sputtering experiment:
a) Initial surface characterisation (AFM for δm; initial light reflection intensity)
b) Dynamic sputtering in linear plasma device
c) Follow intensity of light reflection; estimate δm and calculate sputter yield
d) Follow line radiation intensity of sputtered species [3]
e) Final surface characterisation
If c) and d) compare well over time, specular light reflection would be a tool to assess surface roughness (δm) + effects on W sputtering during dynamic experiments
Note: random (Gaussian) roughness assumed here; EM forces are neglected
2 keV Ar on rough W

## Slide 24
Outline
Diploma Thesis
Fusion@ÖAW Vienna, Austria
Summary
Cupak et al., Appl. Surf. Sci. 570, 2021, 101924 Szabo et al., Surf. Interfaces 30, 2022, 151204 A. Lopez-Cazalilla & C. Cupak et al., Phys. Rev. Mater. 6, 2022, 075402
δm
RMS
QCM and SPRAY
Sputtering of rough surfaces
Outlook and potentials
Raytracing
BCA
2 keV Ar on rough W
SPRAY for topography + crystal texture
Light reflection to assess δm during dynamic erosion
PhD Thesis C. Cupak (2023) https://doi.org/10.34726/hss.2023.76544
He et al., ACM SIGGRAPH Comput. Graph. 25 (1991) 175-186 J. Brötzner et al., Nucl. Mater. Energy; 37 (2023), 101507
QCM
SPRAY