## Slide 1
Energy, angular and atomic level distribution functions of sputtered tungsten based on spectroscopic investigations
S. Ertmer, O. Marchuk, M. Sackers, S. Brezinsek and A. Kreter

## Slide 2: Introduction
Sputtering occurs at solid surfaces at plasma boundary
Sputtering depends on impact energy and incident angle of incoming particles
Different sputtering regimes depending on impact energy
Sputtering at high impact energies well understood
In fusion research impact energy in the range of 100 eV
Energy and angular distribution of sputtered atoms remains open question
Sputtering in ground and/or excited level
[2] R. Behrisch and W. Eckstein "Sputtering by Particle Bombardment", Springer-Verlag (2007)
[2]
Important input parameters
For PWI codes, CRM and S/XB

## Slide 3: Experimental setup
Passive optical emission spectroscopy in the linear plasma device PSI-2
Energy and angular distribution: Line shape analysis by high wavelength resolution spectroscopy ( ≈ 10-6 vs. )
Initial atomic level population: Spectroscopic time-of-flight measurements by imaging spectrometer with high spatial resolution (50 µm/px)
conditions | argon plasma
Te | ≈ 3 eV
ne | ≈ 2 ∙1012 cm-3
Eimp | 70-150 eV
B | ≈ 90 mT
Tsurf | 300 K
High resolution OES
or

## Slide 4: I. Energy and angular distribution

## Slide 5: I. Energy and angular distribution
 | Energy distribution | Angular distribution
High impact energies | Thompson energy distribution [7] | Cosine angular distribution [8]
Low impact energies | Deviations from Thompson? | Butterfly angular distribution?!
 | Energy distribution | Angular distribution
High impact energies | Thompson energy distribution [2] | Cosine angular distribution [3]
[2] M W Thompson Phil. Mag., 1968
[3] R. Behrisch and W. Eckstein "Sputtering by Particle Bombardment", Springer-Verlag, 2007
[4] A. Goehlich et. al. J. Nucl. Mater., 1999
[5] D. Nishijima et al. J. Nucl. Mater., 2011
[6] M. Stepanova et al, J. Vac. Sci. Technol. A, 2001
Experimentally determined angular distributions of sputtered W atoms from a smooth surface bombarded by Ar [6]
Calculated angular distribution of W sputtered by Ar [5]
Experimental results of the energy distribution of sputtered W [4]
→ Better understanding of energy and angular distribution needed

## Slide 6: I. Energy and angular distribution
Line broadening effects lead to only one broad peak
Change in line shape with change in impact energy
Modeling becomes necessary

## Slide 7: I. Energy and angular distribution
Stronger line shape deformation for Al than for W (proof of principle)
Only explanation is light reflection
Erosion of surface leads to decrease in reflection
Al-target before and after exposure
Al-target in argon plasma Eimpact ≈ 110 eV
0° to the normal
0° to the normal
90° to the normal

## Slide 8: I. Energy and angular distribution
Stronger line shape deformation for Al than for W (proof of principle)
Only explanation is light reflection
Erosion of surface leads to decrease in reflection
Al-target before and after exposure
Al-target in argon plasma Eimpact ≈ 110 eV
0° to the normal
0° to the normal
90° to the normal

## Slide 9: I. Energy and angular distribution
Based on Doppler-shifted-emission model for reflected atoms [7]:
  Infinite target approximation (ITA)
  Cosine angular distribution
  Light reflection at surface (literature: 53%[8])
Adapted:
  Thompson energy distribution
Expanded:
  Zeeman Effect (@ 90 mT)
  Instrumental broadening
[7] S. Dickheuer et al. Physics of Plasmas 26, 073513, 2019
[8] W. S. M. Werner et al. J. Phys. Chem. Ref. Data 38, 2009
ITA model breaks for 90°!
-> Space-resolved model required!

## Slide 10: I. Energy and angular distribution
Space-resolved model
Spectral profile:
… Population density of the upper level
… Instrumental profile
… Instrumental profile
… Energy distribution function
… Angular distribution function
Infinite target approximation (ITA)

## Slide 11: I. Energy and angular distribution
[9] M. Sackers et al. Phys. Scr. 98 115603 (2023)
SRM – space-resolved model/finite size
ITA – infinite target approximation
[9]
[9]
Space-resolved model – solution in cartesian coordinates

## Slide 12: I. Energy and angular distribution
Space-resolved model – angular distribution
Angular distribution
[9] M. Sackers et al. Phys. Scr. 98 115603 (2023)
[9]
[9]
0°
90°

## Slide 13: I. Energy and angular distribution
 Taking the finite size into account allows to consistently model the spectra
120 eV Ar+
00
[10] A. Mutzke et al. IPP-Report 2019-02, (2019)
Ekin (eV) | 100 eV n b | 120 eV n b | 140 eV n b
ITA | 1.83(19) 1 | 2.31(6) 1 | 2.59(11) 1
SRM | 2.24(2) 0.47(3) | 2.13(3) 0.69(3) | 2.03(3) 0.83(5)

## Slide 14: II. Initial atomic level population

## Slide 15: II. Initial atomic level population
Input parameter for Collisional Radiative Models (CRM) and PWI-codes
Not well understood: TEXTOR experiments: population according to effective temperature led to unphysical electron temperature Te (1 eV) at a plasma of 30 eV [12]
Grotrian diagram of W
→ Better understanding of initial atomic level population needed
[11] nist.gov (visited on 24.11.2020)
[12] I. Beigman et al., Plasma Phys. Control. Fusion, 2007
[11]

## Slide 16: II. Initial atomic level population
Rate equation of level N in corona equilibrium
Position of maximum line intensity is proportional to velocity and reciprocal Einstein coefficient:
Angular distribution of sputtered particles leads to:
Ionization and geometrical losses lead to decreasing intensity
[13] O. Marchuk et. al. J. Phys. B: At. Mol. Opt. Phys (2018) Vol.51 025702
[13]
Electron impact excitation
Spontaneous emission

## Slide 17: II. Initial atomic level population
Experimental data: maximum of both lines at the same position
According to Thompson energy distribution:
Agreement only for ground term 5D0
Wavelength [Å] | Lower level | ∑ Einstein coefficient upper level [s-1] [9]
4982.593 | 5D0 | 5.31E+5
4008.751 | 7S3 | 1.65E+7
[11] nist.gov (visited on 24.11.2020)
[11]

## Slide 18: II. Initial atomic level population
Wavelength (Å) | Position maximum (mm) | Einstein coefficient upper level (s-1) [15] | Calculated velocity (m/s) | Relative proportion
4982.593 | 2.34 | 5.31E+5 | 1952 | 0.79
4294.605 | 2.21 | 1.32E+7 | 58212 | 0.94
[11] nist.gov (visited on 24.11.2020)
Grotrian diagram of W
[11]

## Slide 19: II. Initial atomic level population
Wavelength (Å) | Position maximum (mm) | Einstein coefficient upper level (s-1) [15] | Calculated velocity (m/s) | Relative proportion
4982.593 | 2.34 | 5.31E+5 | 1952 | 0.79
4843.810 | 1.80 | 3.37E+6 | 12132 | 0.56
[11] nist.gov (visited on 24.11.2020)
Grotrian diagram of W
[11]

## Slide 20: II. Initial atomic level population
Wavelength (Å) | Position maximum (mm) | Einstein coefficient upper level (s-1) [15] | Calculated velocity (m/s) | Relative proportion
4982.593 | 2.34 | 5.31E+5 | 1952 | 0.79
4244.367 | 4.05 | 1.44E+6 | 11664 | 0.96
[11] nist.gov (visited on 24.11.2020)
Grotrian diagram of W
[11]

## Slide 21: II. Initial atomic level population
Only ground state transition is in agreement with theory
All other transitions peak to late according to Einstein coefficient
[11]
[11] nist.gov (visited on 24.11.2020)

## Slide 22: Summary
I. Energy and angular distribution
Proof of light reflection in the line shape of sputtered atoms
In-situ light reflection measurements by modeling
Consistent modeling of optical emission spectra for both line of sights
 Simultaneous modeling of energy and angular distribution
II. Initial atomic level population:
High spatial resolution spectroscopy measurements
For a cold target (Tsurf= 300 K) and mono-energetic energy of the incident ions in the order of 100 eV, atoms are sputtered in the ground state 5D0
Exited levels 7S3 and 5Dx>0 are not populated during sputtering

## Slide 23: Backup- Outlook
Studying energy and angular distribution for different surface morphology, including nano structured ones
Removal of W-Fuzz
Laser absorption on W I to remove instrumental broadening
Laser induced fluorescence on W I for energy, angular and initial level distribution
0°
90°