## Slide 1: Facilitating SMR fuel fabrication from HALEU UF6
Dr. Marina Sokcic-Kostic

## Slide 2: Overview
  NUKEM’s fuel production history
  Major SMR concepts and their fuel
  SMR fuels from HALEU UF6 deconversion
  Metallic uranium vs. HTR TRISO fuel production route
  High temperature Small Modular Reactors (HT-SMRs)
THTR-300, Hamm-Uentrop

## Slide 3: 1. NUKEM’s Fuel Production History: UO2 and U metal
  NUKEM/Siemens Fuel plant (RBU, Reaktor Brennelement Union) in Hanau Wolfgang (Germany)
    1950’s: Fuel assemblies from U-metal, FR2 (Karlsruhe), ECO (ISPRA)
    1960’s: UAlx in Al, up to 93% U-235 (HEU), FA for material test reactors (MTR)
    1970’s: AUC pilot plant, 93% U-235 (HEU), for Oxide based (UO2) FA, production route for all German power reactors
  1980’s-2000’s: AUC/U metal plant (BATAN, Indonesia)
    for MTR by Siemens
    HALEU, up to 20% U-235
    Rework/recycling included

## Slide 4: 1. NUKEM’s Fuel Production History: HTR fuel
  1960’s: German HTR program
    NUKEM’s responsibility: Fuel specifications, Fuel element design and manufacturing process
  1970’s: HTR fuel plant (HOBEG) in Hanau (Germany)
    250 000 Fuel Spheres for experimental AVR, Jülich
    1 000 000 Fuel Spheres for THTR-300, Hamm-Uentrop
  2000’s: PBMR Project in South Africa (PBMR Pty. Lt.)
    Basic, Detail And Procurement Design
    Unfortunately stopped during procurement phase due to financial reasons
  2010’s: Laboratory-scale facilities
    Indonesia
    South Korea

## Slide 5: 1. The Spherical HTR Fuel Element

## Slide 6: 2. Major SMR concepts and their fuel
Small Modular Reactors (SMR)
IAEA definition:
Advanced reactor up to 300 MWe per module
Liquid-metal cooled SMR | 
Fuel | U metal alloy MOX (low fissile) Pu and DU
Neutrons | fast (mainly)
Coolant | Na, Hg, Pb, Sn, …
Example | Sodium-cooled fast reactor (SFR)
Water-cooled SMR | 
Fuel | UO2 pellets MOX (high fissile)
Neutrons | thermal
Coolant | Light water
Example | Pressurized water reactor (PWR)
Molten-salt SMR | 
Fuel | UF4 in molten salt also, with Pu (or Th)
Neutrons | fast or thermal
Coolant | Molten salt (F-, Li+, Be+)
Example | Molten salt fast reactor (MSFR)
Gas-cooled SMR | 
Fuel | UO2 TRISO particles
Neutrons | thermal
Coolant | He
Example | High temperature gas-cooled reactor (HTGR)

## Slide 7: 3. SMR fuels from HALEU UF6 deconversion

## Slide 8: 4. Metallic Uranium Fuel Production Route
      U metal production
      UF6 + (H2O/CO2/NH3) → AUC + (NH4F)
      AUC + (H2) → UO2 + (NH3/CO2/H2O)
      UO2 + 4HF → UF4 + (4H2O)
      UF4 + 2Ca → U + (2CaF2)
      Calciothermic reduction (4.)
Inside graphite crucible
Filled with UF4/Ca mixture (5 kg U)
Heating up to ignition
Regulus with more than 90% yield
Scrap recycled via recovery
AUC

## Slide 9: 4. HTR TRISO Fuel Production Route

## Slide 10: 4. HTR Fuel Production – Kernels
  Kernel Casting
    Drip casting of Kernels
    ADU Precipitation from Uranyl nitrate and additives
    UO2 or UCO-based

## Slide 11: 4. HTR Fuel Production – Kernels
vibro-dropped
dried
calcined
sintered
  Kernel Casting
  Ageing, Washing, Drying (AWD)
  Calcining
  Sintering
  Sieving, Sorting, Sampling and Portioning (SSSP)

## Slide 12: 4. HTR Fuel Production – Coating Facility
  NUKEM Coater
  Key equipment to achieve standard quality fuel
  Chemical Vapor Deposition (CVD) Coating with Acetylene, Propylene and MTS
  Sieving, Sorting, Sampling and Portioning (SSSP)
CVD Off-Gas Exhaust
Fluidized Bed Nozzle
Graphite Heating Element
Temperature Sensors
Water Cooling Jacket

## Slide 13: 4. HTR Fuel Production – Fuel Facility
  Fuel Compact or Fuel Sphere Pressing
  OCPs are filled into pressing moulds
Fuel Compacts
Fuel Sphere Pressing Line,
(NUKEM HOBEG, Hanau, Germany)
Fuel Spheres
OCP
MGP
CP

## Slide 14: 4. HTR Fuel Production – Fuel Facility
  Carbonizing (800 °C)
  Annealing (1900 °C)
  Final Quality Control
Fuel Spheres
Fuel Sphere Pressing Line
(NUKEM HOBEG, Hanau, Germany)

## Slide 15: 4. HTR Fuel Plant - Uranium Recovery
Precipitation
NH4OH/H2O2
and
Filtration
ADU
UP
Wet UO4 ∙ H2O precipitate
Add H2O2
Dissolution in HNO3
U3O8
UO2(NO3)2 + C
Source: Leiem, wikipedia.org, CC BY-SA 3.0
Clean UO2(NO3)2
Particle Filtering
Dirty U3O8
Source: Chemolunatic, wikipedia.org, CC BY-SA 4.0;
woelen.homescience.net
UO2(NO3)2 (aq.)
Carbon particles
Calcining
NG U3O8
Clean U3O8

## Slide 16: 5. High temperature SMRs
  Nearly all reactor designs (established to Gen IV) can be designed as SMR
  Common HTR concepts:
    High-temperature gas-cooled reactor (HTR), outlet: 750 °C
    Very-High-Temperature Reactor (VHTR), outlet: 1000 °C
  Advantages of high temperatures:
    Replacing fossil fuel generated process heat
    e.g., synchronous electricity and hydrogen production via high-temperature water electrolysis
    High thermal conversion efficiency
Source: Wikipedia, https://en.wikipedia.org/wiki/High-temperature_gas_reactor#/media/File:Very_High_Temperature_Reactor.svg

## Slide 17: 5. High temperature SMRs
  Inherent safety features of the HTR concept:
    Retention of fission products (TRISO fuel)
    Core meltdown impossible: heat can always passively dissipate even without an active helium cooling circuit
    Small core power density (compared to PWR)
    Large heat capacity and temperature stability of graphite-based reactor cores
  Advantages of the SMR concept:
    Less fissile material increases safety
    Standardisation of components
    Design integration to reduce complexity
    Flexible application in industrial cluster areas: less grid restrictions

## Slide 18: Questions?

## Slide 19: Content slide

## Slide 20: Criticality Safety - Practice
Slab Tank
Tube Array Tank
  Safe Mass principle is avoided wherever feasible

## Slide 21: Criticality Safety - Principles
  Safe Mass
  Safe Volume
  Safe Cylinder Diameter
  Safe Slab Thickness
  Assumptions:
    Optimal moderation
    Worst-case reflection

## Slide 22: Area K – Kernel Production
2023-01-18
U3O8
Fresh and Area R
Dissolution in HNO3
and
Pre-neutralisation
ADU ~(NH4)2U2O7
DI Water, NH4OH, HNO3
Utilities
Uranyl Nitrate sol.
Drip Casting
UNOH
Casting Solution
PVA, THFA, Carbon Black, DI Water
Utilities and Area E
NH4OH, NH3
Utilities and Area E
Water, IPA
Utilities and Area E
Used Water, IPA
Area E
Ageing, Washing, Drying
Evaporate NH4OH
Rinse with
H2O
Remove
H2O by IPA
ADU
Calcining
up to 430 °C
Air, Ar, N2
UO3/C
PVA
Oxidation
ADU decomposition
UCO Kernels
Area C
Sieving, Sorting, Sampling and Portioning
Off-Spec UCO Kernels
Area R
Sintering
up to 1890 °C
Ar, H2, CO/Ar
UO2/UC/UC2
UO3 → UO2
Reduction
UO2 + 4C → UC2 + 2CO
Carbotherm. Red.
UO2(NO3)2(aq.)