## Slide 1
Investigation of hydrodynamic and scaling of TRISO coaters for high temperature small modular reactors
Thaar Aljuwaya [1,2], and Muthanna H. Al-Dahhan [1,3,4]
[1] Department of Mining and Nuclear Engineering, Missouri University of Science and Technology, Rolla 65409, MO, United States
[2] Nuclear Technologies Institute, King Abdulaziz City for Science and Technology (KACST),
P.O. Box 6086, Riyadh 11442, Saudi Arabia
[3] Multiphase Flows and Reactors Engineering and Education Laboratory (mFReel), Department of Chemical and Biochemical Engineering, Missouri University of Science and Technology, Rolla 65409, MO, United States
[4] Technology Development Cell (TechCell), Mohamed VI Polytechnic University (UM6P), Ben Guerir 43150, Morocco
20/23/2024

## Slide 2
Introduction
  Generations of Nuclear Reactors, Generation IV Systems: GIF Goals,
  Very High Temperature Reactors (VHTRs),
  TRISO nuclear fuel particles.
  TRISO fuel coating process, Spouted beds.
Motivation & Objectives
Experimental setup and Measurement Techniques
Results and Discussion
Conclusion
Outlines

## Slide 3
Generations of Nuclear Reactors
Notes: Nuclear reactors are characterized by generation and as of today there are four generations (I, II, III, III+, and IV), of nuclear reactors’ designs, only two of them are in actual use in energy production field. The others are still under experimental phase and there are no expectations yet of when these reactors are going to put into service. However, and after the last tsunami accident in Japan in 2011, calls for the deployment of latest developed nuclear reactors were raised from many different disciplines. Reactors counts on enriched uranium fuel rods to generate power through controlled fusion reaction. In new reactors generations these fuel rods turns into particles were the enriched uranium is coated by certain materials that keeps its radio active waste safe and generate more power then in rods operated reactors.
Generation IV International Forum (GIF) is founded on eight technology goals that include to improve nuclear safety, improve proliferation resistance, minimize waste and natural resource utilization, and decrease the cost to build and run such plants
For the purpose of this thesis, it is important to concentrate on the fuel cycle as an important factor among the above-mentioned ones.

## Slide 4
1.Very-High-Temperature Reactor (VHTR):
graphite-moderated
helium-cooled
once-through uranium fuel cycle
2. Supercritical-Water-Cooled Reactor (SCWR):
high-temperature
high-pressure water-cooled
operates above the thermodynamic critical point of water
3. Gas-Cooled Fast Reactor (GFR):
features a fast-neutron-spectrum
helium-cooled
closed fuel cycle
4. Lead-Cooled Fast Reactor (LFR):
features a fast-spectrum lead of lead/bismuth eutectic liquid
metal-cooled
closed fuel cycle for efficient conversion of fertile uranium and management of actinides
5. Sodium-Cooled Fast Reactor (SFR):
features a fast-spectrum
sodium-cooled
closed fuel cycle for efficient management of actinides and conversion of fertile uranium
6. Molten Salt Reactor (MSR):
produces fission power in a circulating molten salt fuel mixture
an epithermal-spectrum reactor
full actinide recycle fuel cycle
Generation IV Candidates Reactors
Notes: For the purpose of this thesis, it is important to concentrate on the fuel cycle as an important factor among the above-mentioned ones. Nuclear reactor’s fuel is used in many different ways and forms, and from that one can identify reactor type. First reactor generations used nuclear fuel in form of rods that slide down the reactor core, which is coated with certain anti radiation materials, and used either light or heavy water as a cooling system for the reaction process and also as a heat transfer channel. Fuel used in IV generation reactors is different form the one used in first and second generation. Fourth generations’ reactors, which are divided into two types, uses nuclear fuel that is commonly known as TRISO Fuel, which takes the form of particles instead of rods. This type of fuel, if used properly, would produce twice the power being produced recently by the first and second generation’s reactors. This type of fuel and reactors using it would be the core objective of my thesis
As for the earlier models, many of it are still functioning and producing in different countries like the European Union, US, Canada, Japan, and China. These reactors are generally functioning well despite some of the accidents (i.e. Ukraine (1987), Japan (2011), US (1987)), however most of it are about time to be replaced or shut down due to building aging or license expiration. As a result, many states now are considering building new reactors with new designs.

## Slide 5
Very High Temperature Reactors (VHTRs)
Prismatic Blocks Reactor
Pebble Bed Reactor
Helium coolant
Coated particle fuel
Reference configurations are the prismatic and the pebble bed
Outlet temperature 750-950°C
Production of electricity and high temperature process heat for industrial applications
Passive safety characteristics
High thermal efficiency
TRISO fuel is at the heart of the operating and safety for the high temperature gas-cooled reactors.
Notes: New reactor designs now days more focused on a concept called passive safety, and security. Passive safety simply means a newly designed feature in newly designed reactors that relay on engineered components of the reactors that would, in the case of any emergency, cool, and eventually shut down the nuclear reaction instead of accelerating it as in the old, yet common reactors designs. Newly designed reactors are simply uses simple physics approaches to build the reactor that allows the core to shut down automatically in case of any emergency without the need to sophisticated engineered safety tools, rotary mechanisms, or human intervention.
The Very-High-Temperature Reactor (VHTR) is
  graphite-moderated (thermal spectrum)
  helium-cooled reactor
  once-through uranium fuel cycle (no reprocessing)
  core outlet temperatures of 1,000 ◦C
High temperature, helium cooled, graphite moderated reactor graphite-moderated
Goal – reach 1000 °C, with near term focus on 700 - 950 °C
Reference configurations are the prismatic and the pebble bed
Many countries remain interested in VHTR, more countries are becoming interested (Safety, high efficiency, process heat application, hydrogen production).

## Slide 6
Chinese HTR-PM demonstration plant is under construction Pebble bed core, 750 °C outlet temperature, steam cycle, 40% efficiency
  Two 250 MWt NSSS modules for 210 MWe electricity
  First Concrete in December 2012
  Plant operation expected around end of 2018
Shidao Bay Nuclear Power Plant
HTR-PM demonstration plant
First pour of concrete
Successful construction and operation of the Chinese HTR-PM plant should significantly help the promotion of VHTR technologies.
HTR-PM Reactor & SG Side by side
Fuel Samples for Irradiation in Patten
The Shidao Bay nuclear power plant is a joint venture by China Huaneng Group, China Nuclear Engineering & Construction Group, and Tsinghua University.

## Slide 7
TRISO nuclear fuel particles
Notes: The TRISO nuclear fuel particles consist of fuel kernel made of UO2 or other fertile materials surrounded by four layers of isotropic materials for protection and containment.
The coated particle fuel has many attractive features, such as the ability to operate at high temperatures, to achieve high burn up, and to survive adverse conditions.
Size from approximately 920 µm to 1000 µm, the particles are durable and impervious to moisture for long periods of times, making them an attractive alternative to current metallic fuel containers.
Layers are designed to keep the fuel and the fission products contained.
Failure of the layers can result in fuel failure and radioactive contamination in the primary system.

## Slide 8
TRISO fuel coating process
Schematic Diagram of a Spouted Bed
Spouted beds : Gas-solid contactors that can handle heavy coarse particles where the circulation of solids is important and is dictated by the gas dynamics.
Spouted beds has many attractive features including
1- good particle circulation.
2- effective fluid-particle contact
3- high rate of heat and mass transfer
2-inch diameter Spouted beds used for coating TRISO fuel at ORNL.
The issue becomes more complex when we know that probability of successfully coating a layer depends on the success of the preceding coating
The quality of the TRISO fuel, i.e. whether particles produced are uniformly or non-uniformly coated, is strongly impacted by the hydrodynamics of the gas-solid spouted bed, the solids flow field, and the flow regime characteristics.
Notes: They are Gas-solid contactors that can handle heavy coarse particles where the circulation of solids is important and is dictated by the gas dynamics. As you see, bottom of the spouted bed is conical and the rest of the bed is cylindrical. The spouted bed can be all conical. The chemical vapor (gas) is fed from the bottom as a jet where it creates three distinct regions:
  Spout in the center of the bed
  Fountain above the spout
  Annulus where the particles move as packed bed
Spouted beds has many attractive features including
1- good particle circulation.
2- effective fluid-particle contact
3- high rate of heat and mass transfer
Their Applications include:
Coating (e.g., TRISO process), drying, gasification, chemical vapor deposition, etc.

## Slide 9
Spouted beds Nuclear reactor (conceptual)
TRISO

## Slide 10
Motivation
&
Objectives

## Slide 11
TRISO fuel coating process (cont.)

## Slide 12
Experimental Setup
&
Measurement Techniques

## Slide 13
Experimental Setup
Two spouted beds have been used; one is 6-inch and the second one is 3-inch. Both spouted bed columns are constructed from Plexiglas and consist of one-piece column attached to a conical base.
For both columns, the cone is angled at 60 degrees and the diameter of the gas inlet orifice for the gas jet are 19.05 mm and 9.5 mm for 6-inch and 3-inch spouted beds respectively.
Both columns are 1.14 m tall.
The fluidization gas is Dry-air .
Gas Distributor (stainless steel)
Notes: This slid shows the experimental setup_ …….The experimental works were carried out in two Plexiglas conical base spouted bed columns with inner diameter of a 0.152 m (6 inch) and 0.076 m (3 inch). The schematic of spouted bed with detailed dimensions of 6-inch and 3-inch spouted bed is shown here.
Both columns were designed to be geometrically similar with 1.14m tall and conical base of 60-degree angle.
The spouted bed columns are constructed from plexiglass and consist of one-piece column attached to a conical base. Having a one piece column will improve the symmetry of the column and help stabilize the fountain.
At the bottom of the conical base the gas distributor is placed to pass through the gas flow inside the column. The diameter of the inlet orifice is 19.1 mm and 9.5 mm for 6-inch and 3-inch spouted beds respectively.
The gas used was dry compressed air supplied from an industrial compressor with capacity up to 735 CFM and 200 Psig.
The two columns were designed without any ports or connections on the wall because these create non-symmetry, which complicates the CT and RPT data reconstructions.

## Slide 14
Dual Sources Gamma Ray Computed Tomography (DSCT) Technique
Video comes here

## Slide 15: Radioactive Particle Tracking (RPT)
Radioactive Particle Tracking (RPT) is a technique for tracking of a single radioactive tracer particle by detecting the intensity distribution of emitted γ -rays. The γ -ray intensity distribution is detected using an array of NaI scintillating detectors strategically placed around the system being investigated.
Collected radiation intensity data is used to reconstruct the tracer particle trajectory (tracer particle location in time), which is used to obtain the tracer particle:
Calibration points along the 6-inch spouted beds column
Velocity Field Profiles
Turbulent Parameters (Reynolds’ stresses and TKE)
Eddy diffusivities profiles.
RPT experiment comprises two steps:
RPT calibration ( a ‘static’ experiment or in-situ)
RPT experiment (a ‘dynamic’ experiment).
A fully automatic calibration device
Schematic diagram showing the positions of 14-detecors arranged around the 0.152 m spouted bed.

## Slide 16
The lead pig containing the radioactive particles when it arrived
Vial containing tracer particle for 6-inch SPB exps.
￼
The radioactive tracer particles were mad as closely as closely as possible to resample the tagged solid phase particles in:
  Size
  Density
  Shape
Preparation of Tracer particles
Microscopic picture of the Cobalt particle (D = 600µm)
Two tracer particles were manufactured in our lab to track tow solid phases:
  Glass (ρ ~ 2.4 g/cm^3)
  Steel (ρ ~ 7.4 g/cm^3).
The lead pig containing the radioactive particles when it arrived
Each Tracer particle is embedded with Co-60
(D = 600µm) and initial activity of ~ 500 µci.

## Slide 17
Data treatment
The following key parameters of solids flow in the spouted beds were calculated:
Cumulative probability distribution of the solids particles penetration into the spout ().
Cumulative probability of the landing position of the solid particles at the annulus surface.
Cumulative probability of the penetration of the solid particles into the base of the fountain region.
Mean value of the spout radius ();
Mean residence time of solids in the spout (), in the annulus (), in fountain ();
Mean cycle time of solids in the spouted beds ();
Times of transitions between the adjacent regions of the bed:
() () ()
Notes: TRPT experiments were performed for different composition of binary mixture at different gas inlet velocity to quantify the effect of composition of binary mixture on flow behavior of binary mixture spouted bed
Since the flow behavior of the gas-solid spouted beds is chaotic, the RPT experiments were carried out for each one of the solids phases on an individual basis, and then the statistical averages of each flow fields are combined together to formulate the entire picture of the binary mixture flow field
he existing designs fail to capture the impact of particle property and size variation
Few studies have also been reported on the mixing action of binary mixture fluidized bed

## Slide 18
Focus Subjects
Scale-up of gas-solids spouted beds

## Slide 19
Comparison of local detailed solids distribution between 6-inch and 3-inch at similar gas holdup profile condition
Notes: This slide demonstrate the detail local cross sectional distribution of solids holdup between 6 inch and 3 inch and you could see here the mean and variance of the histogram are close. The colors varies due to the variation in the scale of the color verses solids holdup.
The detailed comparison of the cross sectional distribution of local solids holdup confirm the validation of the newly developed mechanistic scale up methodology

## Slide 20
Comparison of local detailed solids distribution between 6-inch and 3-inch at similar gas holdup profile conditions
…
Chart: Level z/D=0.8
| 1.2500000000000001E-2 | 3.7499999999999999E-2 | 6.25E-2 | 8.7499999999999994E-2 | 0.1125 | 0.13750000000000001 | 0.16250000000000001 | 0.1875 | 0.21249999999999999 | 0.23749999999999999 | 0.26250000000000001 | 0.28749999999999998 | 0.3125 | 0.33750000000000002 | 0.36249999999999999 | 0.38750000000000001 | 0.41249999999999998 | 0.4375 | 0.46250000000000002 | 0.48749999999999999 | 0.51249999999999996 | 0.53749999999999998 | 0.5625 | 0.58750000000000002 | 0.61250000000000004 | 0.63749999999999996 | 0.66249999999999998 | 0.6875 | 0.71250000000000002 | 0.73750000000000004 | 0.76249999999999996 | 0.78749999999999998 | 0.8125 | 0.83750000000000002 | 0.86250000000000004 | 0.88749999999999996 | 0.91249999999999998 | 0.9375 | 0.96250000000000002 | 0.98750000000000004
Case A | 0.9162 | 0.92861 | 0.91814 | 0.9119 | 0.906 | 0.88745 | 0.86567 | 0.83546 | 0.8025 | 0.7641 | 0.71473 | 0.6558 | 0.6061 | 0.54688 | 0.4933 | 0.46029 | 0.43572 | 0.419 | 0.4071 | 0.39807 | 0.39649 | 0.3952 | 0.39606 | 0.3985 | 0.39792 | 0.39539 | 0.3965 | 0.3952 | 0.39662 | 0.39609 | 0.3974 | 0.39508 | 0.39743 | 0.39613 | 0.3974 | 0.39325 | 0.3939 | 0.39319 | 0.3946 | 0.39781
Similar Ɛg | 0.91715 | 0.9253 | 0.9072 | 0.8529 | 0.76988 | 0.67828 | 0.56336 | 0.47655 | 0.426 | 0.408 | 0.396 | 0.39829 | 0.39631 | 0.39438 | 0.3954 | 0.3942 | 0.3982 | 0.39485 | 0.39334 | 0.3946
Chart: Level z/D=1.1
| 1.2500000000000001E-2 | 3.7499999999999999E-2 | 6.25E-2 | 8.7499999999999994E-2 | 0.1125 | 0.13750000000000001 | 0.16250000000000001 | 0.1875 | 0.21249999999999999 | 0.23749999999999999 | 0.26250000000000001 | 0.28749999999999998 | 0.3125 | 0.33750000000000002 | 0.36249999999999999 | 0.38750000000000001 | 0.41249999999999998 | 0.4375 | 0.46250000000000002 | 0.48749999999999999 | 0.51249999999999996 | 0.53749999999999998 | 0.5625 | 0.58750000000000002 | 0.61250000000000004 | 0.63749999999999996 | 0.66249999999999998 | 0.6875 | 0.71250000000000002 | 0.73750000000000004 | 0.76249999999999996 | 0.78749999999999998 | 0.8125 | 0.83750000000000002 | 0.86250000000000004 | 0.88749999999999996 | 0.91249999999999998 | 0.9375 | 0.96250000000000002 | 0.98750000000000004
Case A | 0.8462 | 0.85861 | 0.84814 | 0.8419 | 0.82906 | 0.80745 | 0.78567 | 0.75546 | 0.71425 | 0.64541 | 0.57473 | 0.52858 | 0.4861 | 0.45688 | 0.43483 | 0.41479 | 0.41022 | 0.40369 | 0.40021 | 0.39857 | 0.3999 | 0.39502 | 0.39656 | 0.39635 | 0.39642 | 0.39889 | 0.399 | 0.39702 | 0.39912 | 0.39759 | 0.39844 | 0.39958 | 0.39693 | 0.39563 | 0.39724 | 0.39875 | 0.39789 | 0.39869 | 0.3981 | 0.39831
Similar Ɛg | 0.8496 | 0.84611 | 0.8124 | 0.77047 | 0.66944 | 0.57244 | 0.47765 | 0.42965 | 0.4067 | 0.403 | 0.39861 | 0.39596 | 0.40072 | 0.39406 | 0.39863 | 0.39533 | 0.39412 | 0.39515 | 0.39526 | 0.396
Chart: Level z/D=1.8
| 1.2500000000000001E-2 | 3.7499999999999999E-2 | 6.25E-2 | 8.7499999999999994E-2 | 0.1125 | 0.13750000000000001 | 0.16250000000000001 | 0.1875 | 0.21249999999999999 | 0.23749999999999999 | 0.26250000000000001 | 0.28749999999999998 | 0.3125 | 0.33750000000000002 | 0.36249999999999999 | 0.38750000000000001 | 0.41249999999999998 | 0.4375 | 0.46250000000000002 | 0.48749999999999999 | 0.51249999999999996 | 0.53749999999999998 | 0.5625 | 0.58750000000000002 | 0.61250000000000004 | 0.63749999999999996 | 0.66249999999999998 | 0.6875 | 0.71250000000000002 | 0.73750000000000004 | 0.76249999999999996 | 0.78749999999999998 | 0.8125 | 0.83750000000000002 | 0.86250000000000004 | 0.88749999999999996 | 0.91249999999999998 | 0.9375 | 0.96250000000000002 | 0.98750000000000004
Case A | 0.7537 | 0.77102 | 0.76636 | 0.76426 | 0.74549 | 0.72103 | 0.69274 | 0.67064 | 0.62854 | 0.5674 | 0.52811 | 0.48348 | 0.45733 | 0.43422 | 0.42248 | 0.40771 | 0.3981 | 0.39578 | 0.398 | 0.39793 | 0.39604 | 0.3954 | 0.39591 | 0.39584 | 0.3976 | 0.3969 | 0.39516 | 0.3995 | 0.39813 | 0.39722 | 0.39508 | 0.39645 | 0.3978 | 0.3975 | 0.3964 | 0.39875 | 0.3989 | 0.3969 | 0.3981 | 0.3968
Similar Ɛg | 0.7587 | 0.76735 | 0.74164 | 0.68717 | 0.60557 | 0.5049 | 0.449 | 0.4102 | 0.39822 | 0.397 | 0.397 | 0.398 | 0.3996 | 0.39344 | 0.39538 | 0.39582 | 0.39727 | 0.3975 | 0.39805 | 0.39673
Chart: Level z/D=2.4
| 1.2500000000000001E-2 | 3.7499999999999999E-2 | 6.25E-2 | 8.7499999999999994E-2 | 0.1125 | 0.13750000000000001 | 0.16250000000000001 | 0.1875 | 0.21249999999999999 | 0.23749999999999999 | 0.26250000000000001 | 0.28749999999999998 | 0.3125 | 0.33750000000000002 | 0.36249999999999999 | 0.38750000000000001 | 0.41249999999999998 | 0.4375 | 0.46250000000000002 | 0.48749999999999999 | 0.51249999999999996 | 0.53749999999999998 | 0.5625 | 0.58750000000000002 | 0.61250000000000004 | 0.63749999999999996 | 0.66249999999999998 | 0.6875 | 0.71250000000000002 | 0.73750000000000004 | 0.76249999999999996 | 0.78749999999999998 | 0.8125 | 0.83750000000000002 | 0.86250000000000004 | 0.88749999999999996 | 0.91249999999999998 | 0.9375 | 0.96250000000000002 | 0.98750000000000004
Case A | 0.75669 | 0.76662 | 0.77396 | 0.78059 | 0.79479 | 0.80615 | 0.82899 | 0.83784 | 0.85258 | 0.86755 | 0.87591 | 0.88905 | 0.89894 | 0.90435 | 0.91197 | 0.91816 | 0.9202 | 0.92558 | 0.928 | 0.93005 | 0.93244 | 0.93428 | 0.93642 | 0.93501 | 0.93484 | 0.93464 | 0.93895 | 0.94001 | 0.94044 | 0.9414 | 0.93939 | 0.93862 | 0.93848 | 0.9384 | 0.93952 | 0.94015 | 0.9397 | 0.93869 | 0.93668 | 0.93726
Similar Ɛg | 0.75038 | 0.77095 | 0.79167 | 0.82083 | 0.85826 | 0.87881 | 0.90016 | 0.91613 | 0.92176 | 0.92913 | 0.9342 | 0.93992 | 0.93969 | 0.93996 | 0.93988 | 0.93978 | 0.93927 | 0.93977 | 0.93959 | 0.93958

## Slide 21
Dimensionless residence time distribution
The absolute relative deviation in the spout:
1.9% for Similar gas holdup conditions 57.67% for Dissimilar conditions
in the fountain:
3.8% for Similar gas holdup conditions 54.65% for Dissimilar conditions
in the annulus:
9.14% for Similar gas holdup conditions 27.24% for Dissimilar conditions

## Slide 22
Fraction of particle cycle time spent each region of the bed
The absolute relative deviation in the spout:
5.36% for Similar gas holdup conditions 18.26% for Dissimilar conditions
The absolute relative deviation in the fountain:
3.38% for Similar gas holdup conditions 24.83% for Dissimilar conditions
The absolute relative deviation in the annulus:
0.79% for Similar gas holdup conditions 4.29% for Dissimilar conditions

## Slide 23
Spout diameter
The average deviation for the profile of the similar gas holdup case from that of the reference case as found to be 4.32% and for the similar gas holdup case were 19.64%
Considering the fact that the profiles were derived from two independent
experimental techniques, this comparison serves as a validation of results for both the techniques.
Notes: Comparison of the dimensionless spout diameter profiles derived from CT and RPT for the pilot plant-scale spouted beds at the condition of the reference case
Dimensionless spout diameters (or penetration of the solids in the spout) as a function of dimensionless height for the conditions of the reference case, similar gas holdup profiles and dissimilar gas holdup profile.
Cumulative distribution of particles crossing boundaries between regions for binary spouted bed at U/Ums =1.1. (a) Landing on annulus surface; (b) Being entrained into spout from the annulus; (c) Entering fountain at z = H.

## Slide 24
Our New scale-up methodology implementation
Performing measurements of the gas holdup radial profile at selected heights in the lab or pilot plant spouted beds that is needed to be scaled up or down.
Applying validated computational fluid dynamics (CFD) simulation to seek out the similar or closer gas holdup radial profile in larger or smaller sizes spouted beds and/or different operating conditions.
Designing, constructing and operating the newly identified size and conditions of the gas-solid spouted bed.
Evaluating the radial profile of the gas holdup of the constructed and operated spouted bed of step 3.
If needed, refining and tuning the operating conditions that are possible to adjust during the operation of the constructed and operated spouted bed in step 3 to ensure as close as possible to the radial profile of gas holdup to that of the bed under investigation of step 1
Notes: Performing measurements of the gas holdup radial profile at selected heights in the lab or pilot plant spouted beds that is needed to be scaled up or down. The measurements step can be performed without disturbing the flow using our method of non-invasive measurement techniques such as the gamma-ray densitometry (GRD), and gamma-ray computed tomography (CT). The selected heights in the spouted bed have to include the spout-annulus regions in the cylindrical part of the bed.
Applying validated computational fluid dynamics (CFD) simulation to seek out the similar or closer gas holdup radial profile in larger or smaller sizes spouted beds and/or different operating conditions. The implementation of CFD will allow defining the scale-up or scale-down sizes and the conditions that will provide similar or closer gas-holdup radial profile of that of the bed under investigation measured in step 1. Note that the first condition in the scale-up approach “when spouted beds with different sizes and/or conditions are geometrically similar” has to be met in the larger or smaller sizes of spouted beds when performing the CFD.
Designing, constructing and operating the newly identified size and conditions of the gas-solid spouted bed.
Evaluating the radial profile of the gas holdup of the constructed and operated spouted bed of step 3 using our method of gamma-ray densitometry technique which is an on-line monitoring technique that has been developed in our laboratory (cite kanta paper of GRD ) to measure radial/diameters profiles of gas and solids holdups and flow regimes in a non-invasive manner and at both laboratory and pilot plant conditions. Also, the optical fiber probe technique that has been implemented in our laboratory can be applied to large-scale and pilot plant condition to measure radial profiles of gas and solids holdup and solids velocity. The measurements can be utilized to provide benchmarking data to refine the validation of the validated CFD used in step 2.
If needed, refining and tuning the operating conditions that are possible to adjust during the operation of the constructed and operated spouted bed in step 3 to ensure as close as possible to the radial profile of gas holdup to that of the bed under investigation of step 1.
The above steps can be implemented on larger spouted bed of those studied in this work and at pilot plant conditions as well. Furthermore, for liquid-solid spouted beds where the hydrodynamics, in this case, are dictated by the dynamics of the liquid, same steps and methodology can be applied.
%%%
Cite his paper

## Slide 25: Conclusions & Recommendations

## Slide 26
The hydrodynamics of gas-solid spouted beds largely depend on the particle properties. Also, the results have shown that the assumption that stable spouting mode would result in uniform coating layers for the particles in the TRISO fuel coating process is not adequate.
Also, the results showed that even though the particles were operated at the stable spouting state and same U/Ums and Ho, differences were obtained in the solids holdup distributions in the spout and the fountain regions.
The common assumption that the gas holdup in the annulus is equal to the loos-packed bed value, particularly with increasing the applied gas flow rate.
The principle conclusion is that that segregation always takes place in the spout due to the unlike behavior between the different solids phases in terms of mean solids velocities, fluctuating velocities, turbulent stresses and kinetic energy which are determined by particle-particle interaction and other forces exerted on the different solids phases.
Conclusion remarks

## Slide 27
Thank you