## Slide 1
Sebastijan Brezinsek and JET contributors / TSVV-7 team
Institute of Fusion Energy and Nuclear Waste Management - Plasma Physics
Forschungszentrum Jülich
Faculty of Mathematics and Natural Sciences
Heinrich Heine University Düsseldorf
Plasma-Wall Interactions
in all-Metall Fusion Devices
- the W erosion quest
JET

## Slide 2
25 years of PWI fusion research in a nutshell (my view)
The dream is to get plasma-facing components based on an element „TOKAMAKIUM“:
no sputtering, no fuel retention, neutron resistant, good thermomechanical properties, …
The dream is a plasma „T-MODE“ with perfect confinement:
no plasma-wall interaction, no CX-wall interaction, highly radiative in the divertor, …
=> Both doesn‘t exist as such and we need to find a compromise (now)
Novel components on basis of W under qualification and close to the material needs.
Plasma solutions on basis of radiative x-point or mantle are close to the plasma needs.
Boronisation used as „fix“ to overcome issues with W if O present
Note, some plasma properties are masked by the low-Z impurities

## Slide 3
Plasma-Surface Interaction Processes
Divertor und SOL plasma conditions:
Te=1-100 eV
ne=5x1017-1x1021m-3

## Slide 4
ITER PFC selection history and Tungsten PFCs
Fuel retention predictions for ITER
by the EU Task Force PWI in 2009
~1 year full DT
operation
J. Roth et al.
J. Nucl. Mat. 2009
Demonstration in JET: from
C to Be+W retention drops
and predictions for ITER OK
K. Schmid et al.
J. Nucl. Mater. 2015
S. Brezinsek
Nucl. Fus. 2013
Be damage due to disruptions in JET,
ITER construction delays and new
W results from ASDEX Upgrade, etc.:
=> full-W ITER PFCs from day 1
better reactor proxy
recover part of delay
early physics exploitation
use of B as O getter
New issue to be addressed:
Can Q=10 be achieved with W?
What is the tolerable W wall source?
How to deal with the B as “fix”?
R.A Pitts PSI 2024

## Slide 5
Physical Sputtering of W
Binary-collision approximation with perpendicular impact of mono-energetic projectiles (SD-TRIM)
Be sources and
migration in JET
W sputtering by intrinsic (Be, C) or seeding impurities (Ne, Ar, N) above threshold energy Eth
Noticeable sputtering by D+ above Ein~250eV
Dominant in JET-ILW: Be ions ~ 0.5-1.5%
S. Brezinsek et al.
NF 2015
JET

## Slide 6
Source: gross and net erosion of tungsten
Larmor radius: rL = M·v/q·B
Ionisation length: lion = v/<sv>ion·ne
rprompt = lion/rL
 B
lion
rL
Be+
W+
rL
lion
Be0
W0
wall element
Prompt re-deposition of W if rprompt < 1
Results in LOW net erosion for W if rprompt < 1
S. Brezinsek et al.,
Nucl. Fus. 2019
A. Kirschner et al.
Spectroscopy measures gross W erosion via WI emission
WI to WII spectroscopy can provide the redeposition factor
Post-mortem analysis measures integrated net W erosion
ERO-Modelling can disentangle gross and net erosion
Notes: Tierry

## Slide 7
Gross and Net Erosion of W
Optical Emission Spectroscopy (WI):
gross erosion of W [in situ]
Difference provides local W balance: eroded, re-deposited, and transported away
Erosion of W is in general low => enough fluence to compare both methods required
W bulk
Mo
W
RBS
M. Mayer et al.
NME 2017
Marker Coating Technique
used for dedicated PFCs
W I
edge plasma
W PFC
+
*
S
'
W II
X'
B '
W+
h
n
W+
W
S
Bt
Z
Imp
Y
H,D,T
re-deposition
IoniSation
Branching Ratio
EXcitation
Erosion Yield
W
*
X
B
h
n
W I
Post-Mortem Analysis Techniques:
net erosion of W [ex situ]

## Slide 8
Gross and Net Erosion of Tungsten in JET
Net W erosion at OSP measured [M. Mayer JNM 2017]
~1.5µm at OSP in 900s H-mode phase (C30C)
Net W erosion: 2.4-4.8 g (RBS and marker tiles)
Gross W erosion: 40-60 g (WI spectroscopy)
W prompt re-deposition fraction: >95%
ERO confirms very high W re-deposition: > 98%
Very effective “screening” of gross eroded W
S. Brezinsek et al.
Nucl. Fus. 2019
M. Mayer et al.

## Slide 9
ELM-induced W Sputtering in Detached Conditions
Inter-ELM W source can be eliminated
when divertor is semi-detached and impact
energies below the threshold for impurities
Intra-ELM W source can burn through the
cushion of hydrogen and seeding neutrals
Partial detachment required
ELM suppression required
Spectroscopy often used
for W and “power”
control => Te sensitivity
ELM

## Slide 10
Photon Effciencies: Experiment and ADAS
Experimental data is “effective” assuming WF6 dissociation is complete
Experimental data in general in good agreement with ADAS (lower)
Largest deviation for the “lowest” ground state transition (l=498.3nm)
SOL
TEXTOR W calibration
S. Brezinsek et al.
Phys. Scripta 2017

## Slide 11
Injected W and Sputtered W: WI emission
  Calibration of W lines with WF6 injection (dissociation at about Te~0.1eV)
W from WF6 dissociation representative for W from sputtering?
  No difference in line shape of different WI and WII lines
  Lines and ratios of WI lines comparable in sputtered and injected W
  WII lines measured and quantified in WF6 injections

## Slide 12
Tungsten Migration: Erosion, Transport, and Deposition
W migration
W transport
W depostion
short range
long range
W erosion
e.g. within
divertor leg
e.g. divertor
to main chamber
W „graveyard“
erosion
transport
deposition
Local balance equation => net erosion = gross erosion – deposition
Large Larmor radius for W+ => competes with ionisation length => prompt re-deposition
Surface roughness increases the re-deposition probability => reduces net erosion
very short range
e.g. within
one gyration

## Slide 13
What would be different in a full-W ITER?
Exchange Be by W in ERO2.0 and keep the semi-detached Q=10 scenario*
A. Eksaeva et al.
NME 2022
Net erosion of the first wall is drastically reduced by about 4 orders of magnitude for the peak erosion
Residual sputtering caused mainly by impurity ions, 0.5% Ne ions (used to seed), and energetic CX HI
x1021
x1017
A “full-W ITER” would provide:
Low first wall W erosion
Low T co-deposition with W
Residual T retention by implantation in the wall
Increase of T retention with neutron damage in FPO-2
Require boronisation in case
of high O content (e.g. start-up)
What is the tolerable W wall source and W influx to the plasma?

## Slide 14
DEMO: Plasma Extrapolations up to the first wall
electon density [m-3]
1018
1010
SOLPS-ITER plasma solution for H-mode with Ar seeding and detached divertor => F. Subba NF et al.
Extrapolation of the plasma up to the first wall and 3D contour
Exponential decay
Scan in temperature to the wall to investigate threshold effects
2eV beyond Ar ion threshold
5eV at Ar ion threshold
10eV ITER assumption
plasma
w
a
l
l

## Slide 15
DEMO: Fluxes to the W wall
All ionisation stages of Ar ions spatially resolved included
C. Baumann et al.

## Slide 16
W sputtering sources by impinging ions and CX atoms
No W sputtering by residual D ions
as below W sputtering threshold and low residual flux
Here: strong CX induced W sputtering
=> CXN from EIRENE post-processing
C. Baumann et al.
ERO2.0

## Slide 17
Net W sputtering pattern for a DEMO run with ERO2.0
C. Baumann et al.
c.baumann@fz-juelich.de
2 eV
5 eV
10 eV
Very sensitive on input plasma parameters at recessed areas!
Waiting for SOLPS-ITER wide-grid plasmas with full-W and Ne seeding for ITER
Provide W influx to ITER from the first wall is next!

## Slide 18
The Challenge with W Transport and Spectroscopy
Fractional abundance as function of Te or R => not fully ionized in core
Structure complex => multiple approaches to simulate and model W
AUG and JET used as test bed / provision of atomic data for W / EBIT
Extrapolation to ITER conditions challenging (Te range)
fractional abundance
edge
core
divertor
T. Pütterich PPCF 2008
Benchmark of workflow in full-W ASDEX
Upgrade with improved diagnostic set in W without BORONISATION would be useful to validate ERO2.0
simulations for ITER!
This includes also spectroscopy of higher
W ionisation stages
(WII..W IX)
to be simulated in ERO2.0.

## Slide 20: Gross erosion rate …
rate is the same for all cases
peak flux at OMP is 5.41x1016 m-2s-1
calculated using 12 spectra provided by Sven (green locations)  each spectra gives us an effective yield at this location
for surface cell not directly connected to a spectrum, interpolation with the two closest effective yields will be done based on distance to these locations
D0  W
gross erosion flux [m-2s-1]
5x1016
0

## Slide 21
Selection of Plasma-Facing Materials: Low or High-Z?
Lifetime and safety
Core plasma compatibility
Tritium cycle and safety
Low-Z: strong wall erosion;
for C due to chemical erosion
High-Z: low erosion;
for W mainly induced by impurities
Low-Z: limited by dilution
High-Z: limited by radiation
Main fuel retention process
for C and Be: co-deposition
W: implantation only
Steady-state plasmas operation for a DT plasmas in a reactor class device

## Slide 22
Challenges in the use of Tungsten Walls
Need to adapt scenario and ensure impurity control / wall conditions
Melting of high-Z metals
can occur and cause
stop of plasma operation!
J. W. Coenen et al., J. Nucl. Mater. 2013
Cooling of plasma
core can occur and “switch off” the hot plasma!
V. Arunasalam et al., EPS 1978
Experience to operate successful with W gained in ASDEX Upgrade, JET, WEST: review JET+AUG: R. Neu et al. IEEE Trans Plasmas 2013
ASDEX Upgrade

## Slide 23
Large challenge: ground state population of W
Thesis Curtis 2020
Auburn CRM
Role of metastables in the population of most prominent lines
relevant (see also A. Eksaeva 2017)
Different experiments under evaluation and cross-CRM
benchmark ongoing and revisited
New experiments in PSI-2 with LIF to measure
direct the W ground state in preparatio

## Slide 24
What can get wrong? Microscopic W particle influx
81578
PNBI
PICRH
Prad
n_elinecentre
n_elineedge
Tmax
Be II in. divertorI
Be II out. div.
H98y
FGDL
W accumulation occurs when ELM frequency / gas is too low
81765
Single W particles are also a problem
hollow Te profile
ELM frequence too low
W peaking
Sawteeth die out
W accumulation
Temperature collapse
G. F. Matthews et al.
hollow Te profile
B. Sieglin et al., FED 2020 / L. Baylor et al., Nucl. Fus. 2019
Plasma performance lost, but discharge survives often (L-mode transport)
If W event too large => disruption => disruption avoidance or mitigation system mandatory

## Slide 25
From JET to ITER with the ERO2.0 code
JET
4 m
8 m
Be deposition on inner divertor apron
Be deposition: main
chamber: 18%
divertor: 58%
“gaps”: 24%
Be deposition: main
chamber: 90%
divertor: 10%
“gaps”: <1%
case with zero SOL flow
ITER
J. Romazanov PSI2020

## Slide 26
W source: physical sputtering of W in JET with ILW
Gross sputtering yield of W from spectroscopy
W sputtering by intrinsic (Be) or seeding impurities (Ne, Ar, N) when above threshold energy Eth
Operation in detached divertor inhibits W sputtering
(cold divertor plasmas with Te<8 eV)
S. Brezinsek et al.,
Nucl. Fus. 2019
G. van Rooij et al.,
J. Nucl. Mater. 2013
Increasing seeding by N
L. Aho-Mantilla et al.
J. Nucl. Mater. 2013
detached
detached
All measured on bulk W tiles with low surface roughness!

## Slide 27
ne
JET: Intra-ELM W sputtering
Critical measure: pedestal
temperature before/after collapse
Fuel ions and impurity ions “ballistic” when hitting
the target plate (<0.5ms) – no time to fully
thermalize => very high impact energy (keV)
(free streaming model: C. Guillemaut et al.)
W sputtering determined by impact of ionic species: fuel ions dominates at <1% Be incident flux
If seeding species present in pedestal, they can dominate…
S. Brezinsek
NF2019

## Slide 28
ELM flushing operation window in H-mode plasmas
N. den Harder et al.
Nucl. Fus. 2016
S. Brezinsek et al.
Nucl. Fus. 2019
Increase of W source in ELMy H-mode up to max frequency of ~60Hz in JET
Reduction of W source at higher frequencies / type III ELMs?
Indication of W-flushing or increased transport at ELM frequencies above 40Hz
Gas injection is changing ELM frequency and W inter- and intra-ELM source

## Slide 29
Comparing JET-ILW and ITER Conditions
JET-ILW – a test bed for ITER and its operational phases
 | JET-ILW (D/C30C) | ITER (DT baseline) | ITER (H PFPO-1)
Plasma time (H-mode) | 900 s | 400 s | 200 s
Number of pulses | 151 | 1 | 1
Input power | 12 MW | 150 MW | 20 MW
Energy input | 7.2 GJ | 60 GJ | 4 GJ
Divertor ion fluence | ~2.0x1026 D/m2 | ~2.5x1027 D/m2 | ~2x1026 D/m2
Divertor ion flux | ~2.2x1023 D/sm2 | ~6.3x1023 D/sm2 | ~1x1023 D/sm2
Wetted area | ~1 m2 | ~2.5 m2 | ~2.5 m2
ELM frequency | 30 Hz | ~30 Hz (pacing) | -/tbe
Number of ELMs | 30 000 | 12 000 | -/tbe
Deduced from SOLPS calculations
S. Wiesen et al. J. Nucl. Mat. 2015
A. Kukushkin et al. Fusion Eng. Des 2011
comparable in plasma-wall interactions physics
comparable in scrape-off layer and exhaust plasma physics

## Slide 30
Quasi-steady-state Conditions in JET-ILW
For comparison - first year operation:
105 000 ELMs during H-mode
12 h in divertor configuration
“footprint” of JET-ILW in H-mode plasmas
Global material erosion/deposition pattern
Global fuel retention studies
Comparison in-situ and ex-situ analysis
Campaign 30C – quasi-steady-state conditions:
High reproducibility of discharges (#151)
H-mode plasmas with static divertor strike-line
  attached outer divertor (Te~35eV)
  semi-detached inner divertor (Te~7eV)
fELM=30Hz, DWELM=160KJ, 30 000 ELMs
Low disruption rate (<3%)
16.07.2024
IR
top
view
toroidal direction
Tsurface [°C]
plasma duration
target coordinate [mm]
S. Brezinsek NF2013, K. Schmid NF2014, S. Wiesen NME2017
J. Romazanov NME 2019, J. Denis NME 2019

## Slide 31
Intra- and Inter-ELM Sputtering of W: semi-detached leg
ERO-modelling (MC+impurity transport) coupled with PIC simulation of ELM events (1keV, 500ms) reproduces the W sputtering by burn-through in otherwise detached conditions (A. Kirschner et al.)
95%-98% of W is locally re-deposited in the model => agrees well with experiment
Left: ELM-induced W sputtering

## Slide 32
Rough vs. Smooth W Surface: AUG Experiment
A. Lahtinen EPS 2017
ASDEX Upgrade Standard L-mode plasma
Net erosion at OSP by impurity ions (C, N, O)
Net deposition in SOL close to OSP in case of nominal/rough surface
No deposition in SOL in case of smooth surface
smooth: Ra~0.3 μm
nominal: Ra~1.0µm
rough: Ra~4.0µm
20-30 nm W layer
on graphite with
different roughness:
Same plasma: W surface can vary between NET erosion and NET deposition due to surface roughness
Mixture of local re-deposition of eroded W and
W flux from main chamber responsible

## Slide 33
Tungsten Hydride: : 6P-6S+ Transition
33
Observation of WD molecule at very high D+ fluxes (1023ions s-1m-2) on cold W surfaces (<600K)
Chemically Assisted Physical Sputtering by C ions
with sufficient high impact energy (~100eV)
S. Brezinsek NME 2019

## Slide 34
Tungsten Hydride: : 6P-6S+ Transition
AUG
l [nm]
Intensity [arb. units]
Intensity [arb. units]
S. Brezinsek PSI 2018
34
Not produced in plasma
as WF6 injection in D plasma
Observed in ASDEX Upgrade
and produced during ELMs
too (D+ ions at high energy)
Looking forward to see a
molecular modelling….

## Slide 35
Tungsten hydride (isotopologues)
S. Brezinsek et al.,
NME 2019
E. Pawelec et al.
KT3C WT at R~2.7m
#100109
KT3C WH at R~2.7m
#98386
time [s]
Intensity [arb. units]
SOL
PFR
KT3C
WT Q
Radius [tracks]
time [s]
Intensity [arb. units]
SOL
PFR
KT3A
WI 400.9nm
Radius [tracks]
Te at OSP
Eth
Eth
continuum
continuum
Molecular release via WX with X=H,D,T
WD
Additional channel for W erosion
Vanishes at low Te => Eth identified
Quantification ongoing, but “very low” in comparison to PS
WI and WX spatially shifted