## Slide 1: Bulk, surfaces, and grain boundaries
Byeongchan Lee Kyung Hee University, Korea, July 18, 2024
in the lifetime of cascades in W
@ Metsätalo, University of Helsinki, Finland
AMPMI 2024

## Slide 2: Acknowledgments
PhD students: Younggak Shin, Vichhika Moul (Kyung Hee University)
Collaborator: Keonwook Kang (Yonsei University)
Funding
National Research Foundation of Korea (NRF) grant funded by the Korea government (MSIT) (No. 2020R1A2C201510913)
Korea Hydro & Nuclear Power Co., LTD (No. 2022-Tech-11).

## Slide 3: Mechanical properties
depend on grain uniformity (let alone H-P)
Y. J. Lee et al. | Int. J of Refractory Metals and Hard Materials 60, 99 (2016)
Sprayed W

## Slide 4: Mechanical properties
of n-irradiated materials
X. Hu et al. | JNM 480 235 (2016)
J. Marian et al. | Nucl. Fusion 57, 092008 (2017)

## Slide 5: Grain boundaries remain nearly unchanged
Microstructure has changed though
(a) Inverse pole figure and (b) image quality map produced using EBSD
D.E.J. Armstrong et al. | JNM 432, 428 (2013)
self-ion irradiated W

## Slide 6
Is GB transparent
to neutron irradiation?

## Slide 7
Likely!!
Insufficient facts always invite danger.
Is GB transparent
to neutron irradiation?

## Slide 8: What’s in this talk…
Primary Knock-on Atoms to simulate n-irradiated cascades
Cascades
  In periodic bulk
  Near surface
  Near grain boundary
    Damage detection methods
    Preliminary results

## Slide 9: Irradiation damages
in single crystalline bulk
FS-AT / ZBL as implanted by Fikar and Schaeublin
Wigner-Seitz (W-S) analysis
H.G. Lee, S. Yoo, B. Lee, and K. Kang | Nuclear Fusion 60 (2020)

## Slide 10: Total defect neutrality in periodic bulk
# vacancies = # SIAs
H.G. Lee et al. | unpublished
Young’s modulus

## Slide 11: Irradiation damages
in W foils
D. R. Mason et al. | J. Phys.: Condens. Matter 26 (2014) 375701
sheared
1/2⟨111⟩ vac loop
edge 1/2⟨111⟩ vac loop
⟨100⟩ vac loop
~ 0.01 dpa w/ 150 keV W+ @ 300K
“the largest loops to be predominantly of prismatic 1/2⟨111⟩ type and of vacancy character”

## Slide 12: Irradiation damages
near surface
Mobile (vacancy) dislocation loop
Immobile (vacancy) dislocation network
H.G. Lee et al. | Nuclear Fusion 60 (2020)
Surface ~ a defect sink w/ infinite capacity

## Slide 13: Irradiation damages
near grain boundary (GB)
Common Neighbor Analysis (CNA) showing non-BCC atoms
Grain boundary ~ a defect sink w/ finite capacity

## Slide 14: GBs absorb defects
Then what?
Possible scenarios
  Diffusion inside GBs
  Dislocations
  Crystal growth
    May be in the form of GB motion for small-area boundaries

## Slide 15: We need defect counts
Wigner-Seitz as implemented in popular tools
Based on initial atomic positions
Interstitial
Initial state
Final state
1 vac + 1 int

## Slide 16: W-S0
with a fictitious perfect lattice
Volume-based

## Slide 17: W-S0
with a fictitious perfect lattice

## Slide 18: W-S0
fails in polycrystalline structures
Interstitials
Vacancy
Interstitial-vacancy pair FALSE detection
Translation of reference lattice hardly matters
Rotation matters!!
W-S cell
(Primitive cell)

## Slide 19: W-S
fails even for a clean GB
100 nm x 100 nm x 300 nm
PKA Energy = 300 keV @ 823K
PKA location = 1nm from GB
<100>
<111>
Vacancy
Interstitial
Due to rotation and/or distortion of lattice around cascade residuals

## Slide 20: CNA+WS
Interstitial loops
Vacancy
Interstitial

## Slide 21: CNA+DXA

## Slide 22: How to separate defects
in GB from those in bulk w/ defect type info?
0 ps
defect count = 65,798
bcc <100>/<111>
100 nm x 100 nm x 300 nm
PKA Energy = 300 keV @ 823K
36.13 ps
Initial GB
<100>
<111>
defect count = 70,170
CNA only tells you either crystalline or other

## Slide 23: Deep inside
atom of interest
probe neighbor
common neighbors
CNA
B. Lee et al. | JCP 129, 024711 (2008)

## Slide 24: CNA goes beyond non-bcc
vacancy
<111> DB
<110> DB

## Slide 25: CNA
with pair types

## Slide 26: Crystal growth
from GB
0 ps
GB atoms : 3,771
Bulk defects : 0
36.13 ps
CNA w/ pair type results
GB atoms : 3,686
Bulk defects : 1,118
Front view
Side view

## Slide 27: Irradiation damages
Pt Σ3 {112} GBs
near GB
~ 1 dpa w/ 2.8 MeV Au4+
C. M. Barr et al. | Sci. Adv. 8, eabn0900 (2022)

## Slide 28: End of evolution scenario?
Moving Vs Flattening?
Kinetically limited
Energetics driven
(annealing?)
End of evolution
Against energetics

## Slide 29
Is GB transparent
to neutron irradiation?

## Slide 30
Likely… as far as GB degradation goes
GB is a defect sink, which in turn make it the source of other defects
It will be interesting to see how GBs do
in the presence of transmutation and hydrogen

## Slide 31: Remarks
During irradiation
CNA seems promising for detections of various defects including GBs
  Fine-tuning in progress
Irradiation may stabilize the microstructure?
  GBs may realign to reduce energy penalty
  GB energy reduction = grain growth?

## Slide 32: Future outlook
K. Heinola et al. | Phys. Rev. B 82, 094102 (2010)
Y. Shin et al. | unpublished

## Slide 33
Thank you!
Suomenlinna, July 17, 2024

## Slide 34: Defect counts
Dose Vs microstructure
Wigner-Seitz (W-S) analysis
arc-spa
K. Nordlund et al. / Nature Comm (2018)9:1084

## Slide 35: Residual defects
Due to stress field
Chart: SIA Formation energy (eV)
| <111> DB | <111> CWD | <110> DB | <100> DB | octa | tetra
0 GPa | 0 | 0.003317 | 0.30664 | 1.977 | 2.0463 | 1.4645
185.56 GPa | 0 | 0.002303 | 0.9049 | 3.8077 | 3.8962 | 2.3257
806.222 GPa | 0 | 0.00093 | 1.9044 | 6.573 | 6.6636 | 3.8522

## Slide 36: Residual defects
Due to temperature field
Mart ́ınez et al., J. Appl. Phys. 130, 215904 (2021)

## Slide 37: Irradiation damages
in bulk
P downwind:
SIA concentration increasing
T downwind:
SIA concentration decreasing
PKA E = 20 keV @ 300K
Defects within 10 nm radius
Y. Shin and B. Lee, unpublished

## Slide 38: CNA Vs. PTM
Polyhedron Template Matching
0 ps
defects = 65 798
PTM
defects = 58 615
CNA
100-111 / 1nm / 300keV
In cascade region
Selected sample:
36.13 ps
defects = 70 170
defects = 63 150
PTM
CNA

## Slide 39: W-S
fails even for a clean GB
100 nm x 100 nm x 300 nm
PKA Energy = 300 keV @ 1nm from GB
<100>
<111>
Vacancy
Interstitial
Due to rotation and/or distortion of lattice around cascade residuals

## Slide 40: Crystal growth
from GB
0 ps
Non-BCC : 65,798
BCC : 0
bcc <100>/<111>
100 nm x 100 nm x 300 nm
PKA Energy = 300 keV @ 1nm from GB
36.13 ps
Initial GB
<100>
<111>
Non-BCC : 57,354
BCC : 8,444
CNA results

## Slide 41: GB evolution
C. M. Barr et al. / Sci. Adv. 8, eabn0900 (2022)
Grain boundary thickness increases
PKA Energy = 10 keV @ 300K

## Slide 42: GB energetics
to find optimum
Nucleation
  Crystal growth
  Dislocations
Energetics
  GB facet/surface energies
  GB area

## Slide 43: How to quantify point defects
near GBs
CNA
  atom-based
  Unable to detect vacancy
  GBs detected
  Could be expensive
  Hyperparameter dependence

## Slide 44: How to quantify point defects
near GBs
W-S
  Lattice-based
  Initial configuration assumed to be perfectly crystalline
  Unable to detect GBs but may detect changes in GBs

## Slide 45: How to quantify point defects
near GBs
W-S0
  Lattice-based
  Initial configuration assumed to be perfectly crystalline
  Symmetry-based
  Unable to detect GBs