## Slide 1
CHANGE OF WALL MATERIAL FROM BERYLLIUM TO TUNGSTEN IN THE NEW ITER BASELINE: PHYSICS BASIS, IMPLICATIONS FOR RESEARCH PLAN AND WALL DESIGNS FOR ITS OPERATIONAL PHASES
Alberto Loarte
On behalf of co-authors from ITER Organization and ITER Members
The views and opinions expressed herein do not necessarily reflect those of the ITER Organization.
30th IAEA Fusion Energy Conference, Chengdu, China, 15 October 2025

## Slide 2
Summary of new baseline, W Wall strategy and risks
    W wall advantages + risks
    ITER Research Plan and wall strategy
Vacuum conditions
Scenario Phases
  Limiter
  L-mode diverted
  H-modes : SRO and DT-1
W wall design to optimize advantages for SRO and DT-1
Conclusions
Outline

## Slide 3
New baseline, W wall strategy and risks

## Slide 4
Physics basis for tokamak operation with W walls much stronger than at start of ITER construction
W wall provides advantages to new ITER baseline compared to Be
▪ Low erosion rate  Longer PFC lifetime
▪ Low Tritium retention
▪ High melting point  Higher resilience to disruption loads (higher Ip before large scale melting in unmitigated events and easier mitigation )
W wall introduces new risks
    ▪ Loss of O2 gettering  vacuum conditions
▪ Increased plasma W contamination risk  large Prad (radiative collapse, loss of H-mode, ….)
W wall advantages in ITER and risks
New baseline has been optimized to maximize W wall advantages and reduce risks

## Slide 5
Robust achievement of Projects’ goals in three phases : Start of Research Operation (SRO), 1st DT phase (DT-1) + 2nd DT phase (DT-2)
Realistic operational assumptions and minimization of technical risks
  SRO : scenario development and commissioning of systems  inertially cooled W wall
  DT-1 : W water cooled wall + Paux = 103 – 120 MW  higher Prad in scenario development + D - DT
New baseline and IRP : W wall strategy

## Slide 6
W wall and Vacuum Conditions

## Slide 7
Boronization system reduces O2 risk
Boron provides O2 gettering  14 diborane injection points + 11 GDC anodes
    E. Geulin – WEST wall conditioning with Boron – 18/10 8: 30 P7
    J. Hobirk - Tungsten limiter Start-up experiments (ASDEX Upgrade, WEST) – 15/10 17:30
Lifetime of B layer evaluated by erosion-deposition (WallDYN3D)
  short on plasma exposed areas
  ~ few 104 s in remote areas  O2 gettering not to cover W by B
50 nm B binds ∼1–5 × 1020 O2/m2  10% wall area absorbs 2.5 -12.5 weeks 316 SL outgassing
Maximum boronization frequency 2 weeks (STM)
    D. Mateev – Fuel retention and recovery in JET – 16/10 17:05
K. Schmid NME 2024 and ISFN R&D
t = 0 s
100 nm B
Wall-deposited B erodes and migrates to divertor or is covered by W  0.3 H per B
Plasma operation + ICWC to remove H
t = 105 s
< 10 mm B:W
T. Wauters NME 2025

## Slide 8
Scenario phases : Limiter

## Slide 9
Limiter phase  easy W penetration into core plasma  strongly self regulated system Te GW Prad Te (ITER modelling and experiments)
Central ECH required to avoid radiative collapse by W  Bt = 2.65 & 5.3 T
W radiation: low limiter loads but central ECH essential
    J. Hobirk - Tungsten limiter Start-up experiments (ASDEX Upgrade, WEST) – 15/10 17:30
    X. Gong – EAST experiments to support IRP – 14/10 14:25
    M. Schneider – Integrated Modelling – 15/10 17:30
ITER - Y. Zhang – NF 2025
ITER - JINTRAC - Pitts- NME 2025
EAST

## Slide 10
Scenario phases : L-mode diverted

## Slide 11
Low/medium Ip ECH heated L-modes resilient to W accumulation & radiative collapse (low absolute ne and high Te) due to limited equipartition
Low W wall risk for ECH heated L-modes
ITER - JINTRAC – Loarte - PPCF 2025
ASDEX Upgrade – Dux – NF 2011
    D. Fajardo – Validated integrated modelling of W in experiments and ITER – 18/10 8:30 P7
    M. Schneider – Integrated Modelling – 15/10 17:30
    S.H. Kim – Development of High-Fidelity Plasma Simulator – 17/10 14:00 P6

## Slide 12
Scenario phases : H-mode
SRO ELMy H-mode
Controlled ELM H-mode Q ≥ 10

## Slide 13
ELMs melt divertor monoblock gaps for Ip ≥ 5 MA/2.65 T and also contaminate core plasma by W  H-mode scenario to be developed in SRO
<GELMW influx> (SOLPS + experimental guidance) + JINTRAC  requirements
ELM control essential for SRO ELMy H-modes
ITER - JINTRAC – Loarte - PPCF 2025
    S.H. Kim – Development of High-Fidelity Plasma Simulator – 17/10 14:00 P6
    M. Schneider – Integrated Modelling – 15/10 17:30
  fELM ≥ 20 Hz required  4 pellet injectors (fpellet ~ 60 Hz) and full set of ELM control coils
  5 MA/2.65 T ECH H-mode resilient to W influxes : Low <ne>, Te ~ 10 keV + W pedestal screening
JET- Huber – NME 2020

## Slide 14
Suppressed/no-ELM regime required for Q ≥ 10  modelled with Dped, cped anomalous for main ions and anomalous + neoclassical for W
Improved evaluations : W sources from modelling + self-consistent SOL plasma (largest Pwall and Gwall compatible with design)  Ne main driver for W wall source
ITER - SOLPS – Pshenov
    E. Kaveeva – First SOLPS-ITER wide grid SOL simulations of Q ≥ 10 – 15/10 14:00
ERO2.0 (W gross erosion) – C. Bauman
Impact of W wall on Q ≥ 10 is low/moderate - I

## Slide 15
Integrated modelling : JINTRAC core plasma + near SOL + ad-hoc wall source to match nW/ne|sep for “largest possible” W source
  Paux ~ 80 MW and Pfusion = 500 MW with Psep/PLH > 1.5  Q > 6 for “worst possible case”
  W pedestal screening confirmed as key to maintain fusion performance
ITER – JINTRAC - Köchl
Impact of W wall on Q ≥ 10 is low/moderate - II

## Slide 16
ICH antenna flexibility used to achieve ~ 3-strap like EII
W source by ICH << W wall source (~1021 W/s) to be confirmed in SRO  upgrade to 20 MW for DT-1
DT-1 ICH and W source
ITER – JINTRAC - Köchl
SOLPS-ITER
wide grid
PICH = 10 MW
V, Bobkov NME 2024 & L. Colas NME 2025

## Slide 17
W wall design to optimize advantages for SRO and DT-1

## Slide 18
SRO wall : Scenarios + resilience to unmitigated loads :
In-vessel VS to decrease risk of downwards VDE
W (wt.%) 97
Ni (wt.%) 2
Fe (wt.%) 1
Tmelt~1500 oC
Tmelt ~ 3400 oC
Cost: choice of W material based on stationary & transient loads (up to 15 MA)
Optimized for resiliency to unmitigated/partially mitigated transient loads
ITER 15 MA unmitigated VDE – JOREK – Artola
    M. Schneider – Integrated Modelling – 15/10 17:30
    J. Artola – Modelling of thermal Loads during VDEs at JET and ITER – 18/10 8:30 P7

## Slide 19
ITER – GEANT4 + MEMENTO - S. Ratynskaia – Sub. PPCF 2025
Stationary heat fluxes input to design as for Be wall
Resilience to disruptions (high Tmelt) + high stopping power (runaway electrons)
  W thickness increased to 12 mm to reduce risk of water leaks in runaway loaded areas
  Runaway mitigation remains essential with DT-1 W wall
on FW-apex
    S. Ratynskaia – https://arxiv.org/abs/2509.20261
ERE-kin ~ 2000 KJ/ Ip-RE(MA)
ERE-mag ~ 200 MJ (Ip-RE(MA)/9.5)2
DT-1 wall: high Q scenarios + runaway loads
on FW-apex

## Slide 20
Conclusions
Advantages/risks of W wall in ITER assessed using experiments and modelling
New baseline includes new/modified systems and operational strategies to mitigate risks of W wall : boronization, increase of PECH & Ptot (also for Q ≥ 10 with 3.1025 n in DT-1), operation with central ECH at 2.65 T and 5.3 T, etc.
Staged installation of systems (SRO and DT-1) includes risk minimization : inertially cooled W wall and ELM control schemes in SRO
W wall design in SRO & DT-1 optimized to maximize resilience to disruption loads : reduce melting by unmitigated disruptions and runaway risk (DT-1)
  Support by Members’ fusion researchers is essential to:
  Perform experiments to address open R&D issues ITR-25-005
  Further develop integrated models and their validation with experiments

## Slide 21
Thanks for your attention !

## Slide 22
Boronization - I
Boron provides O2 gettering  14 diborane injection points + 11 GCD anodes
Non-symmetric GDC anode distribution at in SRO & non-uniform boronization  experiments show boronization needed but spatial distribution not too critical
B2H6 ionization and dissociation in SRO
T. Wauters NME 2025
    E. Geulin – WEST wall conditioning with Boron – 18/10 8: 30 P7
    J. Hobirk - Tungsten limiter Start-up experiments (ASDEX Upgrade, WEST) – 15/10 17:30

## Slide 23
Boronization - II
Lifetime of B layer evaluated by erosion-deposition WallDYN3D  short on plasma exposed areas and ~ few 104 s in remote areas  boronization for O2 gettering not to cover W
50 nm B binds ∼1–5 × 1020 O2/m2  10% wall area 2.5 -12.5 weeks 316 SL outgassing
Maximum boronization frequency 2 weeks (STM)
K. Schmid NME 2024 and ISFN R&D
t = 0 s
100 nm B
t = 105 s
< 10 mm B:W
Wall deposited B erodes and migrates to divertor or is covered by W  0.3 H per B in deposits
Plasma operation + ICWC to remove H
    D. Mateev – Fuel retention and recovery in JET – 16/10 17:05

## Slide 24
During limiter phase plasma is in direct contact with W wall
Strongly self regulated system Te GW Prad Te in ITER modelling and experiment (EAST, ASDEX Upgrade, WEST, …)
Limiter - I
    J. Hobirk - Tungsten limiter Start-up experiments (ASDEX Upgrade, WEST) – 15/10 17:30
ITER - Y. Zhang – NF 2025
    X. Gong – EAST experiments to support IRP – 14/10 14:25
EAST - Pitts- NME 2025
    M. Schneider – Integrated Modelling – 15/10 17:30

## Slide 25
W accumulation and radiative collapse can occur due to unfavourable core W transport and power balance in ITER and present experiments
Central ECH needed to avoid ITER limiter phase collapse  Bt = 2.65 & 5.3 T
Limiter - II
    J. Hobirk - Tungsten limiter Start-up experiments (ASDEX Upgrade, WEST) – 15/10 17:30
    X. Gong – EAST experiments to support IRP – 14/10 14:25
ITER - JINTRAC - Pitts- NME 2025
    D. Fajardo – Validated integrated modelling of W in experiments and ITER – 18/10 8:30 P7
    M. Schneider – Integrated Modelling – 15/10 17:30

## Slide 26
L-mode plasmas with conditions typical of 15 MA ramp-up flat-top modelled
Low/medium Ip L-modes resilient to W accumulation & radiative collapse
L-mode diverted - I
ITER - JINTRAC – Loarte - PPCF 2025
ASDEX Upgrade – Dux – NF 2011
    D. Fajardo – Validated integrated modelling of W in experiments and ITER – 18/10 8:30 P7
    M. Schneider – Integrated Modelling – 15/10 17:30
    S.H. Kim – Development of High-Fidelity Plasma Simulator – 17/10 14:00 P6

## Slide 27
Low <ne> and Te ~ 10 keV by use of central ECH provide resilience to W accumulation and radiative collapse for low/medium Ip
L-mode diverted - II
ITER - JINTRAC – Loarte - PPCF 2025
    D. Fajardo – Validated integrated modelling of W in experiments and ITER – 18/10 8:30 P7
    M. Schneider – Integrated Modelling – 15/10 17:30
    S.H. Kim – Development of High-Fidelity Plasma Simulator – 17/10 14:00 P6

## Slide 28
ELMs expected to melt divertor monoblock gaps for Ip ≥ 5 MA/2.65 T
Instantaneous GELMW-div influx modelled from SOLPS modelling and used to evaluate average <GELMW influx> using experimental guidance
SRO ELMy H-mode - I
SOLPS-ITER – Dux – NME 2017
ITER - JINTRAC – Loarte - PPCF 2025
    S.H. Kim – Development of High-Fidelity Plasma Simulator – 17/10 14:00 P6
    M. Schneider – Integrated Modelling – 15/10 17:30

## Slide 29
Wall source scanned in JINTRAC to compare with <GELMW influx>
  fELM ≥ 20 Hz required  4 pellet injectors (fpellet ~ 60 Hz) and full set of ELM control coils
  5 MA/2.65 T ECH H-mode resilient to W influxes : Low <ne>, Te ~ 10 keV + W pedestal screening
SRO ELMy H-mode - II
ITER - JINTRAC – Loarte - PPCF 2025
<nW/ne>
    S.H. Kim – Development of High-Fidelity Plasma Simulator – 17/10 14:00 P6
    M. Schneider – Integrated Modelling – 15/10 17:30
Instantaneous PradELM-W  Max tolerable DWELM

## Slide 30
Suppressed/no-ELM regime required for Q ≥ 10: Dped, cped anomalous for main ions and anomalous + neoclassical for W  W wall low/medium risk
Initial evaluations : W sources from modelling + ad-hoc far SOL
  W divertor/wall sources (edge modelling + ad-hoc far SOL) : Ne main driver for W source
  Integrated modelling (near SOL ad-hoc wall source) : W pedestal screening essential
DT-1 Q ≥ 10 - I
    M. Schneider – Integrated Modelling – 15/10 17:30
K. Schmid NME 2024
ITER - JINTRAC – Loarte - PPCF 2025

## Slide 31
Improved modelling for “largest possible” W source with SOLPS-ITER wide grid + ERO2.0  Pwall ~ 20 MW and Gplasma-wall/ Gplasma-div ~ 0.1
W divertor/wall sources : Ne confirmed as main driver for W source
DT-1 Q ≥ 10 - II
ITER - SOLPS – Pshenov
    E. Kaveeva – First SOLPS-ITER wide grid SOL simulations of Q ≥ 10 – 15/10 14:00
1015
erosion flux [m-2s-1]
1016
1017
1018
1019
1020
1021
ERO2.0 (W gross erosion) – C. Bauman

## Slide 32
Integrated modelling : JINTRAC core plasma + near SOL + ad-hoc wall source to match nW/ne|sep for “largest possible” W source
  Paux ~ 80 MW maintain Pfusion = 500 MW  Q > 6 for “worst possible case” confirmed
  W pedestal screening confirmed as key to maintain fusion performance
DT-1 Q ≥ 10 - II
ITER – JINTRAC - Köchl

## Slide 33
ICH antenna flexibility used to achieve ~ 3-strap like EII
W source by ICH << W wall source (~1021 W/s) to be confirmed in SRO  upgrade to 20 MW for DT-1
DT-1 ICH and W source
ITER – JINTRAC - Köchl
SOLPS-ITER
wide grid
PICH = 10 MW
V, Bobkov NME 2024 & L. Colas NME 2025

## Slide 34
Wall design for SRO (inertially cooled)
ITER - JINTRAC - Pitts- NME 2025
In-vessel VS to decrease risk of downwards VDE
W (wt.%) 97 Ni (wt.%) 2 Fe (wt.%) 1
Tmelt~1500 oC
Tmelt ~ 3400 oC
Stationary heat fluxes and integrated energy input to design
Resilience : widest risk possible operational space (inc. unmitigated disruptions)
Cost: choice of W material based on stationary and transient loads
ITER – JOREK – Artola
    M. Schneider – Integrated Modelling – 15/10 17:30
    J. Artola – Modelling of thermal Loads during VDEs at JET and ITER – 18/10 8:30 P7

## Slide 35
Wall design for DT-1 (water cooled)
ITER – GEANT4 + MEMENTO - S. Ratynskaia – Sub. PPCF 2025
Stationary heat fluxes input to design
Resilience to disruptions (high Tmelt) + high stopping power (runaway electrons)
  W thickness increased to 12 mm to reduce risk of water leaks in runaway loaded areas
  Runaway mitigation remains essential with DT-1 W wall
on FW-apex
on FW-apex
on FW-apex
    S. Ratynskaia – https://arxiv.org/abs/2509.20261
ERE-kin ~ 2 MJ/ Ip-RE(MA)
ERE-mag ~ 200 MJ (Ip-RE(MA)/9.5)2