## Slide 1
5th Technical Meeting on Divertor Concepts, IAEA HQ, Vienna, Austria 28 Oct. 2025 IDM UID: EEG3BQ
Is impact of neutron irradiation sufficiently well understood?
    Should trying to shield HHF areas from neutron flux be more of a design driver?
    Structures behind main armour  are they determining the limit instead of the W?
    Do we know enough about neutron irradiation of advanced materials – too much Cu in W-Cu?
Is the monoblock design optimized?
    Bonding technology stable, but:
    Width  can relax bevel angle to limit reduction in projected area, fewer welds etc.
    Thickness above cooling channel (1.4 margin to CHF) – physics load spec, trade-off between stationary surface temperature and resilience to transients
    Cooling pipe dimensions (increased diameter, tube thickness)
Are monoblocks even really necessary everywhere?
    Minimize curved PFU designs – unnecessary complexity – MB’s only on straight regions?
    XPR/CRD type solutions may relax the need for extremely high stationary heat flux resilience and we should restrict the HHF areas to the absolute minimum
Divertor engineering and materials session: discussion (I) R. A. Pitts, E. Tsitrone

## Slide 2
5th Technical Meeting on Divertor Concepts, IAEA HQ, Vienna, Austria 28 Oct. 2025 IDM UID: EEG3BQ
J. P. Gunn et al., NME 42 (2025) 101838
Divertor engineering and materials session: discussion (II) R. A. Pitts, E. Tsitrone
T. Liu et al., IJRMHM 134 (2026) 107459
Can MB’s be replaced by flat tile technology  combined with new advanced materials (e.g. W-K, W-Y2O3)?
    What comprehensive test program to be ready for DEMOs
What about completely different designs the for HHF components?
    Or use AM for more complex/optimized cooling channels?
    Need for permeation barrier?
    Liquid metal concepts losing any traction now?
Cassette design?
    Should reactors decouple cassette body from PFC’s  BEST solution, easier for remote maintenance /replacement
    Should any form of embedded diagnostic be simply excluded in reactor designs  makes cassette integration extremely difficult on ITER
    Consider designs optimized for new regimes (XPR)