## Slide 1: Towards Advanced Wall Modeling Using Machine Learning and Its Integration with Neutral Transport Simulations
S. Saito Yamagata Univ., Japan
H. Nakamura NIFS, Japan
K. Sawada Shinshu Univ, Japan
K. Hoshino Keio Univ., Japan
Y. Homma QST, Japan
S. Yamoto QST, Japan
Neutral transport code
Fluid model (SONIC code)
Wall model

## Slide 2
Contents
Background
Molecular dynamics simulation of hydrogen recycling on tungsten wall
Integration with fluid codes and neutral transport simulation
Machine learning approaches for the wall model
Future work: towards advanced wall modeling

## Slide 3: Hydrogen recycling and plasma-material interaction
Hydrogen recycling on the wall
Core plasma
Edge plasma
H
Incident
hydrogen
Neutral transport
H2
H
Recycled
hydrogen
collision, ionization
dissociation, recombination
atom
molecule
Core
plasma
First wall
Edge
plasma
Divertor
Separatrix

## Slide 4
Background：Importance of detached plasma and hydrogen molecular processes
Figure 13 from Y. Hayashi et al 2016 Nucl. Fusion 56 126006 doi:10.1088/0029-5515/56/12/126006
Vibrational states v
Transport of neutrals (hydrogen atoms / molecules)
by Neutral transport code + Collisional radiative model
Hydrogen recycling model by MD
Molecular Assisted Recombination: MAR
Charge exchange recombination (CX) :
Dissociative recombination (DA):
Detached plasma
Key technology to reduce heat load on the wall (prevent walls from melting)
Neutral gas (hydrogen, nitrogen, neon, etc.) is injected into the divertor region to neutralize the plasma.

## Slide 5: Overview of our wall model
Spatial distribution of hydrogen molecule’s density in the edge plasma of JA-DEMO
（Neutral transport simulation）
We would like to use machine learning (ML) model
S. Saito, et al., Nucl. Fusion 64 126067 (2024).
Context and Motivation
We would like to calculate neutral transport in the edge plasma under the dynamically changing interaction between the plasma and the wall.
By using machine learning, we can dynamically generate the distribution of released hydrogen (especially the rovibrational states of hydrogen molecules) from the plasma parameters near the wall.
H
W
H/W=0.23 T=300K Ti=2.81eV
0
Rotational states
Number of Emissions / Number of Samples
5
10
0.0000
15
20
25
30
0.0025
0.0050
0.0075
0.0100
0.0125
0.0150
0.0175
0.0200
0.1
Electron temperature Te [eV]
1
10
50
Distribution of Rotational states of released hydrogen molecules
Output: emission distribution of hydrogen (translational energy, rovibrational states)
Fully connected network
Input
Ion temp.
Mater. temp.
H/W
Elec. temp.
Output
Training data
Prediction
① MD simulation
② Training ML model
③ Prediction of release distribution
Evaluation of rovibrational states of emitted hydrogen molecules
S. Saito, et al., Contrib. Plasma Phys. e201900152 (2020).
S. Saito, et al., Jpn. J. Appl. Phys. 60, SAAB08 (2021).
Notes: ・炉壁から放出された水素分子の振動・回転準位をMDで計算する。
・得た振動・回転準位をもとにNT計算を実施し、周辺プラズマ周辺の振動回転準位のポピューレションの分布を計算
・分光計測との比較も検討

## Slide 6
Contents
Background
Molecular dynamics simulation of hydrogen recycling on tungsten wall
Integration with fluid codes and neutral transport simulation
Machine learning approaches for the wall model
Future work: towards advanced wall modeling

## Slide 7: Hydrogen Recycling Model on Tungsten Materials （MD）
Target material ：Hydrogen contained
bcc tungsten
Boundary condition：Periodic in x and y
Material temperature：300 K
Interaction：EAM potential [1]
Incident atom：Hydrogen atom
Number of Incidents：One
Thermostat： Langevin
Incident energy： 0.1-100 eV
H/W：0.2
[1] Li-Fang Wang, Xiaolin Shu, Guang-Hong Lu, and Fei Gao: J. Phys. Condens. Matter 29 (2017) 435401.
Tungsten (W)
Hydrogen (H)

## Slide 8
H (Incident atom)
(containing incident atom)
H (in the material)
(Not containing incident atom)
When the incident energy is low, many molecules containing incident hydrogen are emitted.
→ There is a possibility that a large amount of hydrogen molecules are released under detached condition.
H (Incident atom)
H (in the material)
(Not containing incident atom)
Incident energy dependence of hydrogen emission
S. Saito, et al., “Emission of high rovibrational hydrogen molecules under detached plasma conditions by recycling on the tungsten wall”, Nuclear Fusion 64 126067 (2024).

## Slide 9: Trajectory analysis of H2 generation on the surface in low incident energy case
When the incident energy is low, most of the incident hydrogen atom
forms molecules on the surface.
S. Saito et al., Jpn. J. Appl. Phys. 60, SAAB08 (2021)
Tungsten atom
Hydrogen atom
Tungsten atom
Ein = 0.1 eV, H/W=0.2

## Slide 10
Incident hydrogen atoms acquire surface binding energy (~1.5 eV) when they are trapped on the surface.
When forming a molecule on the surface, the molecule acquires the binding energy (~4.5 eV) between two hydrogen atoms.
After forming a molecule on the surface, the molecule receive a repulsive force from tungsten wall and the molecule is accelerated (less than 1.0 eV?) in the vertical direction.
→ Possibility of forming molecules with high rovibrational states
Energy acquisition mechanism of hydrogen molecules
r = 0.733Å
Interaction energy between two hydrogen atoms
Interaction energy between a hydrogen molecule and tungsten wall

## Slide 11: Incident energy dependence of distribution of rovibrational states of released hydrogen molecules
Ein=0.1eV
Ein=1eV
Ein=10eV
Ein=100eV
Ein=0.1eV
Ein=1eV
Ein=10eV
Ein=100eV
0.1000
0.0100
0.0010
0.0100
0.0010
0.0600
0.0005
0.0005
0.3000
Count / Number of Trials
Count / Number of Trials
Rotational state J
Vibrational state v
0
5
10
15
20
25
30
0
2
4
6
8
10
12
14
Even if the incident energy is low, molecules with relatively high rovibrational states are formed.

## Slide 12
Contents
Background
Molecular dynamics simulation of hydrogen recycling on tungsten wall
Integration with fluid codes and neutral transport simulation
Machine learning approaches for the wall model
Future work: towards advanced wall modeling

## Slide 13
Figure 13 from Y. Hayashi, et. al. 2016 Nucl. Fusion 56 126006 doi:10.1088/0029-5515/56/12/126006
Initial value
H,
H2 (v,J)
Divertor
MD sim.
Combining NT-CR code, MD, and SONIC code
Te, ne (SONIC code)

## Slide 14
Place No.
0
Inner divertor
5
10
15
20
25
30
0
5
10
15
20
25
30
Place No.
Outer divertor
Te
ne
Emission distribution of rovibrational states (v, J ) by MD sim.
NT simulation with CR model
N. Asakura, K. Hoshino, Y. Homma, Y. Sakamoto, Joint Special Design Team for Fusion DEMO, “Simulation studies of divertor detachment and critical power exhaust parameters for Japanese DEMO design”, Nuclear Materials and Energy 26 (2021) 100864.
Te & ne by SONIC
Neutral transport simulation with SONIC + MD for JA-DEMO

## Slide 15
Spatial distribution of H2 near divertor
d
The data suggest that the molecules with rotational states higher than J=15 are produced by the collisions with electrons, H+ ions, or neutral H atoms near the divertor, even though the absence of those higher-level molecules in the emission distribution.
S. Saito, et al., Nucl. Fusion 64 126067 (2024).
S. Saito, et al., Nucl. Fusion 64 126067 (2024).

## Slide 16
Rovibrational state dependence of absorbed energy by collision with electrons
v :
J :
0〜31
0〜30
〜28
〜27
〜25
23
22
20
18
16
14
12
10
7
2
0
1
2
3
4
5
6
7
8
9
10
12
14
Rovibrational states before collision
Absorbed energy by collision with electrons
[eVcm-3s-1]

## Slide 17: Dependence of rotational states distribution of plasma near wall on wall temperature
A. Terakado, et al., Plasma Fusion Res. 13, 3402096 (2018).
Actual rotational temperature by spectroscopic measurement in GAMMA10
2 cm from the inner divertor at No. 0
Simulation results using wall model + neutral transport for JA-DEMO
Wall temperature (K)

## Slide 18
Contents
Background
Molecular dynamics simulation of hydrogen recycling on tungsten wall
Integration with fluid codes and neutral transport simulation
Machine learning approaches for the wall model
  Prediction model for emission distribution
  Deep learning assisted kMC-MD hybrid simulation
Future work: towards advanced wall modeling

## Slide 19
Application of Machine Learning (ML) to Hydrogen Recycling Model
Incident atom
Wall
Retained hydrogen atoms/molecules
H
H
H2
Incident species
Incident angle
Incident energy
Molecule
Atom
Emission species (atoms/molecules)
Emission angle
Transrational energy
Rovibrational states
Temperature
Density
Crystalline structure
Input-A: Irradiation condition
Output: Information of emitted particle
Input-B：
Material condition
Training data
Machine Learning
model
Hydrogen recycling model （MD code）
Neutral transport code
Limited results for hydrogen emission
Reference
Call
Results
Results
Training
Hydrogen recycling model （MD code）
Neutral transport code
Conventional method (Full MD)
Proposed Method (Predicted by ML)
Applicable to
a wide range
of conditions
Notes: Our calculation scheme successfully revealed the physics in the edge plasma.
However, when we would like to extend our calculation scheme to the wide rage of condition, we encounter a difficulty.
This figure shows the schematic diagram of the hydrogen recycling model.
We have two kind of input parameters and output parameters.
Input-A is the irradiation condition such as …
Input-B is the material condition such as …
We obtain the output such as … corresponding to the input parameters.
However, because of the computation time, it is difficult to calculate the all input conditions by MD simulation.
Therefore, in the case of conventional method which is calculated by only MD, we could only apply the limited input parmaters.
Then, we propose a method assisted by machine learning.
In this scheme, first, we obtain the training data by MD code.
Then, we train the deep learning model from the training data.
The deep learning model can apply to wide ragen of conditions even though we only obtained the training data for limited conditions.

## Slide 20
H/W=0.23 T=800K Ein=50eV
Num of Emissions / Num of Samples
Translational energy [eV]
10-1
100
101
0.00
0.05
0.10
0.15
0.20
Prediction results of release distribution
H
Translational energy of H atoms
H/W=0.23 T=800K Ein=50eV
Num of Emissions / Num of Samples
Translational energy [eV]
10-1
100
101
0.10
0.25
0.20
0.15
0.05
0.00
0
5
10
Rotational states
0.000
0.005
0.010
0.015
0.020
0.025
0.030
0.035
0.040
Num of Emissions / Num of Samples
15
20
25
30
H/W=0.23 T=800K Ein=50eV
H/W=0.23 T=800K Ein=50eV
0
Vibrational states
0.00
Num of Emissions / Num of Samples
2
4
6
8
10
12
14
0.02
0.04
0.06
0.08
0.10
0.12
0.14
0.16
H
H
H
H
H
H
)))
(((
0
500
1000
1500
2000
2500
3000
3500
4000
4500
10-5
10-4
10-3
10-2
10-1
Loss
Epoch
Input
Output
Evolution of Loss function (MSE)
Network models for prediction of translational energy of H aotms
Translational energy of H2 molecules
Rotational states of H2 molecules
Vibrational states of H2 molecules
S. Saito, et al., ”Machine learning-based hydrogen recycling model for predicting rovibrational distributions of released molecular hydrogen on tungsten materials via molecular dynamics simulations”, Nuclear Materials and Energy. 43 101942 (2025).

## Slide 21
Consideration of incident energy distribution (Shifted-Maxwellian)
Distribution of incident energy considering acceleration by sheath （Shifted-Maxwellian）
, : Ion/Electron temperature,, : Ion/Electron mass
: H/W
: Material temperature
Machine learning model for the distribution of x
: Translational energy / Rotational state J / Vibrational state
Integrate the output distribution of the machine learning model
according to the distribution 𝑓 of the incident energy
sheath
sheath edge

## Slide 22
atoms
H/W=0.23 T=300K Ti=2.81eV
10-1
Translational energy [eV]
0.04
Number of Emissions / Number of Samples
100
101
0.02
0.00
0.06
0.08
0.10
0.12
The higher the electron temperature and the deeper the sheath, the greater the amount of atoms emitted.
0.1
Electron temperature Te [eV]
1
10
50
H/W=0.23 T=300K Ti=2.81eV
10-1
Translational energy [eV]
0.04
Number of Emissions / Number of Samples
100
101
0.02
0.00
0.06
0.08
0.10
0.12
The lower the electron temperature and the shallower the sheath, the greater the amount of molecular emission.
Translational energy distribution of recycled atoms and molecules considering Maxwell distribution
molecules

## Slide 23
Contents
Background
Molecular dynamics simulation of hydrogen recycling on tungsten wall
Integration with fluid codes and neutral transport simulation
Machine learning approaches for the wall model
  Prediction model for emission distribution
  Deep learning assisted kMC-MD hybrid simulation
Future work: towards advanced wall modeling

## Slide 24
W surface
H
Injection
W surface
W surface
Injection
time
Diffusion
non-equilibrium
equilibrium
non-equilibrium
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
 | Comp. Cost | Sim. in Non-Eq. States
MD | × | ○
kMC | ○ | ×
Molecular dynamics (MD)
kinetic Monte Carlo (kMC)
Comparison of methods
Injection: MD
W surface
H
H
H
H
H
Diffusion: kMC
W surface
H
H
H
H
H
Hybrid simulation method
~ 1 ps
~ 0.1 μs
~ 1 ps
Attempt at a Deep Learning Assisted kMC-MD Hybrid Method
Objective: Simulation of hydrogen atom accumulation due to continuous injection

## Slide 25: Purpose and method
Hybrid method has the problem that it needs considerable computation cost for the calculation of the migration barrier and trapping site required for kMC calculation.
W
H
H
H
H
injection
(MD)
W
H
H
H
H
injection (MD)
H
diffusion (kMC)
H
H
H
H
W
diffusion (kMC)
H
H
H
H
W
H
Predicting the following three values by deep learning models :
      3D potential energy distribution
      Migration barrier
      Minimum potential point (trapping site)
Today’s topic
Under development
Notes: Therefore, in this study, we propose a method that adds a deep learning process between the injection and diffusion phases to enable fast computation by predicting potential minima and migration barriers.
Specifically, we will develop a model that uses deep learning to predict three key elements: 3D potential energy distribution, Migration barrier, and Minimum potential point.
In this study, I developed a deep learning model to predict the 3D potential energy distribution, and the migration barrier was determined using the Nudged Elastic Band method.

## Slide 26: Network model (Generator)

## Slide 27: Results of prediction of 3D potential energy distribution
Ture values
Predicted values
S. Saito, et al., “Deep learning model for predicting the spatial distribution of binding energy from atomic configurations”, Japanese Journal of Applied Physics, 63, (2024).
The accuracy is good based on the comparison between the true and predicted values
Absolute error
Input
EAM potential
4 hours
by 1 CPU(1 core)
DL model
0.2 second by
1 CPU(1 core) + 1 GPU
Notes: Here, about result of predicting test data.
The left figure is the label data, the center figure is the prediction data, and the right figure is the error.
The error is the absolute difference between the label data and prediction data, and it is plotted with a maximum value set to 4.
The accuracy is generally good based on the comparison between the Ture and Predict.
However, the absolute error indicates that predicting the contours of the particles is challenging.

## Slide 28
Contents
Background
Molecular dynamics simulation of hydrogen recycling on tungsten wall
Integration with fluid codes and neutral transport simulation
Machine learning approaches for the wall model
  Prediction model for emission distribution
  Deep learning assisted kMC-MD hybrid simulation
Future work: towards advanced wall modeling

## Slide 29
Deep learning Assisted
MD-kMC Method
for calculation of density
Wall model
Future work: towards advanced wall modeling

## Slide 30: Summary
Hydrogen recycling on tungsten walls was investigated using MD simulations.
Emission distributions of rovibrational states of recycled hydrogen were predicted using machine learning techniques.
The developed wall model was integrated with the SONIC code and neutral transport simulations.
Future plan: We will develop a deep learning-assisted kMC–MD hybrid method to generate training data for machine learning models that predict particle density. The model will provide input for emission distribution predictions and enable to solve the dynamical interaction between plasma and wall.

## Slide 32: Radiation damage to walls (helium bubbles)
Emission of material atoms by collisions with plasma particles
retention
sputtering
Accumulate of the Plasma particles in the material
He+
He+
He+
Helium bubbles
Changes in the material surface structure (generation of helium bubbles)
N. Ohno, et. al., J. Nucl. Mater. 363 (2007) 1153
Helium bubbles

## Slide 33
Time evolution of absorption rate by helium irradiation
Fluence [×1020 He/m2]
Ein=1 keV
Plot of stopping positions of incident helium atoms
Trajectories of incident helium atoms
S. Saito, et al., JJAP. 55 (2016) 01AH07
S. Saito, et al., proc. JSST2017 (2017)
S. Saito, et al., JJAP. 56 (2017) 01AF04

## Slide 34
Energy absorption on the fuzz structured surface
S. Kajita, et al., JJAP. 50 (2011) 08JG01
Fuzz structure of tungsten surface
formed by helium plasma exposure.
S. Saito, et al., JJAP. 55 (2016) 01AH07
S. Saito, et al., proc. JSST2017 (2017).
S. Saito, et al., JJAP. 56 (2017) 01AF04

## Slide 35
S. Saito, et al., Jpn. J. Appl. Phys. 63 9SP03 (2024).
Results of prediction of 3D potential energy distribution
surface: 正解と予測の絶対誤差
random: 正解と予測の絶対誤差
bulk: true data
surface: true data
random: true data
bulk: prediction
surface: prediction
random: prediction
bulk: absolute error
surface: absolute error
random: absolute error

## Slide 36
: Electron density and temperature of edge plasma
: Electron temperature, ion temperature, and flux to the wall at the sheath edge
: Increments in density, momentum, and energy of ions resulting from neutral transport
: Wall temperature
: Incident angle of magnetic field lines to the wall
: Deuterium, tritium, and helium densities in the wall
: The distribution of rovibrational states, and translational energy of released molecule 𝑥
: The distribution of translational energy of released atom 𝑥
Wall model
Heat conduction sim. using FEM
Deep learning Assisted
MD-kMC Method
For calculation of density
automatic generation system for ML mode

## Slide 37
cf. pix2pix
Generative adversarial network (GAN) for 2D image to 2D image conversion
input image
output image
Generator
Discriminator
GAN
pix2pix
Example: Converting grayscale image to a color image
Phillip Isola, Jun-Yan Zhu, Tinghui Zhou, Alexei A. Efros,
Image-to-Image Translation with Conditional Adversarial Networks
https://arxiv.org/pdf/1611.07004.pdf
Overview of GAN
GAN consists of two networks: a generator and a discriminator.
Generator
Output the desired image from the input image.
Discriminator
Judge whether the image is generated or real one.

## Slide 38
Usage of deep learning in kMC
255 | 255 | 0 | 0 | 0
255 | 255 | 0 | 0 | 0
255 | 255 | 100 | 100 | 100
255 | 255 | 100 | 100 | 100
2D image
Pixels (arranged in 2D array)
Pixel value represents the intensity of the pixel.
3D image
Voxels (arranged in 3D array)
Voxel value ​​represents the potential energies.
Expansion of pix2pix from 2D to 3D

## Slide 39
Structure discriminator

## Slide 40
Generation of training data by MD simulation
Training Data
・H/W (): 0.1, 0.23
・Material temperature (): 300, 600, 1000 [K]
・Incident energy (): 0.1, 1, 10, 100 [eV]
2(H/W)×3(temperature)×4(incident energy) = 24 patterns
Simulation Condition
・Target material: bcc tungsten containing hydrogen
・Boundary condition: Periodic boundary condition (x and y directions)
・Atomic interaction: EAM potential
・Heat bath: Langevin thermostat
・Incoming atom: Hydrogen atom
・Number of incident atoms: 1 atom
・Simulation time: 1ps
Test Data
・H/W (): 0.23
・Material temperature (): 400, 800 [K]
・Incident energy (): 5, 50 [eV]
2(temperature)×2(incident energy) = 4 patterns
H
W

## Slide 41
Machine Learning Model
Training Data
1500 samples
1000 samples
1000 samples
1000 samples
1distribution
1distribution
1distribution
1000 samples
1000 samples
1distribution
1distribution
random selection
Training Data
2(H/W)×3(temperature)×4(incident energy) = 24 patterns
→ 24×5(random selections) = 120 training data
Incident Energy ()
Distributions of translational energy of emitted H atoms
Distributions of translational energy of emitted H2 molecules
Distributions of rotational states of emitted H2 molecules
Distributions of vibrational states of emitted H2 molecules
Fully Connected Network
Input
Material Temperature ()
H/W()
Num of Emissions / Num of Samples
回転準位
0
0.00
0.02
0.04
0.06
0.08
0.10
5
10
15
20
25
30
Example: =0.23,
=1000K, =0.1eV
Output

## Slide 42
Direct prediction model for emission distribution considering Maxwellian distribution
Emission distribution considering Maxwellian distribution
Fully Connected Network
Input
Emission distribution for monochromatic incident energy
Input: , ,
Emission distribution considering Maxwellian distribution
Input: , , ,
Integration with Maxwellian distribution
Prediction by machine learning
合計: 11664
Emission distribution considering Maxwellian distribution
Training Data | Test Data
9331 | 2333
80%
20%

## Slide 43
0
Vibrational state v
Num of Emissions / Num of Samples
0.00
2
4
6
8
10
12
0.02
0.04
0.06
0.08
0.10
0.12
14
16
0.14
0
Rotational state J
Num of Emissions / Num of Samples
0.000
5
10
15
20
25
30
0.005
0.010
0.015
0.020
0.025
0.030
10-1
Translational energy [eV]
Num of Emissions / Num of Samples
0.00
100
101
0.02
0.04
0.06
0.08
0.10
0.12
H/W=0.23 T=900K
Ti=0.85eV Te=11.72 eV
Result of prediction
入力
出力
321
41
141
0
50
100
150
200
250
10-5
10-4
10-3
Loss
Epoch
300
10-6
350
400
H/W=0.10 T=300K
Ti=0.42eV Te=48.94 eV
10-1
Translational energy [eV]
Num of Emissions / Num of Samples
0.00
100
101
0.02
0.04
0.06
0.08
0.10
0.12
H
Transrational energy of H
Transrational energy of H2
Rotational state of H2
Vibrational state of H2
H
H
H
H
H
H
)))
(((
H/W=0.23 T=400K
Ti=2.21eV Te=1.74 eV
H/W=0.23 T=400K
Ti=2.21eV Te=1.74 eV
Atom translational energy distribution Prediction model loss function (MSE)
Atom translational energy distribution prediction model

## Slide 44
Energy absorption due to excitation of rovibrational states
: Hydrogen molecule density at vibrational/rotational level 𝑝
,
: Vibration/rotation level before collision
: Vibration/rotation level after collision
: Excitation rate coefficient due to collision with *
: Energy eigenvalue at rovibrational state 𝑝
Notes: 1eVを１つのプラズマに注入すると約10000度になる。しかし温度はマクスウェル・ボルツマン分布にし
エネルギー固有値とは
ポピュレーションいくつだ？1.0*10＾14eV
10000eVほど奪われている
めっちゃ奪われていない？
より長い時間を計算したらどうなるの？

## Slide 45
: Hydrogen molecule density
at vibrational/rotational level 𝑝
,
: Vibration/rotation level before collision
: Vibration/rotation level after collision
: Excitation rate coefficient
due to collision with electron
: Energy eigenvalue at
rovibrational state 𝑝

## Slide 46: Calculation of vibrational state v and rotational state J of H2 molecule
1. Calculate rotational state J from total angular momentum L of hydrogen molecule in center-of-mass coordinate system obtained from MD
2. Calculate the total energy E in center-of-mass coordinate
3. Find the v closest to the values ​​of J and E from the table of J, v and E pairs obtained by solving the Schrodinger equation in center-of-mass coordinate system.
Classical
system:
Quantum
system:
：Internuclear distance μ：Reduced mass
： Potential function
Notes: Of cores, no theoretical method to obtain quantum values from classical values.
However, as one possibility, we translate the classical values obtained by MD to the quantum values by these procedure.
round ~ to the nearest whole number