## Slide 1: Updates on neutron-induced reaction cross section measurements on structural materials
M. Diakaki1, G. Gkatis1,2, A. Karakaxi1,2, A. Mengoni3,4,
G. Noguere2, C. Paradela5, E. Pirovano6, A. Plompen5,
P. Schillebeckx
1 Department of Physics, National Technical University of Athens, 15780 Athens, Greece
2 CEA/DES/IRESNE/DER/SPRC/LEPh, Cadarache, 13108 Saint Paul Lez Durance, France
3 European Organisation for Nuclear Research (CERN), Switzerland
4 ENEA Bologna / INFN, Sezione di Bologna, Italy
5 European Commission, Joint Research Centre, 2440 Geel, Belgium
6 Physikalisch-Technische Bundesanstalt, 38116 Braunschweig, Germany
INDEN meeting on Structural Materials, 16-20 December 2024, IAEA

## Slide 2
OUTLINE
Neutron scattering measurements at the ELISA setup (GELINA facility) with enriched Fe samples (54Fe, 56Fe)
Transmission measurements with natural Fe samples.
I will not show new results on direct capture (the same from last year)
Near future perspectives
The 54Fe, 56Fe is the PhD thesis of Georgios Gkatis (CEA Cadarache-NTUA).
A new PhD student is starting soon on the continuation with the Cu isotopes.

## Slide 3
Neutron induced scattering (elastic/inelastic) on Iron isotopes at GELINA with highly enriched targets: 56Fe, 54Fe
Transmission measurements using natural Fe samples of different thicknesses
Experimental campaign at GELINA

## Slide 4
En ~ 1-6 MeV:
No theoretical model able to reproduce the fluctuating behavior present in medium-mass nuclei
Neutron scattering dominant BUT difficult to measure => Cross section data very limited and scarce even for very important isotopes (double differential and angle integrated)
EXFOR data on Fe(n,el)
54Fe
56Fe
Neutron scattering on 54Fe and 56Fe with the ELISA setup (JRC-Geel)
=> Evaluated (n,el) data often obtained by subtracting total and competing reaction cross sections
Notes: 2 proton based kai 2 deuteron based per angle.

## Slide 5
ELISA setup (Elastic and Inelastic Scattering Array)*:
High-resolution neutron scattering double differential cross section data En ~1-8 MeV
32 liquid organic scintillators at 8 scattering angles : detection of scattered neutrons
4 detectors per angle for redundancy/ cross checks (2 types of detectors per angle : EJ301, EJ315).
Fission chamber (1.37m from the sample) : measurement of the neutron flux
The setup is placed at a 30 m distance from the GELINA neutron source (FP1_30m).
Already used for (n,el) on natural Iron [2] -> this experiment lacked statistics.
Highly enriched targets:
*[1]M. Nyman et al., EPJ Web of Conferences 239, 17003 (2020)
[2]E. Pirovano et al., Phys. Rev. C 99, 024601 (2019)
54Fe
56Fe
Neutron scattering on 54Fe and 56Fe with the ELISA setup (JRC-Geel)
Notes: Two types of measurements were performed. One
with the sample in place (sample-in) that lasted almost
360 hours, and a second one without the sample (sampleout)
that lasted for almost 330 hours. The sampleout
measurement was carried out in order to establish
the background contribution from in-beam neutrons that
scattered once or multiple times in the air and surrounding
materials and then got detected by one of the scintillators.

## Slide 6
1) Detector characterization :
a) Resolution function: γ-ray sources / b) Response function: natC(n,el)
2) Photon / neutron separation via Pulse Shape Analysis (charge integration method)
3) Background subtraction (sample-out measurement)
4) Elastic–Inelastic separation
5) Multiple scattering correction (Monte Carlo simulations)
6) Cross section calculation:
neutrons
photons
1) 12C(n,el)
2)
4)
elastic
inelastic
Neutron scattering on 54Fe and 56Fe with the ELISA setup (JRC-Geel)
Notes: Carbon was chosen for its high inelastic
threshold of 4.81 MeV,

## Slide 7
Validation of the analysis
Extraction of the natC(n,n) cross section
Cross section known with <1% uncertainty up to 4.8MeV
Very good agreement between this work and JEFF-3.3, ENDF VIII.0 + EXP. DATA
G. Gkatis et al., Physical Review C, 110(3), 034609, (2024):
(Angular distributions : 1 - 8 MeV)
Neutron scattering on 54Fe and 56Fe with the ELISA setup (JRC-Geel)

## Slide 8
θLAB = 163.8o
θLAB = 79.4o
θLAB = 142.8o
θLAB = 58.3o
θLAB = 121.7o
θLAB = 37.2o
Similar at 56Fe, natFe, not seen at 12C !!!
G. Gkatis et al., Phys. Rev. C 109, 034612 (2024)
Neutron scattering on 54Fe : 54Fe(n,n) Differential cross sections vs Energy
θLAB = 100.6o
θLAB = 16.2o
Notes: Uncertainties 5-25%

## Slide 9
=ENDF-VIII.1=INDEN
G. Gkatis et al., Phys. Rev. C 109, 034612 (2024)
Neutron scattering on 54Fe : 54Fe(n,n) angle integrated cross section
Fluctuations can / should be included in the new evaluations
Notes: Uncertainties 5-8%

## Slide 10
θLAB = 163.8o
θLAB = 79.4o
θLAB = 142.8o
θLAB = 58.3o
θLAB = 121.7o
θLAB = 37.2o
θLAB = 100.6o
θLAB = 16.2o
G. Gkatis et al., Phys. Rev. C 109, 034612 (2024)
Neutron scattering on 54Fe : 54Fe(n, n1’) Differential cross sections vs Energy

## Slide 11
G. Gkatis et al., Phys. Rev. C 109, 034612 (2024)
All Data submitted to EXFOR since March 2024
Neutron scattering on 54Fe : 54Fe(n, n1’) angle integrated cross section
During evaluation
both techniques based on
γ –ray and neutron detection
should be considered.
Different systematic uncertainties/
Complementary.
Notes: UNCERTAINTY : 6% and 20%.

## Slide 12: Neutron scattering on 54Fe : Extraction of the 54Fe(n,tot)
=σ(54Fe(n,n))+ σ( 54Fe(n, n1’))
Notes: Cornelis :NORMALISATION ISSUES?

## Slide 13
θLAB = 163.8o
θLAB = 79.4o
θLAB = 142.8o
θLAB = 58.3o
θLAB = 121.7o
θLAB = 37.2o
θLAB = 100.6o
θLAB = 16.2o
Neutron scattering on 56Fe : 56Fe(n,n) Differential cross sections vs Energy

## Slide 14
Neutron scattering on 56Fe : 56Fe(n,n) angle integrated cross section
Good agreement with INDEN 2023
Notes: 3-6%

## Slide 15
θLAB = 163.8o
θLAB = 79.4o
θLAB = 142.8o
θLAB = 58.3o
θLAB = 121.7o
θLAB = 37.2o
θLAB = 100.6o
θLAB = 16.2o
Neutron scattering on 56Fe : 56Fe(n, n1’) Differential cross sections vs Energy
Threshold: 845 keV
More significant discrepancies with evaluations ~ systematically higher
Uncertainties at low neutron energies currently under analysis.

## Slide 16
Data agree very well
Neutron scattering on 56Fe : 56Fe(n, n1’): angle integrated cross section
Notes: Beyer : nELBE

## Slide 17: Neutron scattering on 56Fe : Extraction of the 56Fe(n,tot)
(n,tot) from INDEN/ENDF/JEFF :
BASED ON JEFF 3.2
(Vonach - Tagesen +
superimposed
Berthold high-resolution
data on natural sample
(+contribution from minor
isotopes)
Normalisation???
Maybe could be increased ??
=σ(56Fe(n,n))+ σ( 56Fe(n, n1’))+ σ( 56Fe(n, γ))
First point not to take into account because (n,n1’)
not extracted at this point

## Slide 18: What’s next on scattering at ELISA (GELINA)
Effort to expand the measurement capabilities to En < 1 MeV (ELISA setup upgrade with Li-glass detectors) - ongoing
Study of gamma emitting reactions with the Liquid scintillators’ response.
63,65Cu campaign : - severe lack of experimental data.
- ELISA setup ideal for (n,n) and (n,n1’) on Cu isotopes
63Cu
65Cu

## Slide 19
Transmission measurements at GELINA (JRC-Geel)
New transmission measurements planned and partially performed at GELINA on natFe samples
Useful:
Very thick target
(Harvey-1975)
56Fe
Total cross section minimum at 24.5keV :
=> Total cross section Capture
Maybe s-wave direct capture component with transmission on very thick sample??
Transmission: fraction of the neutron beam traversing a sample without any interaction:
: total cross section
: areal number density
Shown at INDEN-2019: Very thick samples probing into the
Total cross section minima
Notes: In this type of measurement the:
Incoming neutron fluence rate cancels
Detection efficiency cancels

## Slide 20
natFe samples: 3 metallic discs bought:
Li-glass detector used.
Sample at ~24 m flight path, detector at ~50 m.
Moderated neutron beam used (with 10B and Pb
filters)
Transmission measurements at GELINA (JRC-Geel)
ID | Thickness (mm) | Mass (mg)
1 | 1.194 | 667
2 | 4.486 | 2506.4
3 | 4.488 | 2504
No. 1 (1.2 cm) and no. 2 (4.5 cm) measured (summer 2023.)
Combination of no. 2 and no. 3 (=> 9 cm) PENDING:
to be measured as soon as GELINA is back to normal => probe into cross section minima with better statistics (similar to nELBE).

## Slide 21: Transmission calculation
: counts of the sample-in and the sample-out measurement
: background contributions
: normalization factor to account for the losses due to dead time in the detector and electronics chain
: correlated uncertainty component for systematic effects due to the background model
: time-of-flight (-start signal / -stop signal / -time offset)
detector
sample
sample

## Slide 22
The background contribution needs to be considered in a consistent way, with the black filters technique (Na –Co –W).
𝐵(t)= 𝑏𝑜 + 𝑏1𝑒−λ1𝑡 + 𝑏2𝑒−λ2𝑡 + 𝑏3𝑒−λ3(𝑡+𝑡0)
Transmission results
Data up to 100keV.
First REFIT calculation with
adjustment of the resonant parameters of JEFF 3.3.
Will follow:
-9 cm thick sample measurement
-Proper Resonance analysis of all datasets

## Slide 23
Direct Capture Calculations:
DC calculations with the pdix code completed.
DC calculations to be continued with CONRAD
Direct capture important (confirmed by independent teams/codes)
Neutron Scattering Measurements at GELINA:
54,56Fe(n,el/inl) reactions measured high resolution for the forst time with enriched targets (finalisation of 56Fe ongoing)
New experimental campaign on Neutron Scattering Measurements on 63,65Cu with enriched samples (OR 65Cu and natCu) will be perfomed (APRENDE) at the ELISA setup, in the context of a new PhD thesis (CEA / NTUA).
Improvement of the ELISA setup (with the local staff at JRC-Geel).
Evaluations could (should?) take into account the elastic channel when measured with high accuracy.
Evaluations could (should?) take into account the measurements of (n,n1’)both with γ- and n-detection
Transmission Measurements at GELINA:
Natural Fe samples of two thicknesses already measured at GELINA, analysis nearly finished.
Natural Copper samples of different thicknesses already measured at GELINA (flight path : 50 m, analysis ongoing (Master thesis Anna Karakaxi)
A “thick” natural Fe sample (~9 cm) will also be measured once GELINA is functional again.
Conclusions and future perspectives
Thank you!

## Slide 24: Extra slides

## Slide 25: Results of the 56Fe(n,n1’) - EXFOR
En = 3.25 MeV
En = 2.25 MeV
En = 3 MeV
En = 2. 5 MeV
En = 2. 75 MeV
En = 4 MeV
En = 4.65 MeV
En = 5 MeV
Notes: Pirovano large statistical uncertainties compared to current data.

## Slide 26: 54Fe results zoomed

## Slide 27: Results of the 56Fe(n,n) - EXFOR
En = 4.55 MeV
En = 1.3 MeV
En = 3.4 MeV
En = 2. 33 MeV
En = 3 MeV
En = 5 MeV
En = 6 MeV
En = 7 MeV
Notes: eLASTIC SCATTERING ENDF VIII.1 :
REFITTED KINNEY DATA + COMPARISON WITH PEREY ENRICHED IN THE OVERLAPPING DATA
>4 MeV: EMPIRE CALCULATIONS

## Slide 28: 63Cu,65Cu

## Slide 29: DRC with CONRAD