## Slide 1: Rez contribution to fusion research: Broomstick and Teflon leakage experiments
Michal Kostal
FENDL 2025
Vienna, May 14th 2025

## Slide 2: Research infrastructure used by CVR group in experiments
4 research reactors LR-0, LVR-15, VR-1 (university, CTU Prague), AKR-2 (TU Dresden)
252Cf neutron sources
  Material blocks for neutron leakage measurements:
    spheres (Fe, Ni … and others)
    cubes (CF2, Al, stainless steel, Cu, graphite … )
  Spherical tank with aqueous solutions for prompt gamma leakage measurements
    NaCl, MnSO4, FeSO4, …. , planned CO(NH2)2 (ad blue) , and many others
DT generators
Well-described AmBe
XRF analyzers
(and many others)
2

## Slide 3: Neutron spectrometry
Well-characterized spectrometer
Validation in PTB
Validation in 252Cf
Verified in Si filtered spectrum
Radulovic et al., IAEA, INDC(NDS)-0746, 2018
Chart: 6.8 MeV
Chart: Energy [MeV]
 | 0 | 0
Chart: Energy [MeV]

## Slide 4: Gamma spectrometry - HPGe
Most important is detector sensitivity
Irradiated pins measurement
  Mathematical model allows arbitrary axial power density profile
Foil measurement
  Mathematical model allows even large samples on detector cap
  Determination of coincidence summing correction
Gamma flux measurement
  Model allows evaluation of gamma flux (only the directionality needed)
Czakoj et al., Rad. Phys. and Chem. 202 (2023) 110542
Chart: Energy [keV]
| 59.540900000000001 | 122.06055000000001 | 136.47355999999999 | 391.69799999999998 | 661.65700000000004 | 898.04200000000003 | 1173.2280000000001 | 1332.492 | 1836.0360000000001
Experiment | 0.025276 | 0.15989 | 0.16466 | 0.08292 | 0.05346 | 0.04135 | 0.03239 | 0.029503 | 0.024243
MCNP verified model | 0.016552 | 0.15391 | 0.1609 | 0.083948 | 0.052926 | 0.041101 | 0.03314 | 0.029787 | 0.022585
MCNP data sheet | 0.094873 | 0.23609 | 0.23514 | 0.11246 | 0.07116 | 0.055373 | 0.044684 | 0.040151 | 0.030561
MCNP radiogram | 0.091889 | 0.22313 | 0.22088 | 0.10123 | 0.063363 | 0.049035 | 0.039428 | 0.035414 | 0.026783

## Slide 5: Uncertainties in gamma spectrometry
Systematic uncertainty
  1.8% End Cap geometry
  1.1% 10cm Above Cap geometry
  0.8% Marinelli beaker geometry
Not only low uncertainties but also arbitrary geometry of irradiated samples can be measured by HPGe with existing model
Chart: Energy [MeV]
| 5.9499999999999997E-2
Am-241 | -0.010778
Co-57 | 0.0017983 | 0.0085654
Sn-113 | 0.036665
Sr-85 | -0.022369
Cs-137 | 0.0099755
Y-88 | 0.0081456 | -0.020488
Co-60 | 0.022685 | 0.022186
 | 0 | 0
Chart: Energy [MeV]
| 5.9499999999999997E-2
Am-241 | 0.0085097
Co-57 | 0.01786 | -0.018039
Sn-113 | 0.02786
Cs-137 | 0.017854
Y-88 | -0.010372 | -0.010634
Co-60 | -0.0046766 | -0.0080281
 | 0 | 0
On Cap
10cm Above Cap
Chart: Energy [MeV]
| 5.9499999999999997E-2
Am-241 | 0.0044822
Cs-137 | -0.012805
Co-60 | -0.007247 | -0.0084622
 | 0 | 0
Marinelli beaker (Volume source)

## Slide 6
Gamma spectrometry stilbene
Chart: E [MeV]
Chart: E [MeV]
| 0.2 | 0.3 | 0.4 | 0.5 | 0.6 | 0.7 | 0.8 | 0.9 | 1 | 1.1000000000000001 | 1.2 | 1.3 | 1.4 | 1.5 | 1.6 | 1.7 | 1.8 | 1.9 | 2 | 2.1 | 2.2000000000000002 | 2.2999999999999998 | 2.4 | 2.5 | 2.6 | 2.7 | 2.8 | 2.9 | 3 | 3.1 | 3.2 | 3.3 | 3.4 | 3.5 | 3.6 | 3.7 | 3.8 | 3.9 | 4
Simulation | 0.020503 | 0.018066 | 0.016958 | 0.015936 | 0.015497 | 0.015449 | 0.01562 | 0.016321 | 0.018013 | 0.022306 | 0.019719 | 0.0077228 | 0.004375 | 0.0041393 | 0.004135 | 0.004451 | 0.0049623 | 0.0043874 | 0.0045235 | 0.0047617 | 0.0050209 | 0.0056229 | 0.006716 | 0.0072982 | 0.0044353 | 0.0012245 | 0.0001619 | 1.42e-05 | 4.1e-06 | 3.1e-06 | 2.9e-06 | 2.8e-06 | 3.1e-06 | 2.4e-06 | 2e-06 | 2.1e-06 | 5e-07 | 4e-07 | 0
Newly developed response matrix
Simulation uses precise probe parameters
  In gamma transport, surrounding materials are essential
Validation in AmBe + 24Na
Chart: Energy [MeV]

## Slide 7: 252Cf(s.f) TFGS spectrum measurement
First measurement in region 0.1 – 14 MeV
Uncertainties
  7 – 10 % in 1 – 7 MeV
  Below 20 % in 7 – 9 MeV
  Up to 90 % in 14 MeV
Consistent with previous results
  Between Stoddard and Trykov results
Czakoj, T. et al. Measurement of total fission gamma spectrum of 252Cf(s.f.). Eur. Phys. J. A 60, 228 (2024)

## Slide 8
Broomstick experiment
Kostal et al., Broomstick experiment with copper in VR-1 reactor, Annals of Nuclear Energy, Vol. 211, 2025, p. 110993
Transport of pinhole beam through broomstick
Integral quantities can usually be measured much more accurately than differential nuclear data, thus are useful to tuning nuclear data evaluations to improve integral performance.
The measured spectra are compared with calculation
The experiment was realized in VR-1 reactor

## Slide 9: Beam characterization
The spectrum in beam is similar to spectrum in channel in previous measurement
Spectra in output and measuring position are identical
    Flux decrease (factor 2.612 ) implies that beam is relatively not divergent
The beam is sharp (1% when moved by 35 mm corresponds to scatter from probe).
Chart: Energy [MeV]
Chart: Energy [MeV]
Misalignment [mm] | Rel. flux
0 (In axis) | 1.000
5 | 0.965
10 | 0.963
15 | 0.905
20 | 0.533
25 | 0.265
30 | 0.044
35 | 0.011

## Slide 10: Background determination
Room effect determined using shielding cylinder
  Iron + HDPE
Its magnitude is affected by aperture diameter
For blocks shorter than 20 cm Cu/Cr (attenuation ~ 1000) room effect is negligible
Chart: Energy (MeV)
Chart: Energy (MeV)
Room efect | 0.11728 | 0.11728 | 0.13434 | 0.13434 | 0.14722 | 0.14722 | 0.087334 | 0.087334 | 0.053894 | 0.053894 | 0.054524 | 0.054524 | 0.054966 | 0.054966 | 0.070691 | 0.070691 | 0.089762 | 0.089762 | 0.067211 | 0.067211 | 0.050157 | 0.050157 | 0.041169 | 0.041169 | 0.033686 | 0.033686 | 0.028497 | 0.028497 | 0.023999 | 0.023999 | 0.026025 | 0.026025 | 0.028176 | 0.028176 | 0.024972 | 0.024972 | 0.022049 | 0.022049 | 0.018772 | 0.018772 | 0.015902 | 0.015902 | 0.012265 | 0.012265 | 0.0093698 | 0.0093698 | 0.0091712 | 0.0091712 | 0.008962 | 0.008962 | 0.0096319 | 0.0096319 | 0.01035 | 0.01035 | 0.0081336 | 0.0081336 | 0.0063426 | 0.0063426 | 0.0083597 | 0.0083597

## Slide 11: Copper results
Chart: Energy [MeV]
 | 0 | 0
JENDL-5
Chart: Energy [MeV]
 | 0 | 0
Chart: Energy [MeV]
 | 0 | 0
JEFF-3.3
INDEN (used in ENDF/B-VIII.1.)
Low uncertainty experiment (beam transmission)
  Simple geometry
  Good source description
Discrepancies from simulation (if any) are on account of cross section evaluation
  JEFF-3.3 highly discrepant
  ENDF/B-VIII.1 GOOD (very similar to ENDF/B-VIII.0)
  JENDL-5 problematic

## Slide 12: Chromium results in new (2025) experiment
Comparison in ENDF/B-VIII.0
Systematic effects
  1 – 1.5 MeV
  1.5 – 4 MeV
Not so bad as 20 cm of chromium is very thick
However, improvement of ENDF/B-VIII.0 is needed for more precise predictions
Chart: Energy [MeV]
 | 0 | 0

## Slide 13: Comparison with various evaluations
Chart: Energy [MeV]
 | 0 | 0
Chart: Energy [MeV]
 | 0 | 0
JENDL-5
JEFF-3.3
Low uncertainty experiment (beam transmission)
  Simple geometry
  Good source description
Discrepancies from simulation (if any) are on account of cross section evaluation
  JEFF-3.3 highly discrepant
  ENDF/B-VIII.1 GOOD
  JENDL-5 problematic
Chart: Energy [MeV]
 | 0 | 0
INDEN (used in ENDF/B-VIII.1.)

## Slide 14: Leakage from copper cube
Leakage spectrum (1 - 10 MeV )
Copper cube evaluated
(>=99.95% Cu )
Support for benchmarks - 2 m above the lab.floor (as usually )
Cone 20cm Fe – 32cm PE
197Au(n,g)198Au
58Ni(n,p)58Co
93Nb(n,2n)92mNb
55Mn(n,g)56Mn
Reaction rates of :
100 cm from center
Background spectrum (room effect)
14

## Slide 15: Comparison of broomstick and leakage
Chart: Outgoing neutron energy (MeV)
Cu block 48 x 50 x 50 cm
Chart: Energy [MeV]
Broomstick – 15 cm Cu
Obtained results are in good consistence with previously measured neutron leakage from copper block
Chart: Energy [MeV]
In broomstick more effective attenuation

## Slide 16: Sensitivities
Chart: Energy [MeV]
Chart: Energy [MeV]
Broomstick is excellent accompanying experiment in cross section validation because sensitivities are different from case of leakage from material block
Chart: Energy [MeV]
Cu block
5cm broomstick
20cm broomstick

## Slide 17: New neutron leakage experiments
Tungsten 35 x 30 x 30 cm
PTFE block
60 × 50 × 50 cm
Support for benchmarks - 2 m above the lab.floor (as usually)
Cones = 32cm PE + 20cm Fe
Aluminium block
55 × 50 × 50 cm
17
252Cf in well defined cladding

## Slide 18: Mmeasurement of Al leakage flux
New approved ICSBEP evaluation
Neutron leakage spectra in 1 m, foils between plates
Stilbene detector 10x10 mm, HPD, In, Ni foils
Not high gamma background (good PSD discrimination)
discrimination in 28 channel ~ 0.86 MeV

## Slide 19: Room effect Al leakage
Experimentally evaluated (it is necessary)
High effect of thermal neutrons (low Al capture)
Horizontal view
Room effect evaluation
Vertical view
Chart: Channel
Chart: Energy [MeV]
Chart: Energy [MeV]

## Slide 20: Al leakage spectra
Chart: Energy [MeV]
Chart: Energy [MeV]
Underprediction in lower energies
Relativelly good agreement in 3 – 9 MeV

## Slide 21: Al leakage – reaction rates
Foils between plates
Nearly all foils are showing underprediction
  115In(n,n’) shows higher underprediction than 58Ni(n,p)
 |  | 115In(n,n') |  |  |  | 58Ni(n,p) |  |  | 
Plate position | Al thickness [cm] | ENDF/B-VIII.0 [%] | JEFF-3.3 [%] | JENDL-5 [%] | Unc. [%] | ENDF/B-VIII.0 [%] | JEFF-3.3 [%] | JENDL-5 [%] | Unc. [%]
6 | 1.18 | -2 | -2 | -2.3 | 3.9 | -9.4 | -9.4 | -9.6 | 12.2
7 | 6.12 | -8.7 | -8.7 | -7.1 | 2.5 | -7.2 | -7.2 | -6.5 | 4.3
8 | 11.06 | -12.2 | -12.2 | -8.2 | 2.5 | -8.7 | -8.4 | -6.6 | 2.9
9 | 16.01 | -12.6 | -12.6 | -6.2 | 2.8 | -11.9 | -11.5 | -10 | 2.6
10 | 20.95 | -18.3 | -18.3 | -10.2 | 2.8 | -8 | -8 | -2.7 | 2.4
11 | 25.91 | -16.9 | -16.9 | -6.8 | 3.5 |  |  |  | 
Chart: Energy [MeV]

## Slide 22: Measurement of W leakage flux
Ongoing experiments (96% W, 3% Ni, 1% Fe )
Neutron leakage spectra in 1 m, In foils between plates
Stilbene detector 10x10 mm, HPD, In foils on block
Not high gamma background (good PSD discrimination)
discrimination in 15 channel ~ 0.6 MeV

## Slide 23: Measurement of W leakage flux
Ongoing experiments (96% W, 3% Ni, 1% Fe )
Neutron leakage spectra in 1 m, In foils between plates
Stilbene detector 10x10 mm in 1m, In foils on block
Not high gamma background (good PSD discrimination)
Ongoing experiments – preliminary results
Chart: Energy [MeV]
Chart: Energy [MeV]
 | Front part (16.2 cm W) | Side part (13.7cm W)
Experimental RR | 4.76E-30 | 1.01E-29
C/E-1 |  | 
ENDF/B-VIII | -15.0% | -11.9%
JEFF-3.3 | 10.9% | 9.9%
JENDL-5 | -8.1% | -6.2%

## Slide 24: W Broomstick
15cm of W in VR-1 beam
Preliminary experiments
Stilbene detector 10x10 mm
Ongoing experiments – preliminary results
Chart: Energy [MeV]
Chart: Energy [MeV]
 | 0 | 0

## Slide 25: Measurement of PTFE leakage flux
New approved ICSBEP evaluation
Neutron leakage spectra in 1 m, foils between plates
Stilbene detector 10x10 mm, HPD, In, Ni foils
Lowergamma background (good PSD discrimination)
discrimination in 34 channel ~ 0.99 MeV
Horizontal view
Room effect evaluation
Vertical view
Chart: Channel
Czakoj et al., Comprehensive validation of fluorine cross-sections, Ann. of Nucl. En., Vol. 218, 2025, P.111426

## Slide 26: C/E comparison of measured spectra
Chart: Energy [MeV]
Chart: Energy [MeV]
Best agreement in case of INDEN (ENDF/B-VIII.1.) however still some discrepancies are notable in region below 2 MeV
Czakoj et al., Comprehensive validation of fluorine cross-sections, Ann. of Nucl. En., Vol. 218, 2025, P.111426

## Slide 27: Foil results
Placement on plate No. back side | C2F4 thickness [cm] | ENDF/B-VIII.0 | INDEN | JEFF-3.3 | JENDL-5 | ur [%]
6 | 1.40 | 4.4 | 2.0 | 4.4 | 2.2 | 3.9
7 | 6.82 | -4.8 | -4.8 | -4.8 | -7.5 | 3.0
8 | 12.28 | -5.2 | -1.8 | -5.3 | -7.5 | 3.1
9 | 17.68 | -14.4 | -8.1 | -14.5 | -15.9 | 4.4
10 | 23.09 | -24.6 | -16.3 | -24.6 | -25.0 | 7.5
11 | 28.48 | -26.7 | -14.7 | -26.8 | -25.1 | 5.5
Placement on plate No. back side | C2F4 thickness [cm] | ENDF/B-VIII.0 | INDEN | JEFF-3.3 | JENDL-5 | ur [%]
6 | 1.40 | 3.1 | 2.1 | 3.1 | 1.8 | 9.0
7 | 6.82 | -2.0 | -1.7 | -2.1 | -3.3 | 3.4
8 | 12.28 | -5.6 | -2.9 | -5.6 | -5.7 | 2.9
9 | 17.68 | -7.8 | -3.0 | -7.8 | -6.6 | 3.3
10 | 23.09 | -12.3 | -5.5 | -12.3 | -9.6 | 3.2
11 | 28.48 | -9.8 | 0.5 | -9.8 | -4.0 | 3.5
Placement on plate No. back side | C2F4 thickness [cm] | ENDF/B-VIII.0 | INDEN | JEFF-3.3 | JENDL-5 | ur [%]
10 | 23.09 | -3.8 | -2.6 | -4.4 | 17.0 | 17.8
Indium 115In(n,n’)
Nickel 58Ni(n,p)
Gold 197Au(n,2n)
Chart: Energy [MeV]
Independent monitors of neutron flux
Even high flux monitored 5g Au foil, 2 month activation, 5d measurement => NPA ~ 1200 cts

## Slide 28: AKR-2 experiment
discrimination in 41 channel ~ 1.1 MeV

## Slide 29: AKR-2 spectra
Chart: Channel
Chart: Energy [MeV]
Large beam diameter ~ D=12 cm in this experiment
Due to geometry (holding table) + beam diameter … notable background ..
In this large beam diameter also elastic/inelastic play role . . . (but not so high as in leakage experiments)

## Slide 30: C/E of measured spectra
Chart: Energy [MeV]
Chart: Energy [MeV]
Above 2 MeV good agreement below discrepancies similarly as in californium experiment
Most likely issue in 19F total cross section below 2 MeV
Chart: Energy [MeV]

## Slide 31: Quasi monoergetic field validation
Formed from 7Li(p,n) reaction
Spectra measurement
  Deconvolution
  TOF
Simultaneous activation
Eprotons | E50% [MeV] | JEFF-3.3 | JENDL-4 | ENDF/B-VIII | Unc.
12.4 MeV | 10.89 | -20.9% | -10.6% | -18.1% | 3.7%
14.4 MeV | 12.57 | -7.7% | 2.5% | -10.2% | 6.6%
Matej et al., Rad. Phys. and Chem., 184 (2021) 109475
58Ni(n,x)57Co validation in quasi monoenergetic field

## Slide 32: Quasi monoenergetic field
2
1
3
Need of experimental characterization
The calculation don’t agree with measured spectra (while TOF and deconvolution)
Background effect
Clasical estimation by room effect using cones
Material and geometrical correction
It is reflection of fact, that spectra is measured in position diffrerent from foils

## Slide 33: Graphite leakage flux using DT gen
Measurement using DT generator and graphite cylinder
Graphite cylinder 60x60 cm, central cavity 17 cm dia.
Stilbene detector 10x10 mm
Calculation in various libraries in progress
Results and calculations will be published soon
Chart: Energy [MeV]

## Slide 34: Prompt gamma measurement
  Measurement of leakage gammas with HPGe and stilbene detectors
  Ideal geometry, because Cf inside is standard
  Due to water solvent – good moderation
  SINBAD benchmarking
Chart: E [keV]
Chart: E [MeV]
Energy range | Cl | Fe
0 - 1 eV | 97.738% | 99.404%
1 eV - 0.1 keV | 2.121% | 0.503%
0.1 keV - 10 keV | 0.134% | 0.053%
10 keV - 20 MeV | 0.007% | 0.039%

## Slide 35: Gamma spectrum measurement in TRIGA
Not as good resolution as in HPGe, but still valuable results
Gamma spectrum above water
Gamma spectrum measurement of activated water (KATANA)
Chart: Energy [MeV]
Chart: Energy [MeV]

## Slide 36: Gamma in various reactors
High energy gamma as important portion of gamma fields
Above 11 MeV gamma has similar shape with 235U PFGS
Over 13 MeV experiment is below evaluated PFGS
Chart: Energy [MeV]
VR-1 (dlouhe) | 2.5201e-06 | 2.1937e-06 | 1.9184e-06 | 1.7068e-06 | 1.5373e-06 | 1.4006e-06 | 1.3027e-06 | 1.2065e-06 | 1.1294e-06 | 1.0571e-06 | 9.909e-07 | 9.2098e-07 | 8.5837e-07 | 8.0249e-07 | 7.5032e-07 | 7.0519e-07 | 6.5481e-07 | 6.1071e-07 | 5.5924e-07 | 5.1292e-07 | 4.7092e-07 | 4.3245e-07 | 4.0416e-07 | 3.828e-07 | 3.6927e-07 | 3.6672e-07

## Slide 37: Epithermal dosimetry
Schulc et al., Appl. Rad. and Isot. 215, (2025), 111586
Planned measurements with B4C (10B) filters (JSI collaboration), spring 2025
In 2023 preliminary experiment with natural boron capsule (nearly equivalent to JSI one) ~ 2.364 g/cm3 instead of JSI 2.36 g/cm3
Kostal et al., Appl. Rad. and Isot. 169 (2021) 109566
 | Poured | Sintered
Density [g/cm3] | 1.197 | 2.36
Thickness [mm] | 7.9 | 4
55Mn(n,g) [s-1] | 3.67E-29 | 3.75E-29

## Slide 38: Conclusions
Broomstick experiment realized at the VR-1 and it seems excellent tool for total cross section testing
There is a strong potential of AKR-2 for broomstick – discussion about use of C2Cl4, Zr in future experiments is planned
The Cf benchmark evaluations of Teflon and Aluminum leakage were approved to ICSBEP
The stilbene gamma spectrometry is promising tool.
The new experiments realized in LR-0 reference field. The new benchmarking is ongoing …

## Slide 39: Thank you for attention
Michal Kostal
Michal.Kostal@cvrez.cz

## Slide 40: Acknowledgements
The results were obtained using the CICRR infrastructure, financially supported by the Ministry of Education, Youth and Sports - project LM2023041 and by the European Union under grant agreement No 101061142.