## Slide 1: Recent updates to the evaluated nuclear data files of structural materials
Andrej Trkov, Jožef Stefan Institute, Ljubljana, Slovenia
(on behalf of the INDEN Collaboration)

## Slide 2: Background
ENDF/B-VIII.1 Library has been released
JEFF-4.0 Library is about to be released
Extensive benchmarking of the libraries has been done
The need for covariance information was expressed by the fusion community
Question:
  Can we take advantage of the improved evaluations?
  Focus on Fe, Cu, Cr, Si isotopes

## Slide 3: Iron isotopes
The neutron emission spectra at high energies agree well with measured data.
However, some problems were identified:
  Excessive spectrum contribution is observed at low energies in integral experiments (observed by B. Jansky).
  The low-energy tail of neutron emission spectra do not go to zero (pointed out by S. Kwon, e.g. Fe-56(n,2n). With 14 MeV neutrons incident on thin slabs the spectra at lower energies are affected).
  Other minor corrections were done in the evaluations for consistency.
Recommendation
  Adopt JEFF-4t5, which includes all corrections for all isotopes from the INDEN contribution

## Slide 4: Neutron emission spectra

## Slide 5: Issues with neutron leakage in Fe CIELO

## Slide 6: Iron isotopes – Validation (presentation by S. Kwon) KwonCapote)

## Slide 7: Iron isotopes - Validation

## Slide 8: Copper isotopes
Significant improvements to Cu-63 and Cu-65 were made
The key point for validation is the bulk transmission experiment from Rez
Improvements to both isotopes are included in ENDF/B-VIII.1:
  New resolved resonance parameters, including MF32
  Improved elastic angular distributions in the energy range 1.0-2.5 MeV
  Interpolation flags in MF6/MT5 switched to 22
  Minor corrections for consistency
  Improvements show the elimination of 800pcm bias in new CERBERUS critical experiment (hmf106)
In addition (INDEN contribution):
  Addition of covariances from JEFF-3.3 above the resonance range
Recommendation:
  Adopt ENDF/B-VIII.1 with addition of covariances by INDEN

## Slide 9: RPI quasi-differential experiment (2021)
Y. Danon, ENDF/B-VIII.1 paper (submitted)
Copper isotopes - Validation

## Slide 10
Cu isotopes, ORNL/IAEA/JSI
Cu cube, neutron leakage (Rez, CZ)
Schulc et al, Rad.Phys.Chem. 2021
n,
discr.
nds.iaea.org/INDEN/data/ALARM-CF-CU-SHIELD-001
INDEN-2024 (B81)
ENDF/B-VIII.0
Copper isotopes - Validation

## Slide 11: Copper Isotopes Validation (Rez cube)

## Slide 12: Fast neutron benchmarks - Cu

## Slide 13: Oktavian shielding 14 MeV benchmark
INDEN latest
shows excellent
fusion performance

## Slide 15: New Cu benchmark (CERBERUS)
INDEN Cu (B81) improved ENDF/B-VIII.0 by -800pcm

## Slide 16: CERBERUS (HMF106) Benchmark

## Slide 17: Copper isotopes – Bulk Criticality Validation

## Slide 18: Copper isotopes - Validation
Zeus
CURIE

## Slide 19: Copper Isotopes Validation - Comments
Insertion of Cu from ENDF/B-VIII.1 significantly reduces the Chi^2/DoF
Certain benchmark sets remain strongly discrepant, but these are most likely NOT related to copper data (e.g. CURIE benchmarks with a copper reflector are sensitive to fluorine in teflon)

## Slide 20: Conclusions - Cu
Chart: 
INDEN 2024 file performs well both in shielding and criticality experiments.
natCu(n,el) angular distributions reviewed vs existing experimental data up to 15 MeV: Popov 86 data below 300 keV consistent with evaluation
Excellent performance achieved, much better than ENDF/B-VIII.0 (do not harm). New Cu evaluations adopted by ENDF/B-VIII.1 and proposed for JEFF-4.
New experiment CERBERUS shows big improvement with new INDEN EVAL
INDEN files available from https://nds.iaea.org/INDEN

## Slide 21: Silicon Isotopes
Status
  The comments in ENDF/B-VIII.1 are more descriptive.
  The (n,p) cross sections in INDEN “iaea_E" are higher by more than 20 % compared to ENDF/B-VIII.1.
  The change in the (n,p) cross section is propagated to the non-elastic cross section.
  The ENDF/B-VIII.1 (n,p) reaction agrees with IRDFF-II.
  The elastic cross sections in INDEN "iaea_E" are lower to preserve the total.
  Deuteron emission spectra were added in ENDF/B-VIII.1.
  Some changes in the energy grid of the double-differential cross sections were done in ENDF/B-VIII.1
  The JEFF-4t4 file is equal to INDEN "iaea_E".
  Cross sections in ENDF/B-VIII.1 have a big impact on criticality, especially in
Recommendation:
  Adopt ENDF/B-VIII.1 for all isotopes

## Slide 23: Silicon Isotope validation

## Slide 24: Fluorine
Status
  Poor performance in criticality benchmarks, particularly in assemblies containing Teflon
  Poor performance in shielding benchmarks

## Slide 25: Morgan 76 data adopted << Broder data
By using Morgan derived INL data (nng x 4pi)
F-19(n,inl) reduced by ~40% from 300 keV
B8 & JENDL-5
followed Broder
with REF Fe !

## Slide 26
Teflon neutron leakage (HPD) - NEW
(JEFF4t5)
(JEFF4t5)

## Slide 27
Teflon neutron leakage (stilbene) - NEW
Neutron leakage drop below 2 MeV
confirmed in broomstick experiments
(JEFF4t5)

## Slide 28
Larson x 0.92
F-19: (n,tot) below 2 MeV
All evaluations based on Larson 76 data
Larson 76 x 0.92
consistent !! with Foster Jr 71
& Abfalterer 2000

## Slide 29
hmf007
cases 32-34
New 19F Criticality impact  -400pcm
hmi011
(CURIE)
New INDEN F19 shows poor performance for JEFF-4t5

## Slide 30
Chart: 
Conclusions – F-19
A new full evaluation using Morgan/Dickens inelastic data and Elwyn elastic DA data needed
ENDF/B-VIII.1 (INDEN) dramatically improved the performance
Neutron leakage experiments showed a ND deficiency below 2 MeV (post – ENDF/B-VIII.1)
A possible problem with Larson 76 total cross section data
Larson rescaled by 0.92 to match Abfalterer 2000 and Foster Jr 71 data
Neutron leakage improved below 2 MeV
ICSBEP benchmark agreement for hmi011 & hmf007/32-34 improved
(about -400 pcm impact !!!)
INDEN files available from https://nds.iaea.org/INDEN

## Slide 31: Chromium Isotopes
Status
  Overall, there is more to be desired !
  MACS of Cr-50,53 are too high
  New resonance analysis is needed
  There are no consistent covariance data available
  Trial patches partly improve the performance but are not sufficient

## Slide 32: Thank you for your attention

## Slide 33: Additional slides

## Slide 34: Chromium isotopes: Cr-50
Status
  The Cr-50 evaluation in JEFF-4t4 is equal to ENDF/B-VIII.1; neither of them includes covariances. Version “cr50v234” is the latest from INDEN and includes covariances. It differs from JEFF-4t4, particularly in the fluctuations above the RRR, which were adopted from the ENDF/B-VIII.0 evaluation.
  The MACS of Cr-50 is too high (measured by ToF). The chromium isotopes would need a thorough re-evaluation.
  The original file recommended by INDEN had no covariances; no covariance information is included in ENDF/B-VIII.0.
  ENDF/B-VIIIb3 contains Comarra covariances from ENDF/B-VII.1 inserted by Sam Hoblit. The files include MF32.
Recommendation
  Adopt INDEN version 2.3.4 on the INDEN web page

## Slide 35: Chromium isotopes: Cr-52
Status
  Cross sections of Cr-52 in JEFF-4t4 are equal to ENDF/B-VIII.1 library, but JEFF-4t4 does not include covariances.
  INDEN versions were tested up to "v234f", but the decision was to stick to "v234c".
  Version “v234c” is numerically equal to JEFF-4t4, except that the latter includes a corrected Q-value for (n,p). Neither of them include covariances. In v234c the covariances were omitted by accident. The ENDF/B-VIII.1 evaluation includes covariances, but requires a correction for the (n,p) Q-value. The corrected file is “cr52e81c.endf”.
Recommendation
  Adopt “cr52e81c” as on the INDEN web page.

## Slide 36: Chromium isotopes: Cr-53
Status
  Cross sections in ENDF/B-VIII.1 are the same as those in JEFF-4t4, but the latter has no covariances. In the INDEN version "v234" the fluctuating total was restored from "e80" and the elastic corrected to preserve unitarity.
  ENDF/B-VIII.1b3 contains Comarra covariances from ENDF/B-VII.1 inserted by Sam Hoblit. The files include MF32.
  Spurious covariances in MF33/MT22 with no corresponding entry in MF3 were removed. The corrected file is “cr53v234s” on the INDEN web page.
  The MACS of Cr-53 is too high (measured by ToF). The chromium isotopes would need a thorough re-evaluation.
Recommendation
  Adopt “cr53v234s” on the INDEN web page until a better evaluation is available.

## Slide 37: Chromium isotopes: Cr-54
Status:
  Version "v234" is equal to ENDF/B-VIII.1 but differs from JEFF-4t4, which does not have the fluctuations above the RRR. None of these files include covariance information, except for the resonance parameters in MF32 in ENDF/B-VIII.1.
  There are covariances in JEFF-3.3, which could be used to patch the Cr-54.
Recommendation
  Cr-54 is the least abundant isotope, so it is probably sufficient to adopt version “cr54v234” from the INDEN web page.

## Slide 38: Chromium isotopes (summary)
The MACS of Cr-50,53 are too high (measured by ToF). The chromium isotopes would need a thorough re-evaluation
The original file recommended by INDEN had no covariances
No covariance information is included in ENDF/B-VIII.0
ENDF/B-VIIIb3 contains Comarra covariances from ENDF/B-VII.1 inserted by Sam Hoblit. The files include MF32.