## Slide 1: Behaviour of Bundles with Cr and Cr/CrN Coated Zirconium Alloy Cladding under Simulating Design Extension Conditions at the DEGREE Facility
Technical Meeting on Advanced Technology Fuels: Progress on their Design, Manufacturing, Experimentation,
Irradiation, and Case Studies for their Industrialization, Safety Evaluation, and Future Prospects
28 - 31 October 2025
IAEA Headquater, Vienna, Austria
Kinya Nakamura, Kenta Inagaki
Juri Stuckert
Martin Ševeček
CRIEPI
KIT
CTU

## Slide 2
  1. Motivation
  2. Contribution to CRP ATF-TS
      A series of SINGLE ROD tests under DEC
      A series of BUNDLE tests under DEC
3. Comparison of degradation behavior
    Specifications of coated Zr-based cladding
    Single rod vs Bundle
4. Conclusions
Outline

## Slide 3
Motivation
3
*1 M. Steinbrück, et al., JNM 559 (2022) 153470.
FeCrAl | Coated Zr-based alloy |  | 
QUECH-19 (2018) | OECD NEA QUENCH-ATF (2021-2026) | IAEA CRP ATF-TS (2021-2024) | EU OFFERR CODEX-ATF-AIT (2024-2025)
First ATF bundle test @QUENCH Ref. QUENCH-15 | Three bundle tests under extended DBA and DEC @QUENCH | Bundle tests and simulation @CODEX and DEGREE | Bundle tests under air @CODEX Ref. CODEX-AIT-3
International Research Projects on ATF Bundle Behaviors under DEC
To improve safety, economics, and reliability of LWRs, long-cycle reactor operation is being promoted by combining HBU, IE, and ATFs.
Full-core accident tolerance requires a combination of AT fuel & components such as CR, CB, and GS.
Validation of the accident behavior model in the SA analysis code requires test data of the fuel bundles composed of core structural materials under adiabatic accident conditions.
Potential more intense temperature runaway has been pointed out in fuel bundle systems. *1
To address these issues, including the still lack of knowledge on degradation behavior, an international collaborative research projects on ATF bundle behavior under DEC is being carried out.

## Slide 4
  Significance of Bundle Test in Accident Conditions
Challenges
Reproducibility of degradation behavior and real-time data acquisition using a high-precision-manufactured ATF test bundle under high-temperature and high-pressure thermal-hydraulic conditions
International standardization of test methods and evaluation criteria
Advantages
To provide validation data for SA analysis codes, which can predict degradation behavior taking into account interactions between fuel rods, CR, CB, and GS
Performance evaluation of FA under accident conditions and feedback to FA design and operation guidelines
Technical basis for regulatory authorities and utilities for safety assessment and licensing

## Slide 5
  Contribution to CRP ATF-TS from CRIEPI
    A series of SINGLE ROD tests (WT1.1)
    Different types of coating material, its thickness, and cladding substrates
    Heated to 1350-1600˚C
    A series of BUNDLE tests (WT1.2)
      Different types of coating material
      Heated to 1350-1500˚C
      WT2.1 : Benchmark exercise for the DEGREE S3 test
      WT2.2 : Benchmark exercise for the DEGREE B3 test
    To improve knowledge of the degradation behavior of bundles with unirradiated coated Zr-based cladding materials

## Slide 6
10µm
16µm Cr
10µm CrN
Zry-4
10µm
20µm Cr
Zry-4
Cross-Sectional Microstructure
      No pre-oxidation
      No pre-hydrogenation
Test Rod with Coated Zr-based Cladding
Coated Zr-based alloy cladding
Tungsten rod as susceptor
Annular pellet, Al2O3 (1350˚C)
ZrO2 (1500-1600˚C)
Coated Zr-based alloy cladding
Grid Spacer, Al2O3
End plug
Pressure gauge
Max. Temperature level
Grid spacer, Al2O3
Gas plenum (He, about 10 cc)
Structure of the Test Rod
Coated Cladding
Item | Zircaloy-4 | Opt. ZIRLO | E110
OD / Thickness (mm) | 10.75 / 0.725 | 9.13 / 0.65 | 9.15 / 0.70
Length (mm) | 225 | 225 | 225
Coating material and its thickness (provider) | 10 µm Cr (KIT) 20 µm Cr (CTU) | 20 µm Cr (CTU) | 
 | 26 µm Cr/CrN double-layer (CTU) |  | 6 µm Cr/CrN multi-layer (AEOI)
Coating method | PVD | PVD | PVD
KIT : Karlsruhe Institute of Technology
CTU : Czech Technical University in Prague
AEOI: Atomic Energy Organization of Iran
225 mm
20 µm Cr (CTU)
26 µm Cr/CrN double-layer (CTU)

## Slide 7
K. Nakamura, K. Inagaki, Proc. TOP FUEL 2021, Santander, Spain, Oct. 24-28, 2021.
Test Scenario
Bundle Test Facility (DEGREE)
Induction power output (controlled)
＜600˚C
Cooling
Heat-up
Conditioning
Pre-heating
Temperature and power output
Steam 0.4 g/s
Ar 2 L/min
Ar 10 L/min
Time
Flow rate
1350 to 1600˚C
2-5˚C/s
Furnace cooling without water quenching
He
Induction coil
Mass Spectrometry
Exhaust
Water tank
Condenser
Boiler
Ar
Heater
MFC
MFC
Mass Flow Controller
Reactor vessel
Pressure gauge
Thermal insulator
(Al2O3, ZrO2)
Quartz tube
Test bundle
Bundle
Test Rod
Single Rod
2
9
6
3
4
5
8
7
1
Heater Rod
The low-insulation DEGREE facility, applying induction heating technology, allows single rod and bundle testing under DEC.
Experimental Setup

## Slide 8
Test Matrix
Single Rod | S1 | S2 | S3 | S4 | S5 | S6
Cladding materials | Zircaloy-4 |  |  |  |  | 
Coating materials | Uncoated | 10 µm Cr | 20 µm Cr | 26 µm Cr/CrN | 10 µm Cr | 20 µm Cr
Max. temperature | 1350 ˚C |  |  |  | 1600 ˚C | 
Rod inter. Pressure | 6 MPa |  |  |  |  | 
Single Rod | S8 | S9 | S10 | S11 | S12 | S13
Cladding materials | Opt. ZIRLO |  |  | E110 |  | 
Coating materials | Uncoated | 20 µm Cr | 20 µm Cr | 6 μm Cr/CrN multi-layer |  | Uncoated
Max. temperature | 1350 ˚C |  | 1500 ˚C | 1350 ˚C | 1500 ˚C | 1350 ˚C
Rod inter. Pressure | 6 MPa |  | 0.1 MPa | 6 MPa | 0.1 MPa | 6 MPa
Bundle | B1 | B2 | B3 | B5 | B6 | B7
Cladding materials | Zircaloy-4 |  |  |  |  | 
Coating materials | Uncoated | 10 µm Cr | 20 µm Cr | 20 µm Cr | 26 µm Cr/CrN | 20 µm Cr
Max. temperature | 1350 ˚C |  |  |  |  | 1500 ˚C
Rod inter. pressure | 6 MPa | 0.1 MPa | 6 MPa | Two rods with 6 MPa & the rest with 0.1 MPa |  | 
      Fuel pitch: 14.5 mm for Zry-4 and 12.6 mm for OZ & E110

## Slide 9
  Comparison of Degradation Behavior
  Microstructure Heated to 1350˚C
Cr coating Formation of ZrCr2 at the α-Zr(O)/β-Zr interface and disappearance of Cr layer
Cr/CrN coating No formation of ZrCr2 and remaining both Cr and CrN layers
Observation Region
Circumferential cross sections
0 - 6 mm above burst opening
  Zircaloy-4
  E110
20 µm Cr (S3)
6 µm Cr/CrN (S11)
along the burst side
90 degree circumferential direction from the burst
Cr
Zr
O
BSE
along the burst side
26 µm Cr/CrN (S4)
Cr
Zr
O
N
Cr
Zr
O
N
ZrO2
90 degree circumferential direction from the burst
  Opt. ZIRLO
20 µm Cr (S9)
Cr
Zr
O
BSE
Zr(Cr,Fe)2
Zr(Cr,Fe)2
Cr2O3
Cr
ZrO2
Cr2O3
Single Rod
Suggest that Inner CrN layer suppresses Cr & O inward diffusion and Zr outward diffusion
  Zircaloy-4

## Slide 10
  Comparison of Degradation Behavior
  Microstructure Heated to 1500˚C or 1600˚C
100 µm
Upward
External
ZrO2-x
Cr2O3/Cr
Invisible due to high contrast
LiquidZrCr2+ β-Zr
438～261 HV
728 HV
391 HV
435 HV
α-Zr(O)
prior β-Zr
Cr diffusion zone
Cr/Cr2O3
ZrO2-x
Sn-rich region
100 µm
Cr diffusion zone
prior β-Zr
Invisible due to high contrast
α-Zr(O)
Upward
External
  Zircaloy-4
  (RIP = 6 MPa, 1600˚C)
  Opt. ZIRLO
  (RIP = 0.1 MPa, 1500˚C)
  E110
  (RIP = 0.1 MPa, 1500˚C)
20 µm Cr (S6)
10 µm Cr (S5)
6 µm Cr/CrN (S12)
20 µm Cr (S10)
100 µm
Upward
External
100 µm
Upward
External
Negligible inward diffusion of Cr & O leading to no formation of Cr diffusion zone
Localized large strain due to formation of Cr-diffusion zone and liquefaction at the α-Zr(O)/prior β-Zr interface regardless of RIP
Significant inward diffusion of Cr & O and outward diffusion of Zr resulting in formation of interdiffusion structures including Cr-Zr eutectic melt
Increasing trend of microhardness in the outward direction ( in BSE image of S6)
Observation Region
longitudinal cross sections
24 mm above the burst
prior β-Zr
Cr diffusion zone
α-Zr(O)
ZrO2-x
Cr2O3/Cr
prior β-Zr
Single Rod

## Slide 11
  Comparison of Degradation Behavior
  Microstructure of Multi-layer Cr/CrN Coated E110
Observation Region
  Burst level
  90 degrees circumferentially from the burst opening
  1350˚C
  RIP 6 MPa (S11)
  1500˚C
  RIP 0.1 MPa (S12)
  Initially, 20 nm each of Cr and CrN alternately deposited to form a multi-layer Cr/CrN with a total 6 μm
  Transformed into another three layers: Cr2O3/CrN/Cr below 1350˚C
  The CrN layer, which is likely to retard the inward diffusion of oxygen, reduces in thickness at HT to form Cr metal.
  Parts of nitrogen diffuses inward to form nitrogen/oxygen-stabilized α-Zr(N,O), which is likely to retard the inward diffusion of Cr and the outward diffusion of Zr.
Cr2O3
Cr2O3
Cr metal
CrN
α-Zr(N,O)
Prior β-Zr
CrN
Nitrogen band
α-Zr(N,O)
α-Zr(N,O) to α-Zr(O) inward
Cr2O3
Cr2O3
Prior β-Zr
Cr metal
CrN
α-Zr(N,O)
Nitrogen band
CrN
CrN
Single Rod

## Slide 12
Vertical Distribution of Hydrogen Concentration Absorbed in the Cladding
Radial Distribution of Hydrogen Concentration at 24 mm above the Burst Opening (S6)
obtained by ToF-SIMS
  Comparison of Degradation Behavior
  Hydrogen Concentration Distribution in Cladding
Hydrogen concentrates in the Cr diffusion zone and in the α-Zr layer that has transformed from the prior β-Zr layer.
Single Rod
Distance from the burst opening (mm)
Hydrogen concentration (ppm)

## Slide 13
Comparison of Degradation Behavior
3×3 Bundle Tests
Identical test conditions for bundle tests B5, B6, and B7
  Pressurized/non-pressurized fuel rod layout
  12 Thermocouple mounting positions (8 R-type and 4 K-type)
  Tmax 1350 or 1500˚C
2
9
6
3
4
5
8
7
1
RIP 6 MPa No. 4 and No.8
RIP 0.1 MPa others
Bundle
Time history of the B6 test (Cr/CrN coated Zry-4, Tmax 1350˚C )
Layout of Bundle

## Slide 14
Comparison of Degradation Behavior
Overview of Post-Tested Bundle
B5
20µm Cr
1350˚C
B7
20µm Cr
1500˚C
B6
Cr/CrN
1350˚C
B7
B6
B5
4
8
1
3
2
7
6
5
9
Pressurized Rods
Bundle

## Slide 15
Pressurized Rods (No. 4, RIP 6 MPa)
Unpressurized Rods (No. 9, RIP 0.1 MPa)
Cr2O3
Comparison of Degradation Behavior
Cross Section at Burst Level
B5
B6
B7
ZrO2 layers connected in the circumferential direction
ZrO2
Cracking of Cr2O3/Cr layer
Large hoop strain
Large hoop strain
Relatively large hoop strain
Next slide
prior β-Zr
prior β-Zr
prior β-Zr
prior β-Zr
prior β-Zr
prior β-Zr
ZrO2
ZrO2
Cracking of Cr2O3/Cr layer
Cracking of Cr2O3/Cr layer
α-Zｒ(O)
Cr diffusion zone
(Liquid at HT)
Cr2O3
Cr diffusion zone (Liquid at HT)
α-Zｒ(O)
ZrO2
ZrO2
α-Zｒ(O)
Prior β-Zr
ZrCr2
α-Zｒ(O)
void
α-Zｒ(O)
α-Zｒ(O)
Cr
B5
20µm Cr
1350˚C
B7
20µm Cr
1500˚C
B6
Cr/CrN
1350˚C
Bundle

## Slide 16
Comparison of Degradation Behavior
Cross Section of Double-Layer Cr/CrN Coated Zry-4, 1350˚C
Cr2(O,N)3
Cr
CrN
α-Zr(N,O) to
α-Zr(O,N) inward
Cr
prior β-Zr (substrate)
Nitrogen band
Cr2(O,N) 3
Oxygen band
BSE Image
Elemental Map
The double-layer Cr/CrN was transformed into a four-layer structure Cr2O3/Cr/CrN/Cr.
The CrN layer was thinned from the original 10 µm to 4 µm.
Formation of nitrogen-dissolved layers: likely Cr2(O,N)3 outward and α-Zr(N,O) inward.
These layers appears to suppress the inward diffusion of Cr and O, and the outward diffusion of Zr.
Similar microstructures are seen in the region at least 18 mm above the burst level.
Expected properties of double-layer and multi-layer Cr/CrN coatings
  Suppressing circumferential strain,
  Reducing the oxidation kinetics, and
  Retarding liquefaction due to the Cr-Zr eutectic.
CrN
Central Rod No. 9 at Burst Level (B6)
O
Cr
Zr
N
Bundle

## Slide 17
Comparison of Degradation Behavior
Single Rod vs Bundle
Burst Temp. and Hoop Strain
E110
OZ
Zircaloy-4
Zircaloy-4
10 µm Cr
10 µm Cr
20 µm Cr
20 µm Cr
20 µm Cr
Cr/CrN
Cr/CrN
uncoated
uncoated
uncoated
20 µm Cr
20 µm Cr
20 µm Cr
20 µm Cr
Cr/CrN
Cr/CrN
E110
OZ
Zircaloy-4
Zircaloy-4
10 µm Cr
10 µm Cr
20 µm Cr
20 µm Cr
20 µm Cr
Cr/CrN
Cr/CrN
uncoated
uncoated
uncoated
20 µm Cr
20 µm Cr
20 µm Cr
20 µm Cr
Cr/CrN
Cr/CrN
2
9
6
3
4
5
8
7
1
Burst Opening Size
Bundle
Single Rod
Bundle
Single Rod
Bundle
Single Rod

## Slide 18
  Conclusions
  In the IAEA CRP ATF-TS, series of single rod and bundle tests were successfully carried out using the DEGREE facility, where three types of fuel claddings coated with Cr or Cr/CrN, were heated up to 1600˚C in a steam-Ar mixed atmosphere under simulated DEC.
  The interdiffusion layer structure formed at the interface between coating and Zr alloy substrate, the radial and vertical redistribution of the constituent elements, the radial profile of the microhardness, and the ballooning and bursting behaviour were clarified.
  The accident behaviours of the different coating materials, their thicknesses, and cladding substrates, as well as between single rod and bundle tests, were also discussed.
For the Cr coating, the Cr2O3 diffusion barrier effect is deteriorated at high temperatures due to cracking in the coating layer, interdiffusion of the components, liquefaction due to Cr/Zr eutectic etc.
For the Cr/CrN coating, regardless of whether it was a double- or multi-layer, the hoop strain was relatively small, and the CrN layer might suppress the interdiffusion of the components, and the diffusion barrier effect was likely to be improved at high temperatures compared with the Cr coating.
Some experimental data were provided for benchmark exercise and uploaded to the ‘IAEA Fuel and Materials Database’.
No temperature runaway was observed under the DEGREE’s low-insulation conditions.

## Slide 19
Expansion of ATF Bundle Test Data under DEC Based on Internationally Standardized Test Methods and Evaluation Criteria
    Reproducibility and repeatability
    High-precision-manufactured ATF test bundle
    Acquisition of lots of experimental data in real time under high-temperature and high-pressure thermal-hydraulic conditions
    Universal test data independent of test equipment
    Limitations of simulating real accident environmental conditions
Improvement of SA analysis code through benchmarking exercises using new or existing ATF bundle test data
19
  Outlook for Future CRP on ATF

## Slide 20
Thank you for your attention!
Acknowledgment