## Slide 1: INTEGRAL TESTING OF ATF FUEL UNDER HIGH TEMPERATURE ACCIDENT CONDITIONS IN THE CODEX FACILITY Zoltán Hózer, Róbert Farkas, Nóra Vér, Berta Bürger, Anna Pintér-Csordás, Márton Király, Péter Szabó, Seif Eddine Habbachi, Tamás Novotny, Erzsébet Perez-Feró, Martin Ševeček, Martin Steinbrück, Juri Stuckert, Mirco Grosse Technical Meeting on Advanced Technology Fuels: Progress on their Design, Manufacturing, Experimentation, Irradiation, and Case Studies for their Industrialization, Safety Evaluation, and Future Prospects, 28–31 October 2025, IAEA, Vienna

## Slide 2
INTRODUCTION

## Slide 3
Development and testing of Accident Tolerant Fuels:
Positive effects seen in several areas (moderate oxidation, reduced hydrogen production, less heat from chemical reactions, delayed embrittlement if any, …)
Which effects will dominate fuel degradation in NPP accident scenarios?
Introduction
Small scale separate effect tests
Integral tests with fuel bundles

## Slide 4
Comparison of ATF and traditional Zr claddings
CODEX-ATF (IAEA ATF-TS):
  Bundle contained both Cr coated and uncoated Zr cladding tubes
  Main information on differences in the post-test examinations
CODEX-ATF-AIT (EU OFFERR):
  Only Cr coated components in the bundle, comparison with the reference tests (CODEX-AIT-3) carried out with uncotaed Zr components
  Possibility for the comparison of on-line measured data
CODEX-ATF and CODEX-ATF-AIT

## Slide 5
CODEX-ATF and CODEX-ATF-AIT
steam
steam+air
Atmosphere

## Slide 6
The CODEX facility
Electrically heated 7-rod bundle in hexagonal geometry

## Slide 7
The CODEX facility
CODEX-ATF CODEX-ATF-AIT

## Slide 8
CODEX-ATF

## Slide 9
Max. cladding temp.
500 s
Power (+800 W external heaters)
600 W
1000 W
0 W
Argon
Steam
0 g/s
Water
1400 °C
0.2 g/s
600 °C
0.2 g/s
10 g/s
2000 W
Preparatory phase
Heat-up phase I
Quench
1000 °C
Burst
800-900 °C
1000 s
Heat-up phase II
0 g/s
technological heat-up of the facility, initiation of steam supply, moderate power and target temperature of 600 °C
further heat-up with increased power, pressurization of fuel rods to reach burst, target temperature of 1000 °C
further heat-up with increased power, target temperature of 1400 °C
injection of water, switching off power and steam supply
CODEX-ATF planned scenario

## Slide 10
Ballooning and burst
Oxidation of cladding external surface
Oxidation of inner cladding surface and secondary hydriding
Eutectic formation
SBO like scenario with recovery of ECCS
optZIRLOTM
Cr-coated optZIRLOTM
CODEX-ATF planned scenario

## Slide 11
Maximum rod temperature
T1_550mm, 1655 °C
Preparatory ph.
Heat-up
ph.
Quench
Heat-up
ph.
Quench
Preparatory ph.
CODEX-ATF power, flowrates, temperatures

## Slide 12
CODEX-ATF pressures

## Slide 13
Total H2 generation 2.9 g
CODEX-ATF hydrogen production

## Slide 14
Top of the bundle
Uncoated rod
Coated rod
CODEX-ATF endoscopic images from the top
Debris

## Slide 15
Rod No. 3 - Cr-coated optZIRLOTM
Rod No. 4 - optZIRLOTM
Cr2O3
ZrO2
“crocodile skin” (Zr-Cr eutectic )
spacer grid
inner oxidation
inner oxidation
mark of spacer grid
elevation 590-630 mm, Tmax>1350 °C
CODEX-ATF broken-off pieces from the top
393 ppm H
150 ppm H

## Slide 16
CODEX-ATF bundle cross sections
Ballooning, burst and brittle failure

## Slide 17
CODEX-ATF oxidation of Cr coated claddings
Cracked Cr-layer on the ballooned tubes => start of Zr oxidation
Ballooned
Non- ballooned

## Slide 18
CODEX-ATF Cr diffusion into Zr
500 – 560 mm (maximum cladding temperature ≈1400 – 1650 °C)
Still significant metal phase
Largest Cr-Zr eutectic formation at rod No. 5. (undamaged Cr coating)
Cr diffusion => accumulation at the α-Zr(O)/β-Zr phase boundary

## Slide 19
CODEX-ATF spalling Cr2O3 layer
Cr2O3
ZrO2
Cr
Zr

## Slide 20
CODEX-ATF-AIT

## Slide 21
CODEX-ATF-AIT planned scenario
Steam and oxygen starvation
Air ingress after preoxidation in steam

## Slide 22
The main objective of the proposed test was to check if Cr coating would have a protective role in case of NPP accidents with air ingress.
The proposed scenario was focused on covering several phenomena of fuel behavior during accidents
  burst,
  oxidation,
  nitriding,
  eutectic formation.
CODEX-AIT-3 experiment was chosen for reference test which was an air ingress test conducted with traditional Zr materials.
CODEX-ATF-AIT planned scenario

## Slide 23
CODEX-ATF-AIT – coating on Zr components
Number of fuel rods | 7
Cladding of fuel rods | Cr-coated optZIRLOTM
Length of fuel rods | 900 mm
External diameter of fuel rods | 9.1 mm
Cladding wall thickness | 0.57 mm
Pellet material | ZrO2
Pellet material in the bottom of the rods | Al2O3
Height of pellet | 10 mm
Diameter of pellet | 7.65 mm
Hole diameter in the pellet | 2 mm
Spacer grid material | Cr-coated Zr1%Nb
Height of spacer grid | 10 mm
Thickness of spacer grid | 0.4 mm
Number of spacer grids | 3
Shroud material | Cr-coated Zr2.5%Nb
Shroud thickness | 2 mm
Length of shroud | 1000 mm
Cr coating: Czech Technical University in Prague, PVD technique
Uniform Cr coating layer around the circumference of the cladding ≈15.5 µm
Thickness of the Cr layer on spacer grid
at the straight sections almost uniform ≈ 10 – 12 µm
at the curved parts ≈ 2 – 3 µm
Number of fuel rods | 7
Cladding of fuel rods | E110G
Length of fuel rods | 1000 mm
External diameter of fuel rods | 9.1 mm
Cladding wall thickness | 0.69 mm
Pellet material | ZrO2
Pellet material in the bottom of the rods | Al2O3
Height of pellet | 10 mm
Diameter of pellet | 7.65 mm
Hole diameter in the pellet | 2 mm
Spacer grid material | Zr1%Nb
Height of spacer grid | 10 mm
Thickness of spacer grid | 0.4 mm
Number of spacer grids | 3
Shroud material | Zr2.5%Nb
Shroud thickness | 2 mm
Length of shroud | 1000 mm
CODEX-AIT-3
CODEX-ATF-AIT

## Slide 24
Power and temperatures
CODEX-ATF-AIT
CODEX-AIT-3

## Slide 25
CODEX-ATF-AIT results – Temperatures
CODEX-ATF-AIT
CODEX-AIT-3
Extra power was needed with Cr coating to accelerate temperature increase
Half hour delay in escalation

## Slide 26
CODEX-ATF-AIT
Top view of the CODEX-ATF-AIT bundle after experiment
CODEX-ATF-AIT results – Pressures

## Slide 27
CODEX-ATF-AIT
CODEX-AIT-3
Total H2 generation:
Pre-oxidation phase: ≈ 3.8 g
Air-ingress phase: ≈ 1.4 g
CODEX-ATF-AIT results – Outlet gas composition
Total H2 generation:
Pre-oxidation phase: ≈ 1.4 g
Air-ingress phase: -
Extra air-ingress phase: ≈ 3.3 g

## Slide 28
Cross section of rods at 125 mm
125 mm
pre-oxidation phase: no balloning, no oxidation (T < 600 °C)
extended air ingress phase: eutectic melt formation (Tmax ≈ 1400 °C)
64 at. % Cr
30 at. % Zr
3 at. % Fe
96 at. % Zr
2 at. % Cr
2 at. % Fe
α-Zr(O) (60-80 at. % Zr – 15-30 at. % O) and thin Cr-rich features (2-5 at. % Cr )
Cr coating
≈100 μm ZrO2 layer
50-60 μm α-Zr(O) layer
150-250 μm eutectic region
≈350 μm β-Zr layer

## Slide 29
Cross sections of rods at 800 mm
No. 2.
ballooned and burst
No. 3.
ballooned and non-burst
No. 6.
non-ballooned

## Slide 30
SUMMARY AND CONCLUSIONS

## Slide 31
Two integral tests with ATF cladding materials were conducted in the CODEX facility in steam and steam+air atmospheres
Summary
 | CODEX-ATF | CODEX-ATF-AIT
Max. temperature | 1655 °C | 1545 °C
Steam atmosphere | Yes | Yes
Steam+air atmosphere | No | Yes
Oxidation | Yes | Yes
Nitriding | No | Yes
Cr-Zr eutectic | Yes | Yes
Quench | Yes | No

## Slide 32
Summary – axial temperature profiles
CODEX-ATF CODEX-ATF-AIT
No steam starvation
Steam and oxygen starvation

## Slide 33
The comparison of results from the CODEX-AIT-3 and CODEX-ATF-AIT tests suggests that ATF materials can increase the coping time in the event of air ingress type reactor accidents.
The ATF cladding reacted significantly less with high-temperature steam below 1200 °C than traditional Zr cladding material.
In the reference test, air ingress led to a temperature excursion, with cladding temperatures reaching 1625 °C within 40 minutes. Under the same conditions in the CODEX-ATF-AIT test, the cladding temperature increased only to 1030 °C over the same period.
Conclusions
Ballooning of Cr coated claddings resulted in crackings of Cr-layer, which lead to local oxidation of Zr at the crack positions.
Cr-Zr eutectic formation and Cr diffusion took place at ≈1400 – 1650 °C.
Similar degree of degradation of Cr coated and uncoated claddings was observed after reaching 1655 °C temperature.
CODEX-ATF CODEX-ATF-AIT

## Slide 34
The Cr coating provided significant protection against oxidation in both steam and air atmospheres as long as the coating remained intact.
  Ballooning: after cracking of the Cr layer, local oxidation of Zr began. The local oxidation spots could facilitate full cross-sectional fracture of the cladding tube wall.
  Cr-Zr eutectic melt formation: can take place if Cr diffuses into the Zr cladding wall to a large extent and the temperature reach the Cr-Zr eutectic melt formation temperature. Fast oxidation/nitriding of the metallic Cr-Zr eutectic melt could start.
The final state of the Cr-coated and uncoated fuel rods after reaching 1500–1600 °C was similar.
The degradation of the ATF fuel occurred more slowly in the integral tests compared to traditional fuel.
Conclusions

## Slide 35
Thank you for your attention!