## Slide 1: IAEA ATF BENCHMARK OF FUEL ROD CODES FOR SIMULATION OF SELECTED SEPARATE EFFECT TESTS
Technical Meeting ATF, 28-31 Oct. 2025, Vienna
A. Bouloré 1, M. Cherubini 2
1 CEA.DES.IRESNE.DEC, Cadarache, F-13108, Saint Paul lez Durance
2 N.IN.E. - Nuclear and INdustrial Engineering S.r.l.

## Slide 2: Introduction
  CRP “ATF-TS” structure
  WT2 : benchmark the computer codes used for ATF behavior simulation
    Specific developments made to improve modelling of ATF materials
    Code “validation” for ATF materials in normal, off-normal and accident conditions
    WT2.1: single rod experiments only (WT2.2: bundle tests)
ATF-TS
WT 1:
Experimental
Programme
M. Sevecek (CZR)
J. Stuckert (GRF)
WT 2:
Modelling & Benchmark Exercises
A. Bouloré (FRA)
M. Cherubini (ITA)
J. Stuckert (GRF)
Z. Hozer (HUN)
WT 3:
LOCA Evaluation Methodology
J. Zhang (BEL)
WT 4:
Material Properties Database for ATF
Ch. Allison (USA)
Co-Chairs: J. Zhang (BEL), M. Sevecek (CZR)
Sci. Secretary: A. Khaperskaya (IAEA)
(former Sci. Secs: K.S.Sim, M.Veschunov)

## Slide 3: Introduction
  ATF concepts
    Chromia doped UO2 pellets in irradiation
      Steady state
      Transient
    FeCrAl claddings
      Separate effect tests (burst tests)
    Cr-coated Zircaloy claddings
      Separate effect tests (burst tests)
      Single rod test (DEGREE facility)

## Slide 4: Cases (Chromia doped UO2 fuel)
  Mandatory: Steady state, IFA716 rods 1 and 6
    AREVA UO2+Cr2O3 pellets
      Thermocouple
      Internal pressure (FGR)
      Fuel elongation (swelling)
  Optional: High initial rating, IFA677 rods 1 and 5
    Westinghouse UO2+Al2O3+Cr2O3
      TCs
      Internal pressure (FGR)
      PIE

## Slide 5: Cases (Chromia doped UO2 fuel)
  Off-normal conditions: SCIP II power ramps
    Cr-doped UO2 fuel (AREVA) irradiated in Oskarshamn-2 (BWR)
    Zy-2 cladding with Zr liner
    Ramp up to 450 W/cm
      Mandatory: Aa2, 12h holding time
      Optional: Aa1, no holding time
    PIE: puncturing and profilometry
Rod number | Aa2 | Aa1
Burnup (GWd/tM) | 28 | 26
Conditioning Power Level (CPL) (kW/m) | 10 | 10
CPL duration (h) | 12 | 12
Ramp Terminal Level (kW/m) | 45 | 45
Holding time | 12 h | 15-30 s
Experimental fission gas release (%) | 1.7 | 0.02

## Slide 6: Cases (ATF claddings)
  SET FeCrAl claddings (similar to ACTOF CRP)
    “Virtual” burst tests from PUZRY (EK lab., Hungary)
      adapted to FeCrAl
      @controlled temperature (800-1200°C)
      Priority tests #8, 18 and 30
      Geometrical data and exp. conditions provided to participants
    Burst tests performed at HUN-REN EK (Hungary)
      FeCrAl cladding provided by KIT
      @controlled T (800-925°C) and Pressure rate
  SET Cr-coated claddings
    Burst tests (CTU, Czech Rep.)
      Cr-coated Optimized ZIRLO
      Temperature range 800-915°C
      Pressurization rate range 5-106 kPa/s
Sample | Temperature (°C) | Pressurization rate (kPa/s) | Burst pressure (MPa)
OPZCR-1 | 804-807 | 105 | 7.29
OPZCR-4 | 835-814 | 105 | 6.13
OPZCR-5 | 902-905 | 94 | 3.53
OPZCR-8 | 902-905 | 6 | 2
Material properties/correlations provided
ACTOF  FeCrAl
ATF-TS WT1  Cr-coated cladding

## Slide 7: Cases (ATF claddings)
  DEGREE single rod test S3
    SET on Cr-coated Zy-4 cladding
    LOCA heating and cooling phase
    Experimental conditions
      Heating power
      Steam flow rate
      Cladding outer temperature (3 locations)
      Internal pressure (detect balloon./burst)
    Post-tests examinations
      Profilometry
      H pickup
      Chemical analysis (Cr diffusion)

## Slide 8: List of participants
  19 organizations
  16 countries
Country | Participant | Code | UO2 Cr doped |  |  | FeCrAl | Coated Zy claddings | Coated Zy claddings
 |  |  | IFA716 | IFA677 | SCIP II power ramps | ACTOF cases + ATF-TS SET | ATF-TS SET | DEGREE Single rod test S3
Argentina | CNEA | DIONISIO | x | x | x | x | x | x
Belgium | Tractebel | FRAPCON/FRAPTRAN |  |  |  |  | x | 
Brazil | IPEN | TRANSURANUS |  |  |  | x |  | 
Bulgaria | INRNE-BAS | TRANSURANUS |  |  |  | x |  | 
China | CNPRI | JASMINE | x | x |  | x | x | 
China | CNPE | FRAPCON/FRAPTRAN |  |  |  | x |  | 
China | NPIC | FUPAC | x | x |  | x | x | 
Czech Republic | CTU | FRAPCON/FRAPTRAN, TRANSURANUS | x |  | x |  | x | 
France | CEA | ALCYONE | x | x | x |  |  | 
Germany | GRS | TESPA-ROD |  |  |  | x |  | 
Iran | ANCC | PARS/PART | x | x | x |  | x | 
Italy | NINE | TRANSURANUS | x | x | x | x |  | 
Japan | CRIEPI | FRAPCON |  |  |  |  |  | x
Korea | KAERI | FRAPCON/MERCURY | x |  |  | x | x | x
Russia | IBRAE | SOCRAT |  |  |  |  | x | x
Slovakia | B&J | FEMAXI | x | x | x |  |  | 
Spain | UPM | TRANSURANUS |  |  |  | x |  | 
Spain | CIEMAT | FRAPCON/FRAPTRAN | x | x | x | x |  | 
USA | UTK | BISON | x | x | x | x |  | 

## Slide 9: Selected results
  Cr-doped UO2 fuel
    Exhaustive comparison of calculated quantities with experimental data to be done in TECDOC
      Fuel temperature
      Pressure evolution
      Fuel stack elongation
      …
    Results in a reasonably good agreement with experiments
    Importance of uncertainty knowledge (experimental conditions)

## Slide 10: Selected results
  Burst tests
    Exhaustive comparison of calculated quantities with experimental data to be done in TECDOC
      Time to burst
      Burst pressure
Case (rod #) | Exp (s) | CNEA | CNPRI | IBRAE | KAERI | Tractebel | CIEMAT | UPM | IPEN | NINE
OPZCR-1 | 83.5 | 67 | 39.5 | 92 | 83 | 83,4 |  |  |  | 
OPZCR-4 | 108 | 58 | 35.5 | 112 | 90 | 109,3 |  |  |  | 
OPZCR-5 | 53.5 | 29 | 27.5 | 60 | 53 | 57.6 |  |  |  | 
OPZCR-8 | 323 | 299 | 230 | 349 | 315 | 296 |  |  |  | 
FCA-1 | 62.7 |  |  |  |  |  | 58.6 | 53.6 | 56.3 | 56.6
FCA-2 | 59.7 |  |  |  |  |  | 52.8 | 49.2 | 51.8 | 51.4
FCA-3 | 38.2 |  |  |  |  |  | 29.4 | 27.1 | 28.6 | 28.6
FCA-4 | 41.7 |  |  |  |  |  | 33 | 31.4 | 33.1 | 27.4

## Slide 11: Selected results
  Burst tests
    Exhaustive comparison of calculated quantities with experimental data to be done in TECDOC
      Hoop strain at # axial level
        FeCrAl : some properties of the materials (e.g. surface treatment) is not taken into account in the analytical models and may play a role in the deformation behaviour.

## Slide 12: Selected results
  DEGREE single rod test
    Exhaustive comparison of calculated quantities with experimental data to be done in TECDOC
      Cladding temperature at # axial position
      Hoop strain
      Time to burst
      Burst pressure
      Oxidation layer thickness (no exp.)
Cladding temperature @TC level (DEGREE single rod test S3)

## Slide 13: Conclusion
  WT2.1 of ATF-TS CRP
    Code improvement for ATF materials
    Code “validation” for ATF materials (claddings, pellets)
    Pre-requisite for participation to WT3 (development of a methodology for ATF assessment)
  Chromia-doped fuel irradiations
    Benchmark results aligned well with experimental data, highlighting the importance of uncertainty analysis in fuel performance code validation
  ATF claddings separate effects tests
    Burst pressure predictions were accurate with available data, though hoop strain predictions varied
    Discussions suggested improvements in code predictions and the need for further work on material properties and deformation behavior

## Slide 14: Conclusion
  General conclusion and subjects for next CRP (future work)
    Validation
      current benchmarks are based on non-irradiated separate effect tests
      Future projects should include integral or semi-integral irradiation tests for comprehensive validation
    LOCA Tests
      No fueled ATF LOCA tests were provided
      Future projects should address this gap
      If no experimental data available, “theoretical cases” could be considered (e.g. boundary conditions provided by system codes corresponding to LOCA scenario)
    Emphasize uncertainty analysis, material property verification, and inclusion of irradiated data for improved code validation

## Slide 15: Thank you for your attention
Antoine Bouloré
antoine.boulore@cea.fr
Marco Cherubini
m.cherubini@nineeng.com