## Slide 1: RIA simulations of ATF fuel in large and WC-SMRs by means of TRANSURANUS
Paul Van Uffelen, Z. Soti, A. Schubert, P. Aragón
IAEA TM on ATF, Vienna, 28-31 October 2025

## Slide 2: Contents
Introduction
ATF properties in TRANSURANUS
Case selection
  RIA simulation in PWR: Nuscale-like WC-SMR of McSAFER project
  RIA simulation in BWR: FK1 case of Fumex-III CRP (IFPE)
Conclusions and perspectives

## Slide 3
HORIZON SCORPION Project
(SiC Composite Claddings: LWR Performance Optimization for Nominal and Accident Conditions)
16 partners (Europe, USA, Japan, Swiss)
Radical performance optimization of the SiC/SiC composite ATF cladding material concept for Gen-II/III LWRs
September 2022 – February 2026
H2020 IL TROVATORE Project
(Innovative Cladding Materials for Advanced Accident-Tolerant Energy Systems)
30 partners (Europe, USA, Japan)
BR2 irradiation of global ATF cladding material concepts (i.e., SiC/SiC composites, Cr-coated zircaloys, ODS-FeCrAl alloys)
October 2017 – March 2025
I-NERI PERSEUS Project
(Advanced PIE of Accident-Tolerant Fuel Claddings Neutron-Irradiated in the BR2 Test Reactor)
7 partners (Europe, USA)
Advanced PIE of BR2-irradiated ATF claddings in H2020 IL TROVATORE
May 2021 – April 2027
I-NERI = International Nuclear Energy Research Initiative
3
Euratom projects with exp. work on ATF (Prof. K. LAMBRINOU )

## Slide 4: Large user network – Excellent collaboration
Collaborations for ATF
POLIMI, NINE, UPM, NFQ, CIEMAT, IPEN, INRNE, USP, CTU, UCAM
And with support from many
Euratom projects: e.g. Il Trovatore, SCORPION, OperaHPC, APIS, CONNECT-NM

## Slide 5: “ATF” in TRANSURANUS
Cladding | Fuel
Zry4 or Zry2 (reference) | UO2 and Gd-UO2 (reference)
M5 | U3Si2
ZIRLO, optZIRLO | Cr-UO2 (and ADOPTTM)
Cr-coated Zry | (Th,Pu)O2, (Th,U)O2
FeCrAl | MOX(-MA)
SiC | UN, (U,Pu)N
Hastelloy | UC, (U,Pu)C
SS | 

## Slide 6: Preparing for Cr-doped UO2 fuel
G. Nicodemo et al, Journal of Nuclear Materials 601 (2024) 155301

## Slide 7: Fuel phenomena for reference pin and switching to ATF in Rolls-Royce type SMR
A. De Lara et al, Annals of Nuclear Energy 218 (2025) 111355

## Slide 8: Extend TU(MECH) with Cr-coated Zry
Simulated Halden LOCA test IFA-650.10 simulated using FRAPTRAN + TUmech
P. Aragon et al, Annals of Nuclear Energy 211 (2025) 110950

## Slide 9: Contents
Introduction
ATF properties in TRANSURANUS
Case selection
  RIA simulation in PWR: Nuscale-like WC-SMR of McSAFER project
  RIA simulation in BWR: FK1 case of Fumex-III CRP (IFPE)
Conclusions and perspectives

## Slide 10: Nuscale-like core

## Slide 11
For the multi-physics calculations we coupled 3 software packages
  Serpent2 (SSS): VTT
  SUBCHANFLOW (SCF): KIT
  TRANSURANUS (TU): JRC
Coupling was done in ICoCo environment of EU Salome platform
We used ICoCo interfaces and supervisor developed in McSAFE project (with HZDR,KIT) and adjusted to needs of RIA
Simulations done on HPCluster of JRC(Petten)
Simulations tools for REA in Nuscale-like core
Zsolt et al, Nuclear Engineering and Design 441 (2025) 114183

## Slide 12: Effect of ATF on fuel temperatures during RIA
Serpent (SSS)
TRANSURANUS (TU)
→High-fidelity simulation recommended for ATF in water cooled SMR

## Slide 13
Warning: simulate ATF with same power pulse as UO2 fuel during a RIA may be misleading (e.g Liu et al with CAMPUS code)
Progress in Nuclear Energy 159 (2023) 104648
Melting in U3Si2 fuel in pellet periphery
during RIA may not happen due to lower
power peak in ATF

## Slide 14: Contents
Introduction
ATF properties in TRANSURANUS
Case selection
  RIA simulation in PWR: Nuscale-like WC-SMR of McSAFER project
  RIA simulation in BWR: FK1 case of Fumex-III CRP (IFPE)
Conclusions and perspectives

## Slide 15: FK1 case of FUMEX-III
RIA test in NSSR
Base irradiated in Fukushima 1
Refabricated BWR fuel rods

## Slide 16: Coolant T during RIA

## Slide 17: Temperature in standard fuel during RIA

## Slide 18: Melting achieved in U3Si2 fuel, assuming peak power of oxide fuel

## Slide 19: Evolution of radial T in ATF during RIA of FK1

## Slide 20: Fuel centre T during RIA

## Slide 21: Gap size during RIA (slice 3)

## Slide 22: Summary
Implemented and tested successfully a variety of ATF properties in TRANSURANUS in collaboration with the large user community, and support from Euratom projects (Il Trovatore, OperaHPC, APIS, etc.)
Pointed out need for careful safety analysis (e.g. Melting in ATF))
High-fidelity coupling of codes proved useful for SMR/AMR, especially where few data are available

## Slide 23: Perspectives Direct support TRANSURANUS for SMR/AMRs
EU-SMR-LFR project (Ansaldo Nucleare, SCK-CEN, ENEA, RATEN)
CityHeat project (Calogena, Steady Energy)
Project Quantum (Last Energy)
European LFR AS Project (newcleo)
Nuward (EDF)
European BWRX-300 SMR (OSGE)
Rolls-Royce SMR (Rolls-Royce SMR Ltd)
NuScale VOYGR™ SMR (RoPower Nuclear S.A)
Thorizon One project (Thorizon)
SEALER (Blykalla)
Hexana
Tractebel
SOLO (Terra Innovatum)
MYRRHA (SCK-CEN)
Projects identified so far by IA SMRs
Other advanced reactor projects
TRANSURANUS license
Under discussion
→JRC directly supports projects and Technical Working groups of IA SMR

## Slide 24: Thank you and keep in touch
© European Union 2024
Unless otherwise noted the reuse of this presentation is authorised under the CC BY 4.0 license. For any use or reproduction of elements that are not owned by the EU, permission may need to be sought directly from the respective right holders.
Notes: Update/add/delete parts of the copy right notice where appropriate.
More information: https://myintracomm.ec.europa.eu/corp/intellectual-property/Documents/2019_Reuse-guidelines%28CC-BY%29.pdf

## Slide 25
H2020 IL TROVATORE (Innovative Cladding Materials for Advanced Accident-Tolerant Energy Systems)
Prof. Konstantina Lambrinou, University of Huddersfield (UoH), UK
H2020 European Research & Innovation Action (RIA)

## Slide 26
H2020 IL TROVATORE
Goal: Help to address the global societal & industrial need for improved nuclear energy safety by optimizing and validating select ATF cladding material concepts in an industrially relevant environment  neutron irradiation in contact with PWR-like water in the BR2 research reactor

## Slide 27
HORIZON SCORPION (SiC Composite Claddings: LWR Performance Optimization for Nominal and Accident Conditions)
Prof. Konstantina Lambrinou, UoH (UK) & IIT (Italy)
HORIZON European Research & Innovation Action (RIA)

## Slide 28
HORIZON SCORPION Project – Introduction & Objectives
Modular Material Design Approach:
connecting the nanoscale to the macroscale
Core Objectives: improvement of SiC compatibility with the coolant (water/steam) & resistance to radiation swelling