## Slide 1: Advancements in Hydrogen-Based Transient Cladding Strain Limits to Support Accident Tolerant Fuel
Michael Orner
Westinghouse – Fuel Rod Design Principal Engineer

## Slide 3: Agenda Items
Background on industry direction and its impact on transient cladding strain
Introduction to transient cladding strain
Historical cladding strain limits
Theory of hydrogen and material strength
Westinghouse hydrogen-based transient cladding strain limit for ZIRLO® and Optimized ZIRLO™ cladding
Extension of the hydrogen-based strain limit to other cladding types
Alternative approach for AXIOM® cladding
Fuel performance margin improvements
AXIOM, ZIRLO, Optimized ZIRLO are trademarks or registered trademarks of Westinghouse Electric Company LLC, its affiliates and/or its subsidiaries in the United States of America and may be registered in other countries throughout the world. All rights reserved. Unauthorized use is strictly prohibited. Other names may be trademarks of their respective owners.

## Slide 4: Westinghouse’s Advanced Fuel Technology
  Chrome Coated Cladding – Chromium coating on the outside of existing zirconium based fuel cladding increases safety and operational margins and may enable greater energy extraction.
  AXIOM® Cladding – A unique zirconium-based alloy developed to enable nuclear fuel to run longer and provide more energy, while increasing safety margins.
  ADOPT™ Fuel Pellets – The large grain size and density of Chromia and Alumina doped fuel pellets, enable increased energy density, improved stability at high temperatures and additional safety margins.
  SiC Cladding and UN Pellets – SiC’s extremely high melting point and thermal conductivity has the potential to offer several significant safety and performance benefits.
  PRIME™ Fuel Features – This is a family of several unique fuel assembly features designed to improve fuel performance, enhance fuel cycle economics, and provide increase safety margins at higher burnup.
  LEU+ and Higher Burnup – This includes the fabrication of higher enriched fuel and a suite of advanced engineering codes and tools that allow utilities to operate their reactors with Westinghouse ATF hardware technologies and deliver measurable benefits.
ADOPT and PRIME are trademarks of Westinghouse Electric Company LLC, its affiliates and/or its subsidiaries in the United States of America and may be registered in other countries throughout the world. All rights reserved. Unauthorized use is strictly prohibited. Other names may be trademarks of their respective owners.

## Slide 5: Industry Direction and Its Impact on Transient Clad Strain
The nuclear industry is advancing toward:
High burnup operation
Extended fuel cycle lengths
Power uprates
These advancements reduce fuel performance margins, particularly affecting transient clad strain.

## Slide 6: Transient Clad Strain
Initial Gap Design:
Fuel rods are designed with an initial open gap between the fuel pellet and the cladding to accommodate thermal expansion.
Steady-State Operation:
The pellet-cladding gap gradually closes as the fuel pellets swell and the cladding creeps due to compressive pressure. Stress and strain develop at the contact point, but these are generally benign and do not cause fuel failure.
Transient Conditions (e.g., Overpower Events):
Transient events where a rapid increase in power causes thermal expansion of the fuel pellet to occur at a faster rate than that of the cladding material results in significant strain on the cladding. Too much deformation during the transient event can cause fuel failure.
Transient Overpower Strain Limit:
Historically, Westinghouse fuel has adhered to a constant 1% cladding strain limit during overpower transient events, as prescribed by the U.S. NRC Standard Review Plan (SRP) Section 4.2
The design limit for the fuel rod clad strain is that the total tensile strain, elastic plus plastic, due to uniform cylindrical fuel pellet deformation during any single Condition I or II transient shall be less than 1% from the pre-transient value.

## Slide 7: Transient Clad Strain Results for New Programs
Chart: Local Burnup (MWD/MTU)
1% Strain Limit | 1 | 1
Chart: Local Burnup (MWD/MTU)
1% Strain Limit | 1 | 1
1% Strain limit violations
Point of gap closure which can also be limiting
Using the traditional 1% strain limit for ATF products would result in failure of the design limit. However, the NRC allows for deviations in the acceptance criteria, including the submittal of an alternative strain limit.

## Slide 8: Transient Clad Strain Limit Alternatives
The current 1% cladding strain limit is a constant value which does not consider the effects of cladding material properties, manufacturing processes, irradiation, temperature, hydrogen uptake, and other factors that impact material strength
Implementation of an alternate, hydrogen-based transient strain limit, which is based on measured test data, provides a more accurate representation of the true behavior of zirconium-based cladding
  It also serves to improve strain margin for most plants

## Slide 9: Theory
Measurements and mechanical testing have shown that the yield strength (YS) and ultimate tensile strength (UTS) of zirconium-based cladding have a strong dependence on hydrogen content
Free hydrogen (H2) and a zirconium oxide (ZrO2) layer are formed due to the chemical reaction between the zirconium (Zr) fuel rod cladding and the reactor coolant (H2O) during operation
Zr + 2H2O  ZrO2 + 2H2

## Slide 10: Hydrogen Solubility
A fraction of the free hydrogen is absorbed by the cladding throughout the fuel rod lifetime, while unabsorbed hydrogen is dispersed into the reactor coolant
Hydrogen absorbed into the cladding is soluble until it reaches the temperature-dependent terminal solid solubility (TSS)

## Slide 11: Hydrogen Absorption
Hydrogen absorbed by the cladding above the solubility limit is considered “excess” hydrogen, which precipitates out as zirconium hydride (ZrH) platelets
ZrH platelets are not uniformly distributed across the cladding wall
  There is a temperature gradient across the cladding, and hydrogen tends to accumulate near the outer cladding wall where temperatures are lower

## Slide 12: Hydride Morphology
Hydride morphology affects the cladding material strength
Zirconium hydrides can precipitate in either the radial or circumferential direction
  Radial hydrides serve as pathways to crack propagation and are far more detrimental to material embrittlement relative to circumferential hydrides
  Circumferential hydrides also cause embrittlement but not to the same degree
For this reason, Westinghouse fuel rod tubing is manufactured to minimize radial hydride formation

## Slide 13: Hydride Reorientation
It is possible for circumferential hydrides to reorient in the radial direction if the applied hoop stress in the cladding exceeds a threshold stress
Hydride reorientation is primarily a concern during cooldown of the fuel rod, such as that which occurs during long-term storage
Hydrogen in the cladding will precipitate as the cladding cools because the terminal hydrogen solubility will decrease
The dissolution of hydrogen during cooldown, in conjunction with a constant hoop stress, will form radial hydrides if the stress is high enough

## Slide 14: Hydride Reorientation Prevention
This hoop stress is applied via rod internal pressure (RIP)
Tensile pressure differential across the cladding cause by high RIP creates a constant hoop stress, which may cause hydride reorientation as the cladding cools
Westinghouse imposes design limits which prevent the formation of excessive radial hydrides by holding RIP values below those which could initiate hydride reorientation either during operation or under storage conditions
Thus, only circumferential hydrides need be considered for a hydrogen-based strain-based limit

## Slide 15: Hydrogen Relation to Uniform Elongation
The relationship between hydrogen content and material strength and ductility of zirconium-based alloys is well-established, both by Westinghouse and other scientific organizations
When ZrH platelets form and concentrate in a circumferential hydride rim near the outer surface of the cladding, it reduces the cladding ductility
Westinghouse has developed a uniform elongation (UE) strain limit as a function of hydrogen content to better model the actual material strength of the cladding

## Slide 16: Uniform Elongation
UE corresponds to the ultimate tensile stress (UTS) of the cladding and represents the strain at which deformation ceases to be uniform and stable
A sample stress/strain curve including UE, UTS, yield stress (YS), and the modulus of elasticity (E)
Total Uniform Elongation (UETotal) is made up of two components, UEPlastic and UEElastic

## Slide 17: Uniform Elongation Strain Limit Concept
Implementing a UE cladding strain limit instead of the current 1% limit explicitly accounts for the effects of hydrogen embrittlement in the cladding while continuing to ensure the integrity of the fuel during an overpower transient
A UE strain limit also increases margin at the limiting time in life by crediting the higher ductility at lower burnup before the accumulation of circumferential hydrides begins to degrade the cladding material strength

## Slide 18: ZIRLO and Optimized ZIRLO Cladding Hydrogen-Based Strain limit
A hydrogen-based strain limit for ZIRLO and Optimized ZIRLO cladding was approved by the NRC in PWROG-21001-P-A
The hydrogen strain limit for ZIRLO and Optimized ZIRLO cladding was based on uniform plastic elongation (UEPlastic)
UEPlastic is a conservative parameter that was used to be consistent with the strain definition in the PNNL Stress/Strain Correlation for Zircaloy report (PNNL-17700)

## Slide 19: Uniform Elongation Strain Limit Generation
Westinghouse developed the ZIRLO and Optimized ZIRLO cladding UEPlastic strain limit based on measured data from the Studsvik Hot Cell Laboratory
  Strain measurements were taken via axial tensile testing (ATT) and ring tensile testing (RTT), and hydrogen measurements were taken using hot vacuum extraction
Of the well-characterized data points from Studsvik, some of the cladding samples have excess hydrogen, while others do not (i.e., the hydrogen in the sample is entirely soluble)
  It is important that these data points are modeled separately because the UE behavior changes once the cladding exceeds the saturation point and hydrides begin to form

## Slide 20: Uniform Elongation Strain Limit Generation
A regression analysis was used to develop the best estimate and lower bound UE strain limit for those Westinghouse data points with excess hydrogen
Statistical methods were used to ensure that the UE lower bound limit constrains the test data on a 95% probability at 95% confidence level (95/95) basis
The UE limit is a function of the total hydrogen content (soluble and excess) where the ratio of soluble and excess hydrogen is determined based on the cladding temperature

## Slide 21: Uniform Elongation Strain Limit Generation
A different approach was taken for those data points which contain only soluble hydrogen
Hydrogen content prior to the formation of ZrH platelets (i.e., the saturation limit) does not affect the material ductility
Unless hydrides are present in the cladding, the material behavior is insensitive to hydrogen content
Thus, the UE limit prior to the terminal solubility limit is a constant value
Once the saturation level is reached, the UE limit reverts to the hydrogen-dependent UE limit

## Slide 22: Challenges with recrystallized (RXA) Cladding
Low RXA Cladding
(ZIRLO and Optimized ZIRLO)
High RXA Cladding (AXIOM)
High RXA Alloys
  High RXA alloys exhibit increased ductility and higher total elongation, offering better performance under certain conditions. However, they exhibit different behavior and are not compatible with the existing hydrogen-based model.

## Slide 23: Updating the UE Basis
The USNRC defines the strain limit as the total elastic and plastic strain.
Using UETotal as the basis for AXIOM cladding hydrogen-based strain limit is consistent with how the NRC categorizes pellet-cladding mechanical interaction driven strain.
A new strain limit model is being developed to utilize UETotal as its basis

## Slide 24: Axiom Testing
Partnerships for Testing
  Westinghouse is collaborating with Studsvik to conduct innovative testing on AXIOM.
Innovative Testing Techniques
  Switching from load-controlled to displacement-controlled tests enhances the representation of real-world scenarios.
  Improvements in ring tensile testing (RTT) techniques allow the elastic loading test phases to conform to the elastic modulus such that it more accurately reflects deformation under PCMI
RTT with hold
The cladding is strained to a target strain of 2% and held for 15 minutes. Then it is either unloaded or strained an additional 2% and held again for an additional 15 minutes. The purpose is to demonstrate cladding stability at deflection limited strains > in reactor transient strains.
This confirms that margin exists for cladding integrity under PCMI loading at strains beyond UETotal

## Slide 25: Extending the Hydrogen-Strain Limit to Other Claddings
Westinghouse is working with the Pressurized Water Reactor Owners Group (PWROG) to extend the applicability of the hydrogen-based transient cladding strain limit to new materials
  AXIOM cladding
  Chromium (Cr) coated cladding
The same hydrogen-based strain limit approved for ZIRLO and Optimized ZIRLO cladding in PWROG-21001-P-A will be used
The hydrogen-based strain limit in PWROG-21001-P-A is bounding for the measured AXIOM cladding UETotal data

## Slide 26: Margin Impact
Once enough hydrogen accumulates in the cladding, the UE strain limit decreases because of the increased brittleness related to the formation of circumferential hydrides
If enough hydrogen is absorbed by the cladding, the UE strain limit can become more restrictive than the current 1% strain limit
However, it is unlikely for modern corrosion-resistant Westinghouse cladding to accrue enough hydrogen such that the UE limit drops below 1%
Therefore, a hydrogen-based UE strain limit recovers design margin, particularly early in life

## Slide 27: Hydrogen Impact
Hydrogen Pick-up Reduction
  Reducing hydrogen pick-up rates in is essential for improving the margin recovered by the improved strain limit.
  Advanced Cladding Improvements
  Both AXIOM and Chromium coated cladding significantly reduce the amount of hydrogen pickup experienced by the cladding.
Chart: Burnup (MWD/MTU)

## Slide 28: Example Analysis
Chart: Optimized ZIRLO
1% Strain Limit | 1 | 1
Chart: AXIOM
1% Strain Limit | 1 | 1
Large margin increase with the use of AXIOM cladding and a hydrogen–based strain limit

## Slide 29: Conclusion
Advanced Fuel Technology is essential for enabling:
  Longer fuel residency times
  Burnup levels up to 75 GWD/MTU
  LEU+ fuel adoption
  Power uprates
  Other major PWR modernization programs
Limitation: Transient Clad Strain
  Transient Clad Strain is currently one of the most limiting design criteria for PWRs using advanced fuel products.
  This is because advanced cladding materials cannot utilize the existing hydrogen-based strain limit, which was developed for legacy zirconium alloys.
Solution: Updated Hydrogen-Based UETotal Strain Limit
  The new UETotal strain limit allows utilities to:
    Adopt advanced products without sacrificing design margin for transient clad strain.
    Preserve or increase performance margin, enabling broader deployment of advanced fuel technologies.
Strategic Impact
  Providing strain margin relief to advanced products is a critical enabler for the future operation and evolution of PWR plants.