## Slide 1
Fuel Retention and Erosion of Metallic Plasma-Facing Materials under the Influence of Plasma Impurities
A. Kreter1, L. Buzi1,2,3, G. De Temmerman2,4, T. Dittmar1, R.P. Doerner5, Ch. Linsmeier1, D. Nishijima5, M. Reinhart1 and B. Unterberg1
1 Forschungszentrum Jülich GmbH, Institut für Energie- und Klimaforschung – Plasmaphysik, Partner in the Trilateral Euregio Cluster (TEC), 52425 Jülich, Germany
2 FOM Institute DIFFER - Dutch Institute for Fundamental Energy Research, Edisonbaan 14, 3439 MN, PO Box 1207, 3430 BE Nieuwegein, The Netherlands
3 Gent University, Sint-Pietersnieuwstraat 41, B-9000, Gent, Belgium
4 ITER Organization, Route de Vinon sur Verdon, 13115 Saint Paul Lez Durance, France
5 Center for Energy Research, University of California at San Diego, 9500 Gilman Drive, La Jolla, CA 92093-0417, USA
25th Fusion Energy Conference (FEC 2014)
Saint Petersburg, Russia
15 October 2014

## Slide 2: Plasma-wall interaction largely defines the availability of fusion reactor
Be
W
Crucial issues for reactor availability
Erosion of plasma-facing components
 Limited lifetime of plasma-facing components
Fuel retention in bulk wall material and deposited layers
 Accumulation of radioactive tritium in vacuum vessel
(amount of in-vessel retained tritium is limited in ITER due to safety regulations to ~1kg)
First wall materials in ITER
Beryllium for main chamber wall
Tungsten for divertor
Impurities in reactor
Helium from D-T reactions
Impurity seeding for edge plasma cooling, argon is one of the candidates
  Influence of impurities on PWI processes needs to be investigated

## Slide 3: This contribution: interaction of impurity containing plasma with beryllium and tungsten
Beryllium
Erosion and fuel retention under influence of helium and argon
Qualification of aluminium as possible substitute for beryllium in relevant studies
Tungsten
Influence of the incident ion flux on fuel retention and surface morphology
Fuel retention under influence of helium and argon
Experimental studies were performed in linear plasma devices PSI-2, PISCES-B and Magnum-PSI

## Slide 4: Linear plasma device PSI-2 (FZJ)
Coils
Side-fed manipulator
Plasma source
Target station
TEAC
Periphery level
3 m

## Slide 5: Linear plasma devices PISCES-B and Magnum-PSI
PISCES-B (UCSD): compatible with beryllium
Magnum-PSI (FOM-DIFFER): high particle and heat loads
[G. De Temmerman et al., Fusion Eng. Des. 88 (2013) 483]
[R. P. Doerner et al, Phys. Scr. T111 (2004) 75]

## Slide 6: Plasma exposure parameters in linear plasma devices
Parameter | PSI-2 | PISCES-B | Magnum-PSI | ITER divertor
Electron temperature | 1 - 40 eV | 3 - 50 eV | 0.1 – 10 eV | ~1 - 10 eV
El. density | ~1017 - 1019 m-3 | ~1017 - 1019 m-3 | ~1019 - 1021 m-3 | ~1020 - 1021 m-3
Particle flux | ~1021 - 1022 m-2s-1 | ~1021 - 1023 m-2s-1 | ~1023 - 1025 m-2s-1 | ~1024 - 1025 m-2s-1
Particle fluence | up to ~1027 m-2 per exposure | up to ~1027 m-2 per exposure | up to ~1027 m-2 per exposure | ~1026 - 1027 m-2 per pulse (400 s)
Incident ion energy | 10 - 300 eV (negative bias) | 10 - 300 eV (negative bias) | 1 - 300 eV (negative bias) | ~10 eV
Wall (sample) temperature | 300 - 2000 K | 300 - 2000 K | 300 - 2000 K | 500 - 1300 K (steady-state)
Special features |  | Beryllium compatibility | High particle flux | 
Transients (ELMs, disruptions) can be simulated by laser or pulsed plasma irradiation
Fluence per experiment is ~10x – 100x higher than in present pulsed tokamaks
Exposure parameters can be pre-selected to simulate particular ITER conditions

## Slide 7
Erosion and fuel retention of beryllium and aluminium

## Slide 8: Erosion of beryllium and aluminium
PISCES-B / PSI-2 exposure conditions
Controlled Ar or He seeding 0-100% (controlled by spectroscopy: uncertainty in Ar fraction due to presence of Ar2+ and ArD+)
Steady-state and reproducible plasma
i ~ 1022 m-2s-1
 ~ 1·1026 m-2
Ei = 40-100 eV
Ts = 35030 K
Be (press-sintered Brush Wellman S-65C) and Al targets
  Diagnostics and sample analysis
Erosion from target is measured by spectroscopy and mass loss
PISCES-B data published in
A. Kreter et al, Phys. Scr. T159 (2014) 014039
PISCES target in plasma
PSI-2 target in plasma
Al sample
Sample holder

## Slide 9: Surface morphology of Be and Al after exposure to D/Ar plasma
3 % 10 %
2 % 6 % 15 %
Ar fraction 100 %
…
5 µm
0 %
…
Beryllium in PISCES-B
Aluminium in PSI-2
Fine-scale grass-like structure in pure D plasma
Gradual smoothing out of surface with increase of Ar fraction

## Slide 10: Surface morphology of Be and Al after exposure to D/He plasma
Helium does not suppress formation
of grass-like structure, unlike argon
1 % 15 %
He fraction 100 %
…
0 %
Aluminium in PSI-2
10 µm
Beryllium in PISCES-B
in pure helium plasma [R. Doerner et al., JNM 455 (2014) 1]

## Slide 11: Measured and calculated sputtering yields in deuterium-argon plasma
Beryllium erosion by argon studied in PISCES-B
Aluminium erosion by argon studied in PSI-2
Reduced erosion of Be and Al in pure D plasma due to rough grass-like surface and dilution of subsurface layer by deuterium
Admixture of Ar to D plasma recovers erosion to expected values
Pure D: Rough Be surface
Pure Ar: Smooth Be surface
5 m
5 m
Pure D: Rough Al surface
Pure Ar: Smooth Al surface
5 m
5 m
Sputtering yield
0
0.01
0.02
0.03
0.04
0.05
0
20
40
60
80
100
Ar fraction of incident D+Ar ion flux [%]
Calculation (TRIM code)
for flat surface
Experiment
discrepancy
agreement
0
0.002
0.004
0.006
0.008
0.010
0
20
40
60
80
100
Ar fraction of incident D+Ar ion flux [%]
Sputtering yield
Calculation (TRIM code) for flat surface
Experiment
discrepancy
agreement

## Slide 12: Measured and calculated sputtering yields in deuterium-helium plasma
Aluminium erosion by helium studied in PSI-2
0
0.01
0.02
0.03
0
20
40
60
80
100
He ion fraction [%]
Sputtering yield
Discrepancy also for pure He plasma  rough grass-like surface still present
rough grass-like structure
Calculation (TRIM code)
for flat surface
Experiment
escaping sputtered particles
trapped
sputtered
particles
Influence of surface roughness on effective sputtering
Pure D: Rough Al surface
5 m
Pure He: Rough Al surface
5 m
Rough grass-like structures can significantly reduce effective sputtering yield

## Slide 13: Deuterium retention in Be and Al under influence of argon and helium
Different TDS spectra of Al and Be
  Typical several-peak structure for beryllium incl. low-temperature supersaturation peak
  Single broad peak for aluminium
Different behaviour of retention Al and Be under influence of argon
Aluminium cannot be used as beryllium surrogate for fuel retention studies
Deuterium retention in beryllium studied in PISCES-B
Deuterium retention in aluminium studied in PSI-2

## Slide 14
Deuterium retention in tungsten as function of incident ion flux
Incident ion flux for this study:
Magnum-PSI  51023 m-2s-1
PSI-2  11022 m-2s-1
Incident ion fluence kept constant by longer exposures in PSI-2 !

## Slide 15: Blister formation in tungsten by deuterium irradiation at high surface temperatures
[L. Buzi et al., J. Nucl. Mater. 455 (2014) 316]
SEM images of tungsten exposed to
low flux in PSI-2
high flux in Magnum-PSI
No blisters
At high flux, blistering occurred for Ts > 800 K !

## Slide 16: Blistering and deuterium retention in tungsten exposed to different ion fluxes
500
600
700
800
900
10
20
10
21
10
22
Deuterium retention [m-2]
Sample temperature [K]
Domain of blister formation
Deuterium retention for different ion fluxes and sample temperatures (total fluence kept constant!)
Magnum-PSI: flux 51023 m-2s-1
PSI-2: flux 1022 m-2s-1
The presence of blisters correlates with the total amount of retained deuterium
At low and moderate exposure temperatures: higher retention for lower flux
At high exposure temperatures: higher retention for higher flux
[L. Buzi et al., J. Nucl. Mater. 455 (2014) 316]

## Slide 17
Deuterium retention in tungsten under influence of helium and argon

## Slide 18: Deuterium retention in tungsten under influence of helium and argon
0
200
400
600
800
0
1
2
3
4
5
6
7
8
D
D + 1% He
D + 5% He
Effect of helium:
Total deuterium retention is reduced by a factor of 3
Nano-size bubbles observed by TEM in depth up to ~10 nm
Effect of argon:
Total deuterium retention slightly increased
TDS spectra show different shapes
  Change in trapping sites due to material damage by argon
[M. Reinhart et al., PSI 2014 Kanazawa, submitted to JNM]
Thermal desorption spectra (TDS) of tungsten exposed to mixed plasmas
Total amount of deuterium retained in exposed tungsten
D release rate [1017 m-2s-1]
Desorption temperature [C]
Desorption temperature [C]
D release rate [1017 m-2s-1]
0
200
400
600
800
0
1
2
3
4
5
6
7
8
D
D + 2% Ar
D + 6% Ar
0.4 K/s ramp
0.4 K/s ramp
0
1
2
3
4
5
6
7
8
0
1
2
3
4
5
Deuterium retention [1020 m-2]
D + He
D + Ar
Impurity ion fraction [%]

## Slide 19: Conclusions
Beryllium
Erosion of beryllium and aluminium exhibits similar features
  Pure D plasma: Fine-scale grass-like structures, reduced measured sputtering yield than calculated (factor ~10)
  Addition of Ar: Grass-like structures are suppressed, sputtering increases to calculated values
Mechanisms of deuterium retention in aluminium are different than in beryllium
Tungsten
Relation of retention for low and high fluxes is temperature-dependent
Blistering occurred for high flux at surface temperatures of >800 K
Helium significantly reduces deuterium retention in tungsten, while argon slightly increases it

## Slide 20: Jülich beyond TEXTOR: integral concept on plasma-material interaction in nuclear environment
Development and integrated characterization of thermo-mechanical and physical-chemical properties of neutron irradiated and toxic plasma-facing materials under high heat loads and plasma exposure
Focus on material optimization for plasma-material interaction processes (tritium retention, embrittlement, erosion)
JULE-PSI linear plasma device (in construction for HML)
PSI-2 linear plasma device (operational outside HML)
JUDITH 1 and JUDITH 2 HHF e-beam facilities
Nuclear infrastructure (Hot Material Labs)
available at FZJ

## Slide 21
Backup slides

## Slide 22: Mechanisms of reduction of Be and Al sputtering in deuterium plasma and effect of argon
Sputtering yield from mass loss measurements in comparison to calculations in binary collision approximation
 | Sputtering yield (Experiment) | Ratio Experiment/TRIM*
Pure D | 1.410-3 | 0.05
3% Ar | 3.110-3 | 0.1
10% Ar | 9.210-3 | 0.3
Pure Ar (0.75 Ar+ + 0.25 Ar2+) | 4.110-3 | 0.9
For pure D exposure, reduced sputtering can be explained by following effects [Doerner et al., J. Nucl. Mater. 438 (2013) S272]
Enhanced prompt re-deposition on rough surface  a reduction factor of 2-3
Protecting effect of D incorporated in Be (by dilution and less efficient change of momentum direction of incident particles necessary for sputtering)  TRIM calculations predict for D/Be = 50% a reduction factor of 4
Two-fold effect of Ar leading to higher erosion of Be by D
Reduction of surface roughness  Less prompt re-deposition
Reduced D retention in Be target  Less efficient protecting effect of D

## Slide 23: Mechanism of development of grass-like structure
Model proposed by R.P. Doerner et al., J. Nucl. Mater. 455 (2014) 1
Y. Yamamura et al., "Angular Dependence of Sputtering Yields of Monatomic Solids", Report No. IPPJ-AM-26, 1983:
f and Σ are parameters for fitting of empirical formula to experimental data
Incident angle on the grass-like structure vs. angle for Y(θ)= 0.5·Y(0):
 | Be (PISCES-B) | Be (model) | Al (model)
Deuterium | 85.0° | 84.8° | 85.5°
Helium | 80.5° | 80.2° | 81.0°
Argon | - | 74.2° | 74.4°
0
20
40
60
80
0.0
0.5
1.0
1.5
2.0
2.5
3.0
3.5
Argon
Helium
Y()/Y(0)
Incident angle  []
Aluminium
Beryllium
Deuterium