## Slide 1
IAEA International Conference
16-20 November 2015
Nikolay Kardjilov, André Hilger, Ingo Manke, John Banhart
Neutron Imaging in Science and Technology

## Slide 2
2
BER II
20 km
BESSY II
Introduction

## Slide 3
The continued development of unique instruments is a major focus of the HZB.
Every year, HZB’s user service enables some 2,500 external scientists (from 35 countries to date) to access measuring methods, which in some cases are quite unique.
The aim is to further the complementary use of neutrons and photons to gain a more complete picture of matter.
User service at HZB

## Slide 4
Institute of Applied Materials
Neutron
Micro CT Synchrotron
Imaging
n
x
Introduction
CONRAD-2
neutron tomography
MicroCT Lab
X-ray tomography
BAM-Line @ BESSY
Synchrotron tomography
3D-Analytics Lab

## Slide 5
Cold neutrons
Wavelength range: 1.5 Å – 10 Å
Large beam
Beam size: 20 cm x 20 cm
High flux
Flux (guide end): 2.7x109 n/cm2s
Instrumentation
Velocity selector
Double-crystal monochromator
Grating interferometry
Neutron polarizers
Labs
Micro-CT Lab
3D Data Analytics Lab
CONRAD-2

## Slide 6
History
2003

## Slide 7
History
2005

## Slide 8
Design phase: 2003 – 2004
Construction phase: 2004 – 2005
Operation: July 2005 – Nov. 2010
Total investment: 250 k€
(shielding + equipment)
CONRAD at HZB
History

## Slide 9
V7 CONRAD
Beam size: 10 cm x 10 cm
Neutron flux: 107 n/cm2s
Maximal sample size: 20 cm
Beam size: 20 cm x 20 cm (x4.0)
Neutron flux: 2x107 n/cm2s (x2.0)
Maximal sample size: 50 cm (x2.5)
V7 CONRAD (Upgrade program)
Gain
longer beam path
better neutron guide
larger curvature of the neutron guide
Upgrade

## Slide 10
10 m
2.6 m
Design
Top view
Sandwich type shielding based on 5 mm B4C and 5-10 cm Pb.

## Slide 11
Construction

## Slide 12
Construction

## Slide 13
Construction

## Slide 14
Construction

## Slide 15
Before
After Upgrade
Larger beam
Before upgrade: 2.0x108 n/cm2s
After upgrade: 2.7x109 n/cm2s
Intensity at the end of the guide:

## Slide 16
  Diffusion dynamics revealed with D-H contrast
  Understanding of ageing mechanisms
  M. Klages Journal of Power Sources 239 (2013) 596
Neutron Imaging @ V7(CONRAD-2)
In-operando visualization of water distribution
Quantification of water amount
Diffusion dynamics revealed with D-H contrast
  How to optimize water management in a PEM fuel cell?
1 mm
Attenuation Contrast
Fuel cells
10 mm

## Slide 17
I. Manke et al, APL 92,
(2008)
A.Schröder et al, Electrochem Commun (2009)
A. Schröder et al, J Power Sources 195 (2010)
C. Tötzke et al, J Power Sources 196 (2011),
A. Lange et al, J Power Sources 196 (2011)
R. Kuhn et al, Int J Hydrogen Energy 37 (2012)
H. Markötter et al, J Power Sources 219 (2012)
0.5
1.0
Current density
(A/cm2)
0.0
15 cm
H2/D2 contrast radiography
water thickness
1 cm
Fuel cells
Attenuation Contrast

## Slide 18
Attenuation Contrast
low
absorption
medium
absorption
(metal)
high
abs.
3
2
1
1+2
2
2
2+3
1
2
1+2
2+3
Time scale
1 – old sediments
3 – fresh sediments
volume histogram
Combustion chamber

## Slide 20
Diffraction Contrast
λ = 4.0 Å
1 cm

## Slide 21: Bragg edges
dhkl
2dhklsinθ=
polychromatic
neutron beam
polycrystalline
material
Bragg‘s law
DCM

Diffraction Contrast

## Slide 22
polychromatic
neutron beam
DCM

2dhklsin90°=
dhkl
2dhkl=
(110)
polycrystalline
material
Bragg‘s law
Cross-sections of iron per atom
Diffraction Contrast
Bragg edges

## Slide 23: 3D Phase mapping in metals
Energy-selective neutron tomography of TRIP-steel
R. Woracek et al., Advanced Materials 26 (2014)

## Slide 24
Phase/Dark-field Contrast
2 mm

## Slide 25
The spatially resolved analysis of the interference pattern (phase, amplitude and offset) reveal information about phase effects, small angle scattering and attenuation introduced by the sample.
Phase/Dark-field Contrast
C. Grünzweig et al, PRL (2008)

## Slide 26
3D domain distribution
G0
G1 G2
Neutrons
Detector
Sample
xG
Source
grating
Phase
grating
Analyser
grating
Multiple refractions at the domain walls results in local degradation of the beam coherence (decrease of the amplitude in the interference pattern).
Magnetic domains in a bulky FeSi single crystal
I. Manke et al, Nature Communications (2010)
Magnetic domain structure can be visualized in 3D by applying tomographic reconstruction from 2D angular projections
Phase/Dark-field Contrast

## Slide 27
Magnetic Contrast
1 cm

## Slide 28
Experimental parameters
Solid state polarazing benders
Beam size (WxH): 20 x 4 cm2
Exposure times: ~10 min / image
1 cm
N. Kardjilov, et al, Nature Physics (2008)
Principle
Magnetic Contrast

## Slide 29
Flux pinning in superconductors
6.8 K
7.0 K
7.2 K
6.9 K
1 cm
trapped flux
Pb cylinder
(polycrystalline)
T
7.196 K (Tc)
7.0 K
Flux pinning at cooling down below Tc while applying a homogenous magnetic field of 10 mT perpendicular to the beam.
The images were recorded after switching off the magnetic field.
Magnetic Contrast

## Slide 30
Flux pinning in superconductors
6.8 K
7.0 K
7.2 K
6.9 K
1 cm
trapped flux
Pb cylinder
(polycrystalline)
T
7.196 K (Tc)
7.0 K
Magnetic Contrast
Flux pinning at cooling down below Tc while applying a homogenous magnetic field of 10 mT perpendicular to the beam.
The images were recorded after switching off the magnetic field.

## Slide 31
Spatial Resolution

## Slide 32
Detector system
Introduction
400
300
200
100
Standard setup (2006)
Scintillator: 200 µm 6LiF
Lens system: 50 mm
Pixel size: 100 µm
Exposure time: 20 s
µm
500
Spatial Resolution

## Slide 33
Camera: Andor DW436
Lens system: Magnification
Pixelsize = 3.375 µm
Szintillator: 5 µm Gadox
Resolution: 7.9 µm (63.2 lp/mm)
Spatial Resolution
2 mm
S. H. Williams et al,
Journal of Instrumentation (2012)

## Slide 34
Resolution: 15 µm (pixel size: 6.5 µm), FOV: 13 x 13 mm2, Exp. Time: 20 s
50 µm
Hydrogen storage (MHGC Ti-Mn)
(L. Röntzsch, IFAM, Dresden, Germany)
Neutron tomography
Spatial Resolution
1 mm

## Slide 35
5 mm
Hydrogen loading of duplex stainless steel
(A. Griesche, BAM, Berlin, Germany)
Electrochemically loading
H2 (~ 100 ppm)
Spatial Resolution
A. Griesche et al., Acta Materialia 78 (2014)

## Slide 36
Conclusions
Over the last 10 years, significant developmental work has been performed to expand the radiographic and tomographic capabilities of the neutron imaging facility at HZB.
New techniques have been implemented, including imaging with polarized neutrons, Bragg-edge mapping, high-resolution neutron imaging and grating interferometry.
These methods have been provided to the user community as tools to help addressing scientific problems over a broad range of topics such as superconductivity, materials research, life sciences, cultural heritage, paleontology and various others.

## Slide 37
Thank you!