## Slide 1: Experiments on FTU with a liquid tin limiter
For the first time a tin limiter has been tested on a tokamak device
Capillary Porous system based tin experiments are promising and indicate high heat exhaust capability.
Up to 18 MW/m2 were measured on the liquid tin limiter during FTU pulse for more than 0.5 s
Low plasma contamination and no plasma degradation have been observed with tin also in the case of strong evaporation nTin/ne≈1x10-4
Liquid metal seems a viable solution to the power exhaust problem
Paper FIP/3-5Rb
The Tin limiter
From the top, the electron density ne,LP, the electron temperature Te,LP and the heat loads qLP versus time are shown for two pulses.
Increased density -Increased heat load