## Slide 1: Improvement of Cu Alloys as Divertor Heat Sink Material
Armor Materials
Pipe
Heat Sink Materials
Example Design for Divortor
Stable Nano-oxide particles in matrix
Suppression of dislocation motion
Improvement of the strength and resistance to irradiation
Dispersed
particles
Matrix
(Cu)
μm
Dislocation
The increase in oxygen concentration improved mechanical properties
(Oxide) Dispersion Strengthening method
Application of Dispersion Strengthening by Mechanical Alloying (MA) and Hot Isostatic Press (HIP) to Copper Alloys
Chart: Tensile Stress (MPa)
| Cu-Al including Low oxygen concentration | Cu-Al including High oxygen concentration | Cu-Zr including Low oxygen concentration | Cu-Zr including High oxygen concentration
UTS | 0 | 365.8 | 246.0255 | 357.7321
Oxygen concentration(Cu-Al) | 0.052 | 1
Oxygen concentration(Cu-Zr) | 0.092 | 0.31
A new process, addition of oxidant(CuO) during the MA, increased the density of oxide particles.
1.Effect of oxygen concentration for Cu-Al and Cu-Zr
2.n-situ fabrication of Cu-Y2O3 alloy